## Slide 1
Sebastian T. B. Goennenwein
Walther-Meißner-Institut, Bayerische Akademie der Wissenschaften
M. Althammer, F. D. Czeschka, J. Lotze, S. Meyer, M. Schreier, M. Weiler, S. Geprägs, M. Opel, H. Huebl, R. Gross, Walther-Meißner-Institut
E. Saitoh and G.E.W. Bauer & groups Institute for Materials Research, Tohoku U, Japan, Kavli Institute of NanoScience, TU Delft, NL
J. Xiao & group, Fudan U, Shanghai
Y. Tserkovnyak & group, UCLA, USA
M. Kläui & group, Uni Mainz
Financial support: Deutsche Forschungsgemeinschaft via SPP 1538 “SpinCAT” (GO 944/4) and Excellence Cluster NanoSystems Initiative Munich
Spin Currents
in Magnetic Insulator / Normal Metal Heterostructures

## Slide 2
Spin electronics = putting a spin to electronics ?
electron =
electronics (charge-tronics):
… ONLY charge
… charge currents in electrical conductors
charge current sources
charge current detectors
charge amplification
spin
charge
Intel Core i7
IBM
spin-tronics:
… ONLY spin
… spin currents
in “angular momentum conductors”
spin currents ?
spin current sources ?
spin current detectors ?
spin current gain ?
magneto-electronics:
… charge AND spin … spin-polarized currents in electrical conductors

## Slide 3: From charge currents to spin currents
J=J + J

## Slide 4: From charge currents to spin currents
J=J + J
Volta
Schulhistorische Sammlung, Bremerhaven
Ørsted
wikipedia

## Slide 5: From charge currents to spin currents
J=J + J
(J- J)
?
?
Intel Core i7
spin current source ?
spin current meter ?
…this talk:
F/N hybrids !

## Slide 6: From charge currents to spin currents
J=J + J
(J- J)
?
?
Intel Core i7
spin current source ?
spin current meter ?
JS can also flow in electrical insulators, as a
magnon (spin) current !

## Slide 7
spin current detection
(in metals with s-o coupling)

## Slide 8: The spin Hall effect (SHE) : spin – charge current conversion
Spin Hall effect
  spin-orbit coupling: interaction between spin and charge motion
  spin Hall angle SHE parameterizes charge current  spin current conversion efficiency
direct spin Hall effect (SHE)
inverse spin Hall effect (ISHE)
charge current spin current
spin current charge current

## Slide 9: Direct spin Hall effect in GaAs
Kerr microscopy
(„spin imaging“)
Kato et al., Science 306, 1910 (2004).
-Jc
Js

Notes: one of the first experiments getting …

## Slide 10: The spin Hall effect (SHE) : spin – charge current conversion
Spin Hall effect
  spin-orbit coupling: interaction between spin and charge motion
  spin Hall angle SHE parameterizes charge current  spin current conversion efficiency
direct spin Hall effect (SHE)
inverse spin Hall effect (ISHE)
charge current spin current
spin current charge current

## Slide 11: iSHE in Metallic F/N Nanostructures
Aluminium:
Valenzuela & Tinkham, Nature 442, 176 (2006).
detection of diffusive spin current
via inverse spin Hall effect
Js
-Jc
Js
Al
FM1
LSH
Gold : SHE=0.0016
Platinum : SHE=0.013 … 0.11 (0.16)
Bi, Bi/Ag, Ta : SHE=0.1 … 0.3
Valenzuela & Tinkham, Nature 442, 176 (2006).
Mosendz et al., Phys. Rev. Lett. 104, 046601 (2010).
Liu et al., Science 336, 555 (2012).
Niimi et al., Phys. Rev. Lett. 109, 156602 (2012).
…and many more …
Notes: non-local due to :
spin polarisation is not a conserved quantity  diffusion in both direction
no magnetic contacts: stray fields, interface problems
Non-local
magnetic probes
Aluminium

## Slide 12: iSHE in Metallic F/N Nanostructures
Aluminium:
Valenzuela & Tinkham, Nature 442, 176 (2006).
detection of diffusive spin current
via inverse spin Hall effect
Js
-Jc
Js
Al
FM1
LSH
Gold : SHE=0.0016
Platinum : SHE=0.013 … 0.11 (0.16)
Bi, Bi/Ag, Ta : SHE=0.1 … 0.3
Valenzuela & Tinkham, Nature 442, 176 (2006).
Mosendz et al., Phys. Rev. Lett. 104, 046601 (2010).
Liu et al., Science 336, 555 (2012).
Niimi et al., Phys. Rev. Lett. 109, 156602 (2012).
…and many more …
take away:
SHE enables “simple” experimental spin current detection (… given the spin Hall angle SHE and the spin diffusion length SF are known ! )
Notes: non-local due to :
spin polarisation is not a conserved quantity  diffusion in both direction
no magnetic contacts: stray fields, interface problems
Non-local
magnetic probes
Aluminium

## Slide 13: From charge currents to spin currents
J=J + J
(J- J)
Volta
ISHE
Schulhistorische Sammlung, Bremerhaven
Ørsted
Hirsch
(1999)
?

## Slide 14: From charge currents to spin currents
J=J + J
(J- J)
Volta
ISHE
Schulhistorische Sammlung, Bremerhaven
Ørsted
Hirsch
(1999)
magnetic excitations
@F/N interface
?

## Slide 15
spin current generation
(in ferromagnet / metal hybrid structures)

## Slide 16: Spin currents in hybrid structures
ferromagnet

## Slide 17: Spin currents in hybrid structures
„normal“ metal
ferromagnet

## Slide 18: Spin currents in hybrid structures
Weiler et al., PRL 111, 176601 (2013).
„normal“ metal
ferromagnet
(out of equilibrium)

## Slide 19: Spin currents in hybrid structures
„normal“ metal
ferromagnet
(out of equilibrium)
Weiler et al., PRL 111, 176601 (2013).

## Slide 20: Spin currents in hybrid structures
coherent phonons: Bömmel & Dransfeld, PR 117, 1245 (1960).
Weiler et al.,
PRL 106, 117601 (2011). PRL 108, 176601 (2012).
Uchida et al., Nature 455, 778 (2008). Jaworski et al., Nature Mater. 9, 898 (2010).
Uchida et al., Nature Mater. 9, 894 (2010).
Weiler et al., PRL 108, 106602 (2012) .
Gepraegs et al., APL 101, 262407 (2012).
Schreier et al., PRB 88, 094410 (2013).
Schreier et al., APL 103, 242404 (2013).
Roschewsky et al., APL 104, 202410 (2014). Geprägs et al.,arXiv:1405.4971
Tserkovnyak et al., PRL 88, 117601 (2002). Saitoh et al., APL 88, 182509 (2006).
Mosendz et al., PRL 104, 046601 (2010).
Czeschka et al., PRL 107, 046601 (2011).
Bai et al., PRL 114, 227201 (2015).
Weiler et al., PRL 108, 106602 (2012) .
Huang et al., PRL109, 107204 (2012).
Nakayama et al., PRL 110, 206601 (2013).
Chen et al., PRB 87, 144411 (2013).
Althammer et al., PRB 87, 224401 (2013).
Vlietstra et al., PRB 87, 184421 (2013).
Hahn et al., PRB 87,174417 (2013).
Lotze et al., PRB 90, 174419 (2014).
Weiler et al., PRL 111, 176601 (2013).

## Slide 21: Spin currents in hybrid structures
coherent phonons: Bömmel & Dransfeld, PR 117, 1245 (1960).
Weiler et al.,
PRL 106, 117601 (2011). PRL 108, 176601 (2012).
Weiler et al., PRL 108, 106602 (2012) .
Huang et al., PRL109, 107204 (2012).
Nakayama et al., PRL 110, 206601 (2013).
Chen et al., PRB 87, 144411 (2013).
Althammer et al., PRB 87, 224401 (2013).
Vlietstra et al., PRB 87, 184421 (2013).
Hahn et al., PRB 87,174417 (2013).
Lotze et al., PRB 90, 174419 (2014).
Weiler et al., PRL 111, 176601 (2013).
Uchida et al., Nature 455, 778 (2008). Jaworski et al., Nature Mater. 9, 898 (2010).
Uchida et al., Nature Mater. 9, 894 (2010).
Weiler et al., PRL 108, 106602 (2012) .
Gepraegs et al., APL 101, 262407 (2012).
Schreier et al., PRB 88, 094410 (2013).
Schreier et al., APL 103, 242404 (2013).
Roschewsky et al., APL 104, 202410 (2014). Geprägs et al.,arXiv:1405.4971
Tserkovnyak et al., PRL 88, 117601 (2002). Saitoh et al., APL 88, 182509 (2006).
Mosendz et al., PRL 104, 046601 (2010).
Czeschka et al., PRL 107, 046601 (2011).
Bai et al., PRL 114, 227201 (2015).

## Slide 22
Spin Seebeck Effect
in magnetic insulator / metal hybrid structures

## Slide 23
longitudinal SSE
magnetic insulator / N
( YIG / Pt )
Uchida, Saitoh et al.,
Nature 455, 778 (2008).
Nature Mater. 9, 894 (2010).
APL 97,172505 (2010). ….
Spin Seebeck effect (SSE)

## Slide 24
longitudinal SSE
magnetic insulator / N
( YIG / Pt )
Uchida, Saitoh et al.,
Nature 455, 778 (2008).
Nature Mater. 9, 894 (2010).
APL 97,172505 (2010). ….
M
Spin Seebeck effect (SSE)

## Slide 25: Spin Seebeck effect (SSE)
Weiler et al., PRL 108, 106602 (2012). Schreier et al., APL 103, 242404 (2013). Roschewsky et al., APL 104, 202410 (2014).
heat baths
(local) laser heating
Joule current heating
many groups around the world
use this „thermoelectric approach“

## Slide 26: Spatially resolved spin Seebeck experiments
… inspired by EPFL, e.g.: Gravier, Ansermet et al., EPL 77, 17002 (2007).
YIG
Pt

## Slide 27: Spatially resolved spin Seebeck experiments
… inspired by EPFL, e.g.: Gravier, Ansermet et al., EPL 77, 17002 (2007).

## Slide 28: Optical imaging ( = reflected intensity )
1 pixel = 12.5 m  12.5 m
1 pixel = 2 m  2 m
YIG
Pt

## Slide 29: Optical imaging ( = reflected intensity )
1 pixel = 12.5 m  12.5 m
1 pixel = 2 m  2 m

## Slide 30: Spatially resolved spin Seebeck effect in YIG/Pt bilayers
optical
H

## Slide 31: Spatially resolved spin Seebeck effect in YIG/Pt bilayers
optical
H
VISHE  spin Seebeck effect

## Slide 32: SSE in YIG(20nm)/Pt(7nm) bilayer
 local emf
H
0H = - 70 mT
room temperature

## Slide 33: SSE in YIG(20nm)/Pt(7nm) bilayer
H
local, bipolar,
magnetically controllable emf
0H = + 70 mT
room temperature

## Slide 34: SSE in YIG(20nm)/Pt(7nm) bilayer
H
Weiler et al., PRL 108, 106602 (2012).

## Slide 35: SSE in YIG(20nm)/Pt(7nm) bilayer
Weiler et al., PRL 108, 106602 (2012).

## Slide 36: SSE in YIG(20nm)/Pt(7nm) bilayer
Weiler et al., PRL 108, 106602 (2012).
Spin Seebeck effect:
thermally driven spin currents give rise to local, bipolar, M-controllable emf
electrically detected magnetometry of magnetic insulators
? SSE mechanism

## Slide 37: Time-resolved SSE
… how quickly can we modulate
the laser power and still
observe a “DC” SSE signal ?

## Slide 38: Time-resolved SSE
Garching:
YIG(55nm)/Pt(<20nm) samples
SSE signal unaltered
up to at least 30MHz
 SSE time constant < 5 ns
Roschewsky et al., APL 104, 202410 (2014).
Kaiserslautern:
YIG(6700nm)/Pt(10nm) sample SSE signal exhibits time dep.  SSE time constant of 570 ns
Agrawal et al., PRB 89, 224414 (2014).

## Slide 39: Spin currents: towards (more complex) spin textures
spin current (e.g., SSE)
=
ferri- magnet
… do spin currents „simply“ mirror the net magnetization ?

## Slide 40: Spin Seebeck Effect in GdIG/Pt
Geprägs et al., arXiv: 1405.4971

## Slide 41: Conclusions
pure spin currents spin Hall effect inverse spin Hall effect
spin Seebeck effect (SSE):
spin-current induced thermopower voltage in a nonmagnetic metal (Pt), governed by M in insulating FM (YIG)
… what is the SSE time constant ?
… spin currents DO NOT „simply“ mirror the net magnetization