## Slide 1
Accelerator-Based Isotope Production at TRIUMF
June 16th, 2015
CAP Conference
Paul Schaffer
Head, Nuclear Medicine
TRIUMF

## Slide 2: Accelerators at TRIUMF
ISAC (RIB linac)
ARIEL
(50 MeV
electron linac)
2 x TR30, CP42, TR13
H- cyclotrons
500MeV
H- cyclotron
New addition: TR24; to be installed

## Slide 3: CP42, TR30, TR13 Operations
TRIUMF Capabilities:
CP42: up to 42 MeV and 200 µA, installed 1980
TR30-1: up to 30 MeV and 900 µA, installed 1990
  first TR30 designed, assembled by TRIUMF, components manufactured by EBCO, commissioned by TRIUMF
TR30-2: up to 30 MeV and 1000 µA, installed 2003
  Manufactured, installed by EBCO, commissioned by TRIUMF
TR13: 13 MeV, 25A, installed 1986 (UBC Neurology)
  Capable of 11C, 18F, 13N, 68Ga, 89Zr, 64Cu, 44Sc, 86Y, 55Co, 52Mn…solid, liquid, gas targets
TR24: 24 MeV, 500+ A, to be installed
Overall
  5 solid target, 3 gas stations operating at 30 MeV
    Commercial production: 67Ga, 111In, 123I, 103Pd, 201Tl
  Future commercial production: 99mTc

## Slide 4
Direct, multi-Curie production of 99mTc on three different cyclotrons
1) TRIUMF
2) University of British Columbia;
3) BC Cancer Agency;
4) Lawson Health Research Institute;
5) Centre for Probe Development and Commercialization

## Slide 5
100Mo(p,2n)99mTc
graphic from http://www.covidien.com/
LEU 235U(n,F)
Alternatives:
98Mo(n,)99Mo
238U(,F)99Mo
100Mo(,n)99Mo
Tc-99m Alternatives: Many options
99Mo/99mTc in high demand (~ 40M doses/yr)
Gov’t owned reactors produce majority of 99Mo supply
NRU going offline Oct. 2016 (~40% of global supply)
Capacity emerging (existing reactors, new technology
Projections range from oversupply to shortages1
Must move to full-cost recovery
1) OECD - NEA/SEN/HLGMR(2014)2
5
Notes: Direct on-target production of Tc-99m has already been accomplished through proof-of-principle experiments – bypasses need for generator
Similar approach can be used for Tc-94m since only difference is target material

## Slide 6: Cyclotrons By the Numbers
Estimated global cyclotron numbers by various manufacturers
(with data from ACSI, GE, IBA and Siemens, Sumitomo data estimated)
Schaffer et al. Phys. Proc. in press (2014).
6

## Slide 7: Direct Production of 99mTc
100Mo Target
Goals:
  Demonstrate routine, reliable, commercial-scale production of 99mTc via 100Mo(p,2n) at multiple sites, multiple brands;
  Obtain regulatory approval for clinical use in humans;
  Establish a business plan;
  Disseminate, commercialize the technology
Hypothesis: Future production will be from variety of sources (neutron, proton, electron) and market driven
Cyclotron Modification
Optimize Irradiation
Purify 99mTcO4
Regulatory QA/QC
100Mo Recovery
J. Beaver, H. Hupf, J Nucl Med 1971;12:739-741
7

## Slide 8: Target Manufacturing
100Mo Target
Cyclotron Modification
Optimize Irradiation
Purify 99mTcO4
Regulatory QA/QC
100Mo Recovery
Schaffer et al. Phys. Proc. in press (2015).
Zeisler et al. WTTC 2014
Press-Sinter-Braze
Electrophoretic deposition
Maximizing 99mTc production, minimizing impurities:
  <19 MeV proton energy entering 100Mo
  >8 MeV proton energy exiting 100Mo
  Stopping power of Mo: Requires <1.2 g of metal
  Reduce density, balance thermal conductivity
8

## Slide 9: Retrofit Existing Infrastructure
100Mo Target
Cyclotron Modification
Optimize Irradiation
Purify 99mTcO4
Regulatory QA/QC
100Mo Recovery
PETtrace
TR19
TR30
9
Notes: TR19: Upgrade included new beamline, 300 uA capabilities
PETtrace: 130 uA capabilities (limited by regulator), technically 160 uA, some components

## Slide 10: Target Type vs. Cyclotron Power
100Mo Target
Purify 99mTcO4
Regulatory QA/QC
100Mo Recovery
TR30 (@24 MeV) target power: 10.8 kW @ 0.6 kW/cm2
TR19 target power: 5.4 kW @ 0.3 kW/cm2
PETtrace target power: 2.1 kW @ ~1.2 kW/cm2
Optimize Irradiation
Cyclotron Modification
10
Notes: TR19: Upgrade included new beamline, 300 uA capabilities
PETtrace: 130 uA capabilities (limited by regulator), technically 160 uA, some components

## Slide 11: Real and Projected Yields of 99mTc
100Mo Target
Cyclotron Modification
Optimize Irradiation
Purify 99mTcO4
Regulatory QA/QC
100Mo Recovery
GE PETtrace
16.5 MeV, 130 μA
Theoretical 4.9 Ci (6h)
Achieved 4.7 Ci
Satn: 75.6 mCi/µA
TR19
18 MeV, 300 μA
Theoretical 15.4 Ci (6h)
Achieved 9.4 Ci (@ 240 µA)
Satn: 103 mCi/µA
TR30 (@24 MeV)
24 MeV, 500 μA
Theoretical 39 Ci (6h)
Achieved ~32 Ci (@ 450 µA)
Satn: TBD

## Slide 12: Purification of 99mTc
100Mo Target
Cyclotron Modification
Optimize Irradiation
Purify 99mTcO4
Regulatory QA/QC
100Mo Recovery
SPE-based method:
  original work: Dowex™ vs ABEC
  new alternative resin: ChemMatrixTM
Process Time: complete in <90 min.
Efficiency Range: 92.7 ± 1.1%
Radiochemical Purity: >99.99% TcO4
Trace analysis: <10 Bq Mo-99, <5 ppm Al3+
non-Tc impurities removed
Disposable fluid path for GMP
Morley et al. Nuc. Med. Biol. 2012, 551-559
Inherent Resin Versatility: Vendor Agnostic
12

## Slide 13: Regulatory Process: CTA nearly complete
100Mo Target
Cyclotron Modification
Optimize Irradiation
Purify 99mTcO4
Regulatory QA/QC
100Mo Recovery
Not currently approved by Health Canada, FDA, etc.
CTA preparation underway:
  GLP preclinical rodent data (complete);
  documentation (complete),
  acceptance criteria: RNP, RCP, Al, Mo, H2O2 (complete);
  process validation (complete)
Shelf life (18 hrs), irradiation parameters are based on projected patient dose (objective <10% add’l vs. pure 99mTc)
  Enrichment and irradiation parameters are interrelated and should not be considered independently
CTA submission – June 2015 (60 patient trial)
Fall 2015 - NDS submission
13

## Slide 14
100Mo Raw Material/Irradiation Specifications
1Maximum increase in patient dose of 9.8 % at 20 MeV, 18 hours after EOB.
2Maximum increase in patient dose of 10.1% at 22 MeV, 18 hours after EOB.
3Maximum increase in patient dose of 10.6% at 24 MeV, 18 hours after EOB.
Based on theoretical yield calculations with 99mTc pertechnetate
Mitigates the impact of dose due to 98Mo(p,3n)96Tc reaction at higher E
Isotope | Proposed max. isotopic impurity to maintain patient dose increase of ~10% compared to pure 99mTcO4 |  | 
 | ≤ 20 MeV1 | 20 – ≤22 MeV2 | 22 - ≤24 MeV3
92Mo | 0.03 | 0.03 | 0.02
94Mo | 0.03 | 0.03 | 0.02
95Mo | 0.03 | 0.03 | 0.02
96Mo | 0.03 | 0.03 | 0.02
97Mo | 0.03 | 0.03 | 0.02
98Mo | 7 | 0.8 | 0.5
14

## Slide 15: We Recycle
100Mo Target
Cyclotron Modification
Optimize Irradiation
Purify 99mTcO4
Regulatory QA/QC
100Mo Recovery
High efficiency recovery process for multi-gram quantities of
100MoO42- required
Some trace long-lived radionuclidic impurities
Target dissolution waste stream (liquid, 10’s of mL/batch)
Original method: ion exchange
>90% efficiency (non-optimized), large column volumes, slow
Currently using acidic precipitation, thermal decomp. process
Routine recovery yields >99%
Analysis of recovered 100Mo underway

## Slide 16: Remaining Challenges for Cyclotron Production of 99mTc
Process: Long-term reliability (machine and target)
Quality Control: Decentralized production inherently leads to a greater likelihood of product variability, dose uncertainty
Regulatory: Considerations need to include target isotopic enrichment, but also batch-to-batch target consistency, irradiation energy/duration, shelf-life (patient dose)
Economic: Arguments in one region may not apply in others but FCR must apply
Availability: A viable alternative/backup needs to be used regularly
16

## Slide 17
Production, Purification and Radiolabelling of Radiometals Produced in a Liquid Target on a 13 or 19 MeV Medical Cyclotron
Notes: Change pictures

## Slide 18: Proposal
Hypothesis: Established cyclotron centers can obtain research, and possibly clinical quantities of various radiometals by irradiating salt solutions in modified liquid targets
  Leverage existing liquid target infrastructure for the production of other PET isotopes (18F)
Accepted trade-off:
Lower production yields in exchange for isotope versatility
Vogg ATJ, et al. Proceedings of the Sixth International Conference on Nuclear and Radiochemistry,
2004; Aachen, Germany.
Jensen M, Clark J. Proceedings of the 13th International Workshop on Targetry and Target Chemistry,
Roskilde, Denmark, July 26-28, 2010.
DeGrado TR, et al. J Label Compound Radiopharm 2011. 54, S248
18

## Slide 19: Project Goals
Goals:
  Allow broader access to a variety of radiometallic isotopes
  Radiometal production without generators, solid-target installation
  Enable faster optimization of vector-isotope pairing
19

## Slide 20: Isotope-Biomolecule Pairing
biomolecule
linker
M
chelate
Proposed application: labeling and in vivo analysis of novel proteins/peptides targeted toward HER2 variants/isoforms
  Larger/slower-clearing constructs  longer-lived isotopes
  Smaller/faster-clearing constructs  shorter-lived isotopes
*D Mitra D et al Mol Cancer Ther. 2009;8(8):2152-2162.
20

## Slide 21: Project Overview
Specific Interests:
  94Mo(p,n)94mTc (half-life: 52.5 min)
  44Ca(p,n)44Sc (half-life: 3.9 h)
  86Sr(p,n)86Y (half-life: 14.7 h)
  89Y(p,n)89Zr (half-life: 78.5 h)
  68Zn(p,n)68Ga (half-life: 68 min)
Approach:
  TRIUMF: TR13 (13 MeV, 20 µA), standard water target (testing, feasibility)
  BCCA: TR19 (19 MeV, 300 µA), large volume water target (application: HER216 binders)
  New target design (i.e. syphon targets)
21

## Slide 22
Assessing Feasibility: Cross-sectional Considerations
T1/2 = 68 min
T1/2 = 3.9 h
T1/2 = 14.7 h
T1/2 = 78.5 h
22

## Slide 23: Production Summary
Prod | Production route | Metal salt | Density (g/mL) | Beam current (μA) | Time (min) | Yield (MBq) | Sat. yield (MBq/ μA)
94mTc | 94Mo(p,n)94mTc | (NH4)6Mo7O24 | 1.66 | 5 | 60 | 110±20 | 40±6
44Sc | 44Ca(p,n)44Sc | Ca(NO3)2 | 1.55 | 7.6 | 60 | 5.55±0.22 | 4.6±0.3
68Ga | 68Zn(p,n)68Ga | Zn(NO3)2 | 1.65 | 6.8 | 60 | 275±1 | 68±5
 |  |  | 1.56 | 6.96 | 60 | 480±30 | 141±6
89Zr | 89Y(p,n)89Zr | Y(NO3)3 x HNO3 | 1.49 | 7.3 | 60 | 32±2 | 360±9
86Y | 86Sr(p,n)86Y | Sr(NO3)2 | 1.43 | 4.6 | 60 | 7.4±0.5 | 31±1
23
Notes: Here is the summarize of the irradiation conditions, yields and saturation yields for all the rest of salt solutions. For Y-86, Zr-89 and Tc-94m, the quantities produced using liquid target are enough for in vitro studies or a small animal scan. For Ga-68, we can achieve a yield of 212 MBq with one hour irradiation time, and we can certainly make more with longer beam time. The will produce enough activity for a human scan.

## Slide 24: Purification – All metals
Prod. | Irradiated metal salt | Column 1 | Column 2 | Final Eluate |  | 
 |  |  |  | Activity received from target (%) | Vol. (mL) | Eluent
44Sc | Ca(NO3)2 | DGA | - | 88 ± 6 (n = 5) | 2.5 | 0.05M HCl
68Ga | Zn(NO3)2 | AG 50W-X8 | DGA | 92 ± 8 (n = 3) | 1.0 | H2O
89Zr | Y(NO3)3 | Hydroxamate resin | - | 82 ± 5 (n = 4) | 0.75 | 1M Oxalic Acid
86Y | Sr(NO3)2 | DGA | - | 99 ± 4 (n = 3) | 1.0 | H2O
94mTc | (NH4)6Mo7O24 | ABEC-2000 | SCX/ Alumina | 70.9 ± 0.7 (n = 4) | 6.0 | saline
24
Specific activity: 44Sc (1.4 TBq/mol), 68Ga (5.2TBq/mol), 89Zr (0.015 TBq/mol),
86Y (0.41 GBq/mol, 94mTc ()

## Slide 25: Radiolabelling chemistry
Chart: ligand conc. (µM)
| 117.64705882352941 | 19.607843137254903 | 9.0909090909090917 | 4.7619047619047619
Y-86 DOTA-NHS-Ester | 95.289 | 94.7973 | 48.2607 | 20.141
Zr-89 DFO | 64.1349 | 74.5732 | 92.1535 | 97.138 | 98.5362
Ga-68 DOTA-NHS-Ester | 87.936 | 86.6683 | 63.118
Radiolabelling conditions |  |  |  | 
Isotope | Temperature | Time | pH | Buffer
Y-86 | 95 ⁰C | 30 min | pH=6 | 0.33M HEPES
Zr-89 | r.t. | 15 min | pH=7 | 
Ga-68 | 95 ⁰C | 10 min | pH=4 | 0.33M HEPES
25
Notes: Clearly, the radiolabelling with 68Ga did not give optimal results. Since the whole separation procedure for 68Ga needs to be optimized (it takes over an hour), no effort has been put into improving the radiolabelling yield for the here reported method.

## Slide 26: Preparation of Liquid Target Solutions
Gas evolution during irradiation = high target pressures in a closed target body
  Radiolysis of water, O2, H2
  1M nitric acid for natZn and natSr salt irradiations*
Compatibility between salt solutions and target components
  Havar foil (Co-based, Cr, Ni, Fe, W, Mo, Mn)
    Failed with Cl- salts (etching evident)
  Al vacuum foil (failed in boil tests)
  Target body (Al) – evidence of corrosion
    Switch to Nb target body
Precipitation
  Need thorough flushing protocol between runs
* Pandey MK, et al., Nucl. Med. Biol. 2014;41:309-16.

## Slide 27: Summary
A simple method for the production of research quantities of various radiometals using a modified liquid-target system.
Salt solutions of natural isotopic abundance were irradiated in a standard water target on our 13 MeV cyclotron for 60 min. After irradiation, all solutions were withdrawn from the target and purified using cation exchange or chelating resins.
Several isotopes (68Ga, 89Zr, 44Sc, 89Y, 94mTc) were produced in a standard water target on our 13 MeV cyclotron
Future work: labeling and biodistribution analysis of breast cancer (HER2) binders; novel target designs (higher production)
27
Notes: production parameters and yields listed in the table

## Slide 28
Production and assessment of radiotherapeutic isotopes

## Slide 29: 500 MeV Cyclotron Capabilities
Previous decade: routine operation at 220-250μA
Recently achieved:
Materials science, 500 MeV isotopes:
  BL1A (100μA)
ISAC program:
  BL2A (100μA)
Sr production:
  BL2C (100μA)
  Total (300μA)
BL1A
BL2A
BL2C
BL4
29

## Slide 30: Isotope Accelerator Program (ISAC): 50 kW ISOL Facility
Isotope production
via spallation of uranium:
Implementation of ISOL technique:
  Uranium carbide target
  480 MeV protons, 10 µA
  Various available ion sources
  ~2500:1 mass separation resolution (~106–109 ions/s)
  Ion energy = ~20-60 keV
Uranium carbide, thorium oxide
30

## Slide 31: Candidate α-emitters for therapy
Isotope | Half-life | Considerations | Production
149Tb | 4.2 h | Good chemistry, alt. isotopes | Spallation, heavy-particle accelerator
211At | 7.2 h | No stable isotope, Thyroid uptake | α-cyclotron
212Bi | 1.0 h | Renal uptake | Generator (224Ra/212Bi)
213Bi | 0.76 h | Renal uptake | Generator (225Ac/213Bi)
223Ra | 10 d | 4 α-decays, bone targeting | Generator (227Ac/223Ra)
225Ac | 10 d | 4 α-decays, | Generator (229Th/225Ac)
31

## Slide 32: 209At-based imaging to establish 211At α-therapy
211At t1/2= 7.2 h
209At t1/2= 5.4 h
Therapy
Imaging
(α-emitter)
(γ-emitter)
209At collected from 213Fr ion beams
209At identified as novel SPECT isotope
32

## Slide 33: Ion beams of therapeutic α-emitters
Isotope | 1st Ionization energy | Ion Source
TANTALUM TARGET |  | 
149Tb | 5.86 eV | Re surface ionizing
URANIUM TARGET: |  | 
211At | 9.54 eV | Plasma/Resonance ionization laser
212/213Bi | 7.29 eV | Plasma (aka FEBIAD)
223/225Ra | 5.28 eV | Re surface ionizing
225Ac | 5.28 eV | Re surface ionizing
Note: |  | 
211/213Fr | 3.94 eV | Re surface ionizing (Most Intense!)

## Slide 34: ISOL pilot study: 209At
Implantation chamber
34
Credit to: Peter Kunz, TRIUMF
Notes: No unexpected inventory. No other astatine isotopes

## Slide 35: From bench to (pre-clinical) bedside
109 ions/s of 213Fr collected for up to 9.5 h
209At recovered by dissolving NaCl targets in 0.1 N NaOH (< 300 µL)
Up to 8.9 mCi 209At (EOB)
(Measured by γ-ray spectroscopy)
209At: 80 keV peak
209At + 123I
123I: 159 keV peak
Labeling Chemistry

## Slide 36: 211Rn/211At generator system from 211Fr ion beams (>109 ions/s)
211Rn/211At generator could increase 211At supply and opportunities for distribution
The 211Fr decay chain provided a novel approach to 211Rn production
211Rn was isolated in dodecane,
other radioactive inventory was washed away with aqueous solution
211At progeny recovered
after several hours of grow-in
36

## Slide 37: 211Rn isolation design
Implant 211Fr in NaCl
Submerge target in dodecane
Dissolve NaCl
in dilute NaOH
Mix and remove aqueous solution (Pb/Bi/At/Po)
211Rn isolated in dodecane →211A
Adapted from Maeda et al, 2015 Radioanal Nucl Chem, 303:1465-1468 (Kanazawa U.)

## Slide 38: Moving on to feasibility of 225Ra/225Ac
Add
0.1 ml 0.1 N HCl
Evaporate
Add and Retrieve
0.1 ml 0.1N HCl
Residual Activity (Bq)
Evap.-Rinse Cycles
Extraction using 0.1N HCl solution
Recoil transfer in vacuum
Source
Catcher
Efficiency ~30%
225Ac
213Po
217At
221Fr
213Po
217At
221Fr
213Bi
Source
Catcher
38

## Slide 39: Future Direction: 225Ac/213Bi
ISOL and Target Dissolution/Extraction
225Ac, 213Bi,
many other options
Image taken from: E Price, C Orvig, Chem. Soc. Rev., 2014,43, 260-290
  TRIUMF capable of producing large (Ci) quantities of isotopes such as 225Ac, 223,225Ra, 213Bi, 211Rn
  Possible to ship targets for off-site processing (short-term)
  Effort in early stages, infrastructure, regulatory capabilities being pursued/implemented (long-term)
39

## Slide 40: Medical Isotopes from ISAC/ISOL
Generators: 211Rn/211At; 225Ra/225Ac; 225Ac/213Bi
Feasibility/Chemistry in lead up to full target harvest:
40

## Slide 41: Acknowledgements: Tc-99m
The Team:
  PIs: F. Bénard, T. Ruth, A. Celler, J. Valliant, M. Kovacs,
  Ken Buckley, Vicky Hanemaayer, Brian Hook,
  Stuart McDiarmid, Stefan Zeisler, Frank Prato,
  Anne Goodbody, Joe McCann, Conny Hoehr,
  Tom Morley, Julius Klug, Philip Tsao,
  Milan Vuckovic, Patrick Ruddock, Maurice Dodd,
  Guillaume Langlois, Wade English, Xinchi Hou,
  Jesse Tanguay, Jeff Corsault, Ross Harper,
  Frank Prato, Constantinos Economou
TRIUMF and BCCA machine shops
Finances/Admin
  Henry Chen, Francis Pau, Jenny Song, Steven Foster, Frank Gleeson, James Schlosser, Jim Hanlon, Ann Fong, Neil McLean, Kevin McDuffie, Niki Martin, Karen Young

## Slide 42: Acknowledgements: ISAC/ISOL
This work has been funded in part by an Innovation Grant from the Canadian Cancer Society (CCS)
Production
Chemistry
Radiation Safety
Animal Imaging
Jason Crawford
Tom Ruth
Peter Kunz
Jens Lassen
Stefan Zeisler
Friedhelm Ames
Colin Morton
Peter Machule
Stephen Chan
Linda Graham
D. Scott Wilbur (UW)
Don Hamlin (UW)
Joe Mildenberger
Danka Krsmanovic
Roxana Ralea
Maxim Kinakin
David Prevost
Roxana Ralea
Mike Johnson
Lynne Lemessurier
François Bénard (BCCRC)
Kuo-Shyan Lin (BCCRC)
Vesna Sossi (UBC)
Chenoa Mah (UBC)
Tina Jorgensen (CCM)
Stephan Blinder (UBC)
Katherine Dinelle (UBC)
Maryam Shirmohammad (UBC)
Oliver Press (antibody)
Hua Yang (TRIUMF)

## Slide 43: Acknowledgements: Salt Target
The Team:
  TRIUMF: E Oehlke, C Hoehr, K Buckley, S Zeisler, M Adam, TJ Ruth,
  V Hanemaayer, M Dodd, B Hook, S McDiarmid, H Yang, Q Miao,
  L Graham, D Prevost
  BCCA: F Bénard, M Vuckovic, G Dias, J Klug, W English, KS Lin
Collaborators, staff and students:
  Mark Martinez (UBC), P Jahangiri,
  C Orvig (UBC), E Price, C Ramogida,
  A Celler (UBC), X Hou
TRIUMF and BCCA machine shops