## Slide 1: J-M Guay1,4, G. Côté1, M. Charron1, A. Cala’ Lesina1,3, J.S. Baxter1, L. Ramunno1,3, P. Berini1,3,4 and A. Weck1,2,4
Plasmonic angle independent/dependent coloring of noble metals using picosecond laser pulses
1Department of Physics, University of Ottawa, 150 Louis-Pasteur, ON, K1N 6N5, Canada
2Department of Mechanical Engineering, University of Ottawa, 161 Louis Pasteur, ON, K1N 6N5, Canada
3School of Electrical Engineering and Computer Science, University of Ottawa, Ottawa, Canada
4Centre for Research in Photonics, University of Ottawa, Ottawa, Canada

## Slide 2: Acknowledgements
Stephen J Bodor, P.Eng
Dr. Iain Brooks, RCM
Dr. Xianyao Li, RCM
18

## Slide 3: Outline
Introduction
Coloring of Silver
FDTD simulations
Coloring of Gold
Passivation of Colored surfaces
Laser Induced Periodic Surface Structures (LIPSS)
Stamping
Conclusion
2

## Slide 4: Introduction
2 main ways of controlling perceived colors by the nanoparticles:
2) Volume fraction
1) Size and Shape
Hentschel, M. et al. ‘Transition from isolated to Collective Modes in Plasmonic Oligomers’, Nano Letters, 2010
Image taken from: ScienceGeist, ‘The Shape of Things’
3

## Slide 5: Colouring of Ag
Colors obtained at 50 mm/s, 1064 nm, fluence of 1.67 J/cm2 (note: lower lightness)
Colors obtained at 1000 mm/s, 1064 nm, fluence of 29.75 J/cm2 (note: higher lightness)
Similar colours can be obtained via different sets of laser parameters
Colours are quantified using LCH colour space
Angle independent colours
4
Raster scanning sample surface
J-M. Guay et al. Submitted (2016)

## Slide 6: Colouring of Ag
All Hue (colour) linked to a unique ‘total accumulated fluence value’
Colours can be ramped up for industrial applications
Coins that took hours now take minutes…
5

## Slide 7: Coloring of Ag
Controlling particle density with line spacing
3 distinct set of particles are deposited on the surface
2 sets capable of color and each changing oppositely with line spacing
Increasing spacing
6
Small
Medium, Large
Total accumulated fluence

## Slide 8: FDTD simulations
Small particles = coupling between the medium size particles
Small particles = plasmon resonances
Embedded small particles are shown to predict the experimental colors
7

## Slide 9: Coloring of Ag
Can color topographical surfaces with ease
For minting it is in fact better than pad printing due to edges
Coloring independent of surface quality
Can color rough (frosted) surfaces
8

## Slide 10: Coloring of Ag
Selective coloring and high resolution coloring of silver
Allows for the creation of color gradients
9

## Slide 11: Burst Coloring of Gold
Using burst, gold was also colored
Colors covered the entire visible and intra-spectral region
The nature of the colors are currently under investigation
Purple gold
16
J-M. Guay et al. In Progress (2016)
J-M. Guay et al. Patent Pending (2016)

## Slide 12: Surface passivation and colour protection
Surface protected while conserving colours using ALD deposition of alumina
Slight red shift in colors
11
Post-ALD coated
Pre-ALD coated

## Slide 13: Surface passivation and colour protection
Tarnish test
Humidity + Temperature Test
Without ALD (control)
Colors survived Tarnish and Temperature + Humidity tests
Temperature + Humidity test = 72h in 85% RH at 38°C followed by 6h in 30% RH at 60°C
Tarnish test = 20 hours in chamber with highly concentrated H2S
J-M. Guay et al. In Progress (2016)
12

## Slide 14: Angle dependent colours
13

## Slide 15: Introduction
Interference between surface EM wave and incoming light
Reduction in periodicity due to grating assisted coupling
Quality of ripples depend on Electron-phonon coupling
14
Huang et al., ACS Nano, 3(12), 2009,
Wang J. et Guo C., Applied Physics Letters, 87, 2005,
Scorticati, D. et al., Journal of Nanophotonics, 6(1), 2012

## Slide 16: Holograms (direct writing on Ag)
Direct writing of LIPSS unto silver using burst
Burst increases Electron-Phonon coupling causing the LIPSS structures to be more defined
15
J-M. Guay et al. internal review (2016)

## Slide 17: Holograms
Creation of laser induced periodic surface structures on steel
Holograms on topography
16

## Slide 18: Hologram (Transfer)
Transfer of 2D structures
Transfer of topographical 3D structures
Transfer of LIPSS via stamping from steel die
Nanometer features can be transferred
Allows for well defined LIPSS on non-plasmonic metals and metals with weak electron-phonon coupling
17

## Slide 19: Conclusion
Angle-independent colours controlled via the particle density deposited on the silver surface
Colours linked through a similar total accumulated fluence value  scalable
Colouring technique independent of surface quality
The small particles are found to be dominantly responsible for the colours  new plasmonic modes
Colouring of gold  covering the entire visible an extra-spectral range of colours
Burst enhancement of LIPSS
Transferring of LIPSS via a stamping process
18