## Slide 1: Investigation of Entropy- Enthalpy Compensation effect in the Ti-V-Cr System.
1. Material synthesis
2. Crystal structure
The crystal structure was studied by X-Ray diffraction (XRD).
3. First hydrogenation properties
Capacity of hydrogen absorption was determined with a Sievert-type apparatus.
All samples were synthesized by arc melting.
Viney Dixit a , Thomas Bibienne a, Jacques Huot a
a Université du Québec à Trois-Rivières – Institut de Recherche sur l’hydrogène - 3351, boul. des Forges, C.P. 500, Trois-Rivières (Québec) G9A 5H7.
INTRODUCTION
Titanium-based alloys with a solid solutions Body Centered Cubic (BCC) crystal structure are well known to be good hydrogen storage materials because of their high volumetric hydrogen storage capacity.
We have recently found that in Ti-V-Cr system, the enthalpy of hydrogenation is linearly related to the entropy change1,2,3 which is represented by the Fig.1. This is the so-called enthalpy-entropy compensation. The aim of the present work is to investigate the entropy-enthalpy compensation effect by varying the elemental concentration of the Ti-V-Cr system.
OBJECTIVES
CONCLUSION
RESULTS
Fig. 2: X-Ray diffraction patterns of as-cast TixV70-xCr30 (x = 10, 20, 30, 40, 50) samples .
ACKNOWLEDGMENT
Crystal Structure
METHODOLOGY
Synthesis and structural characterization of the system TixV70-xCr30 (x = 10, 20, 30, 40, 50).
Hydrogenation studies of these materials.
Verify the Entropy-Enthalpy relationship and find the mechanism
Five different compositions of Ti-V-Cr were investigated.
All samples have the same crystal structure (BCC solid solution).
Large discrepancies in the first hydrogenation behaviour are observed.
Fast kinetics of first hydrogenation may be explained by the presence of a secondary phase.
Microstructure and thermodynamic parameters are now being investigated.
First Hydrogenation
REFERENCES
Fig. 3: First hydrogenation at 24°C and under 20 bar hydrogen pressure. As-cast samples: TixV70-xCr30 (x = 10, 20, 30, 40, 50) + 4 wt.% of Zr7Ni10.
x = 50 has the highest capacity and an incubation time of less than 8 minutes.
For x = 20, no incubation time but capacity is lowered.
Sample x = 10 has shown low storage capacity.
All samples have the BCC structure. Small peaks may indicate the
Presence of a secondary phase.
Crystal parameters of as cast samples are shown in Table. 1.
[1] Bibienne T and Huot J. Journal of Alloys and Compounds, 607 (2014) 251– 257.
[2] ] Bibienne T and Huot J. Journal of Alloys and Compounds, 620 (2015) 101-108
[3] Bibienne T and Huot J. To be published.
V. Dixit would like to thank to Canadian Queen Elizabeth II Diamond Jubilee Scholarships for a Ph.D. fellowship.
ABSTRACT
Selected composition of TixV70-xCr30 (x = 10, 20, 30, 40, 50) alloys doped with 4 wt.% of Zr7Ni10 have been synthesized by arc melting. Crystal structure was characterized by X-ray diffraction pattern. Hydrogen storage properties were investigated using a Sievert- type apparatus. We found a strong discrepancy in the first hydrogenation curves of these samples. Maximum hydrogenation capacity was measured to be 4.0 wt.% for the Ti50V20Cr30 alloy.
Alloy | Lattice Parameter (Å) | Crystallite Size (nm) | Microstrain (%)
Ti10V60Cr30 | 3.000(2) | 18 (1) | 0.43(9)
Ti20V50Cr30 | 3.023(1) | 12.5 (3) | 0.62(4)
Ti30V40Cr30 | 2.999(1) | 16(1) | 0.38(9)
Ti40V30Cr30 | 3.069(1) | 14.4(8) | 0.47(9)
Ti50V20Cr30 | 3.102(1) | 15.6(6) | 0.46(6)
Table.1
Fig.1:Enthalpy-Entropy plot of Ti-V-Cr system