## Slide 1: Microstructure and hydrogen storage properties of FeTi + x wt.% Hf alloys (x = 0, 4, 8 and 12)
By : Volatiana RAZAFINDRAMANANA
Jean-Louis BOBET and Jacques HUOT
At the 2016 CAP Congress – 15th of June 2016

## Slide 2: Outline
1. State of art
Renewable energy
  Hydrogen
    Metal Hydride
      FeTi alloy
Fe-Ti-Hf system
  Microstructure
First hydrogenation properties
State of art
Metal Hydride
Fe-Ti-Hf system
Conclusion
2
  Conclusion
    Outlook
Perspectives

## Slide 3
High population
growth
Limited reserves of fossil fuel
Energy : big challenge of the XXI century
Renewable
energy
Reduction in emissions of greenhouse gases
Electronic
Outline
State of art
Metal Hydride
Fe-Ti-Hf system
Conclusion
Urban transport
HYDROGEN
« Stationary » application
3

## Slide 4
H2
Hydrogen liquid
-253°C / 1 atm
Compressed 25°C / 350 to 700 atm
Metal hydride 25°C – 1 atm
Outline
Conclusion
Best way to store hydrogen
State of art Metal Hydride Fe-Ti-Hf system
Hydrogen storage
4

## Slide 5
Outline
State of art
Metal Hydride
Fe-Ti-Hf system
Conclusion
Metal hydride
Metal
1
2
Adsorption (and dissociation) of hydrogen
Diffusion of hydrogen (absorption)
Total absorption of hydrogen in the material
3

## Slide 6: Outline
FeTi alloy
State of art
Metal Hydride
Fe-Ti-Hf system
Conclusion
Space group Pm3m
Fe
Ti

## Slide 7: Outline
State of art Metal Hydride Fe-Ti-Hf system
Alternative process
Conclusion
Substitute Fe by Mn
Add some dopants such as :
Zirconium (Zr),
Nickel (Ni),
Zr7Ni1O,
Hafnium (Hf)
0
1
2
5
6
7
0,0
0,2
0,4
0,6
0,8
1,0
1,2
1,4
1,6
Temps (h)
FeTi
FeTi+Nickel
FeTi+Zirconium
)
l
a
t
o t
s
d
i
o p
(%
e
n
è g
ro
yd H
3 4
Time (h)
Hydrogen absorbed (wt.%)
Activation curves of FeTi and FeTi doped with
Zr and Ni, at 25°C under 45 bar of H2.

## Slide 8
Outline
State of art Metal Hydride Fe-Ti-Hf system
Conclusion
FeTi + 4wt.%Hf
FeTi + 12wt.%Hf
Matrix (A) + secondary phase (B)
Presence of dendritic phase
A
B
Microstructure
FeTi + 8wt.%Hf
A
B
A
B

## Slide 9
Outline
Conclusion
Phase Composition | FeTi + 4wt.%Hf | FeTi + 8wt.%Hf | FeTi + 12wt.%Hf
Matrix | 48.9Fe – 49.0Ti – 1,9Hf | 49,7Fe – 49,5Ti – 0,7Hf | 49.3Fe – 49.7Ti – 1.0Hf
2nd phase (1) | 53,2Fe – 40.3Ti – 6,4Hf | 58,5Fe – 39,9Ti – 1,6Hf | 56.7Fe – 40.4Ti – 2.8Hf
2nd phase (2) | 34.5Fe – 59.8Ti – 4.7Hf | - | -
Ti
Fe
Hf
Ti
State of art Metal Hydride Fe-Ti-Hf system
Element mapping by EPMA
FeTi + 4wt.%Hf FeTi + 8wt.%Hf
FeTi + 12wt.%Hf

## Slide 10: Outline
Activation curves of FeTi + x wt.%Hf
(x = 4, 8 and 12), at 25°C under 20 bar of H2.
FeTi + 12wt.% Hf
FeTi + 8wt.% Hf
Need a minimum of 8wt.% of Hf to activate FeTi
No incubation time
Kinetic increases with wt.% Hf
FeTi + 4wt.% Hf
% Hf | 4 | 8 | 12
% H abs. | 0 | 1.1 | 1.4
State of art Metal Hydride Fe-Ti-Hf system
Activation properties
Conclusion
10

## Slide 11
Resume
FeTi needs a minimum of 8wt.% Hf to be activated
  Role of the Ti rich phase
FeTi alloy doped with hafnium has a good industrial base
  Low cost
  First hydrogenation at room temperature
  Fast kinetic
Perspective
Identify the 2nd phase by neutron diffraction
Outline
State of art
Metal Hydride
Fe-Ti-Hf system
Conclusion
11

## Slide 12
Thank you for your attention
Questions ?
CAP Congress organizers J.Huot & JL.Bobet
Region Aquitaine My colleagues