## Slide 1: Reversibility of Magnetic Behavior in High Entropy Oxides
Tahereh Afsharvosoughi
Prof. David Crandles
Physics Department
Brock University

## Slide 2: Outline
Introduction
Objective
Methodology
Results
Conclusion

## Slide 3: Hot topic!
Year wise publications in the research area of HEAs (Based on the Scopus analyze search results for “High Entropy Alloys” as on Sep 12, 2017)1.
Chart: Number of documents per year
| 2004.0 | 2005.0 | 2006.0 | 2007.0 | 2008.0 | 2009.0 | 2010.0 | 2011.0 | 2012.0 | 2013.0 | 2014.0 | 2015.0 | 2016.0 | 2017.0
Documents | 1.2043 | 8.1055 | 9.9414 | 16.7502 | 19.2966 | 31.7779 | 29.2078 | 45.5513 | 58.036 | 125.195 | 166.4968 | 277.5222 | 364.4982 | 391.1707

## Slide 4: What are High Entropy Materials?
Mixtures of alloys (e.g: Cr, Mn, Fe, Co, Ni)2
Mixtures of oxides (e.g: NiO, CuO, MgO, CoO, ZnO)3

## Slide 5: Why they are called high entropy materials?
Maximum achieve when equimolar mixtures ()4
Maximum achieve when equimolar mixtures (𝑥_𝑖=1/𝑁 𝑖𝑛 𝑆_𝑐𝑜𝑛𝑓=〖−𝑘〗_𝐵 ∑_(𝑖=1)^𝑁▒〖𝑥_𝑖 〖log⁡(𝑥〗_𝑖)〗)4
Facilitate formation of single phase solid solution5
High configurational entropy
(∆G = ∆H − T∆Sconf)
High configurational entropy
(∆G = ∆H − T∆Sconf)

## Slide 6: Fascinating properties
HEAs
great hardness
toughness
HEOs
colossal dielectric constant6
Superionic conductivity7
Corrosion resistance5
Enhanced exchange bias4

## Slide 7
What are we looking for ?
Whether the magnetic behavior just like structural behavior is reversible by sintering or not?

## Slide 8: Reversibility of structural phase transition by sintering in HEOs
In 2015 ☛Rost et al showed reversible transition from multiphase to single phase by sintering at intermediate and high temperature and vice versa3

## Slide 9: Methodology
Sample Preparation
Structural property measurement
Magnetic property measurement
Mixing MgO, CuO, NiO, ZnO, CoO in ball mill for 2 hours
Rigaku X-ray diffractometer with Cu-Kα radiation
Quantum Design Magnetic Properties Measurement System (MPMS)

## Slide 10: X-ray diffraction measurement results
Chart: 
| Sample sintered at 700oC | Sample sintered at 1100oC | Sample resintered at 700oC
FCC | 0.48 | 1 | 0.72
Tenorite(CuO) | 0.19 | 0 | 0.19
other phases | 0.33 | 0 | 0.09

## Slide 11: Magnetization measurement result

## Slide 12: Four mixtures without CuO
Chart: 
| HEO without CuO sintered at 700oC | HEO without CuO sintered at 1000oC | HEO without CuO resintered at 700oC
FCC | 0.7 | 1 | 0.7
Co3O4 | 0.16 | 0 | 0.3
ZnO | 0.12 | 0 | 0

## Slide 13: Magnetization measurement result

## Slide 14: Comparison of five and four mixtures without CuO

## Slide 15
SEM result for five mixture resintered at 700oC
Co-K𝜶1
Mg-K𝜶1
Ni-K𝜶1
Cu-K𝜶1
Zn-K𝜶1
Secondary electron image(SE)
Backscattered electron image(BSE)

## Slide 16: Conclusion
The SEM, XRD and magnetization data all indicate segregation of CuO when resintering single phase FCC material at 700oC.
There is an interplay between structural and magnetic behavior.

## Slide 17: Thanks for Your Attention