## Slide 1: Characterization of VUV sensitive silicon photomultipliers (SiPMs)
Bindiya Chana
Supervisor: Dr. Simon Viel
CAP Congress, 8th June 2022

## Slide 2: Motivation
Quality control and testing of these large number of SiPMs will be a challenge.
A quick and reliable SiPM testing technique is required at all stages (from single SiPM to fully installed system).
Silicon photomultipliers (SiPMs) are emerging technology in photon detection in particle physics.
Large future experiments like nEXO, ARGO etc. will use SiPM based light detection system
Challenges
SiPM tile

## Slide 3
Goals of this project
Current-voltage (IV) characterization of SiPM
Develop the IV fit model to understand the IV curves
Use fit model to extract the empirical parameters of SiPMs
Compare and verify the results from IV analysis with pulse analysis
Extend the study to different SiPM devices at a range of temperatures in different light conditions

## Slide 4: VERA* setup at TRIUMF
VERA setup at TRIUMF used to take measurements for SiPMs
SiPM devices
Temperature range
Light conditions
-110o C to +20o C
FBK** VUV HD3
Hamamatsu VUV4
Dark
Light source – 175nm & 385nm
*VERA – Vacuum Emission, Reflectance and Absorbance
** FBK - Fondazione Bruno Kessler
Thanks to Dr. Fabrice Retiere and Dr. Mahsa Mahtab (TRIUMF) for their support in this project

## Slide 5: VERA* setup at TRIUMF
VERA setup at TRIUMF used to take measurements for SiPMs
SiPM devices
Temperature range
Light conditions
-110o C to +20o C
FBK** VUV HD3
Hamamatsu VUV4
Dark
Light source – 175nm & 385nm
*VERA – Vacuum Emission, Reflectance and absorbance
** FBK - Fondazione Bruno Kessler
Thanks to Dr. Fabrice Retiere and Dr. Mahsa Mahtab (TRIUMF) for their support in this project

## Slide 6: SiPM IV curve
Pre-breakdown region
Post-breakdown region
Breakdown voltage
Post-breakdown region
SiPMs are usually operated in post breakdown region
Geiger mode – a single charge carrier is able to trigger an avalanche
High gain
Correlated avalanche noise

## Slide 7: Breakdown voltage
Relative logarithmic derivation method to extract the breakdown voltage.
Landau fit function on and mean value gives the breakdown voltage.
Breakdown voltage increases linearly with temperature.
FBK dark at 20o C

## Slide 8: Correlated noise parameters
Cross-talk
Afterpulsing
Figures from Piemonte C and Gola A (2019)
During avalanche, accelerated carriers in the high field region could emit photons
That photon can initiate a secondary avalanche in a neighbouring microcell.
Carriers get trapped in defects in the silicon.
Released after a delay which initiate an avalanche in the same microcell.

## Slide 9: Reverse bias fit model
Pre breakdown fit function :
= Shockley-Read-Hall recombination factor
= Zero bias depletion layer width
, p = CV parameters
, B = empirical parameters (Otte et al (2017))

## Slide 10: Reverse bias fit model (contd.)
Post breakdown fit function : involves the contribution of dark noise and correlated noise – afterpulsing and cross-talk
= Dark noise rate = Overvoltage ,
= Breakdown voltage = Capacitance; = leakage current
PAP = probability of afterpulsing ; PCT = probability of crosstalk
= triggering probability

## Slide 11: IV fits for 2 devices
HPK dark
Preliminary

## Slide 12: IV parameters
* Only statistical error bars are shown
Considering C to be constant over different temperatures, R increases exponentially with temperature
Parameter AP(V) tends to stay constant with temperature, similar results are indicated in literature
Parameter CT(V2) tends to stay constant with temperature

## Slide 13: Pulse analysis
4V overvoltage
SiPM pulse data was taken at two overvoltages (4 & 7V) at 0.5PE threshold.
Primary pulse selection :
  It should be single PE (0.5 - 1.5PE)
  It should happen atleast 500μs later than previous pulse.

## Slide 14: Dark noise rate
Dark count rate (DCR) showed exponential rise with temperature
It also increases with increase in overvoltage

## Slide 15: Optical crosstalk
OC probability increases with overvoltage
Crosstalk seems to be independent of temperature, similar results are indicated by IV analysis as well.

## Slide 16: Summary and future plans
  IV characterization and fit model looks promising over a range of temperatures for both FBK and Hamamatsu SiPM devices
  Improve the IV model for dark data
  Extend the fit functions with some additional terms for light data
  Improve pulse analysis for HPK device data
  Light data has already been taken and analysis for both IV and pulse data are ongoing
  At TRIUMF, Cryo probe facility will use IV characterization to test thousands of SiPMs for nEXO.