## Slide 1: Impact of NH3 consumption in a low frequency Ar-NH3 atmospheric pressure DBD
Raphaël Robert, Luc Stafford, Françoise Massines
June 8th 2022
raphael.robert@umontreal.ca

## Slide 2: Plasma at atmospheric pressure and use of DBDs
In nature
In the laboratory
Tgas ≈ 5000 - 30 000 K
DBD : Dielectric barrier discharge
High ionization rate plasma (>1%) :
 Welding, depollution
Surface treatment
Thin film layer deposition
LAPEX
© Audren Dorval
Tgas ≈ 300 - 500 K
DBD  limits the current flow
Prevents arc transition
 Treatment of large susbtrates
Charges are collected on dielectrics
Create an E opposite to the applied E
Discharge extinguishes due to dielectrics

## Slide 3: Homogeneous and filamentary discharge at atmospheric pressure
Plane to plane electrode at Atmospheric Pressure (AP) : 2 discharge regimes
Filamentary discharge
Homogeneous discharge
Local energy deposit
Statistical surface treatment
Applied voltage, gas voltage and current as a function of time [1]
[1] F. Massines and G. Gouda, J. Phys. D. Appl. Phys., vol. 31, no. 24, pp. 3411–3420, 1998.
[2] N. Naudé, HAL Id : tel-00601053, p. 18, 2011.
Applied voltage, gas voltage and current as a function of time [1]
Max power density : 10 W.cm-2
Current density : 1-10 A.cm-2
Max power density : 1-5 W.cm-2
Current density : 1 mA.cm-2
Energy deposited on the whole electrode

## Slide 4: Use of Penning mixture
DBDs helps prevent arc transition
Pure Ar  filamentary discharge
Need to limit the electronic multiplication during breakdown
Penning mixture :
Decreases the energy needed for the breakdown
Two step ionization  slow down electronic multiplication
Ar + NH3 (Penning Mixture)  homogeneous discharge
Dire
Direct excitation
Collisional
de-excitation
Energy levels for Ar and NH3

## Slide 5: Consumption of NH3 by the discharge
[1] J. Balamuta, M. F. Golde, and Y. Ho, J. Chem. Phys., vol. 82, no. 7, pp. 3169–3178, 1983.
Penning reaction can be ionization or dissociation of NH3:
42% [1]
58% [1]
Consumption of NH3 by the plasma
Experimental setup
Byproducts of NH3 : NH / N2 / OH / NH2
1st
3rd
2 mm gap
1 mm layer of quartz
50 kHz

## Slide 6: Consumption of NH3 by the discharge
Penning reaction can be ionization or dissociation of NH3:
42% [1]
58% [1]
Consumption of NH3 by the plasma
[1] J. Balamuta, M. F. Golde, and Y. Ho, J. Chem. Phys., vol. 82, no. 7, pp. 3169–3178, 1983.
1st
3rd
Ar + NH3
Current and voltage for the 1st and the 3rd discharge with 280 sccm flux
280  28 sccm

## Slide 7: Electrical signature of NH3 consumption
Flow : 28 sccm  gas speed : 0,037 m.s-1  residence time in the discharge : 0,38 s
Flow : 56 sccm  gas speed : 0,074 m.s-1  residence time in the discharge : 0,19 s
Flow : 168 sccm  gas speed : 0,22 m.s-1  residence time in the discharge : 0,063 s
Discharge current is affected by total flow of Ar + NH3 (215 ppm)
Low flow  No discharge
Medium flow  Abnormal current peak (thin peak, slow decrease of the current)
High flow  Typical glow DBD current peak
Current shape linked to the flow, via residence time of the Penning mixture
Current and voltage for as function of the Ar + NH3 flux
Typical glow DBD  below a residence time of 0,1 s

## Slide 8: Optical signature of NH3 consumption
Low flow  NH3 is consumed at the entrance of the discharge
Current peak indicates abnormal discharge
Optically, entrance of the plasma differs from exit
Measurement of the light intensity shows a temporal shift
Combination of electrical and optical measurements
One single discharge  Two behaviors
Ar + NH3
1st discharge
280 sccm
56 sccm
Picture of the 1st discharge cell
Intensity of the visible ligth on one discharge as function of time
1st discharge

## Slide 9: Conclusion
Ar + 215 ppm
Quantity of NH3 is a key parameter in the physics driving Ar based homogeneous DBDs
NH3 consumption induces :
Increase of breakdown voltage
Broadening of the discharge current peak
Two distinct discharge regimes  a typical DBD glow and a low density glow (Townsend ?)
  Measurements as a function of space and inlet flow indicates a critical gas residence time for a typical DBD glow vs hybrid glow discharge

## Slide 10: Electrical signature of NH3 consumption
Flow : 28 sccm  gas speed : 0,037 m.s-1  residence time in the discharge : 0,38 s
Flow : 56 sccm  gas speed : 0,074 m.s-1  residence time in the discharge : 0,19 s
Flow : 168 sccm  gas speed : 0,22 m.s-1  residence time in the discharge : 0,063 s
Discharge current is affected by the total flow of Ar + NH3 (215 ppm)
Low flow  No discharge
Medium flow  Abnormal current peak (thin peak, slow decrease of the current)
High flow  Typical glow DBD current peak
Current shape linked to the flux via residence time Penning mixture
Current and voltage for as function of the Ar + NH3 flux
Typical glow DBD  below a residence time of 0,1 s

## Slide 11: Experimental details
Current and voltage for the 1st and the 3rd discharge with 280 sccm flux
Breakdown on the 3rd electrode occurs later than the one on the 1st electrode
i.e. For a higher applied voltage
Confirms the consumption of NH3 along the gas flow lines
1st
3rd
2 mm gap
1 mm layer of quartz

## Slide 12: Conclusion
Ar + 215 ppm
Quantity of NH3 is a key parameter in the physics driving Ar based homogeneous DBDs
Spacially resolved electrical measurements revealed that NH3 consumption induces :
  Increase of breakdown voltage
  Broadening of the discharge current peak
Spacially resolved optical measurements revealed that NH3 consumption induces :
  Two distinct discharge regimes  a typical DBD glow and a low density glow (Townsend ?)
  Measurements as a function of space and inlet flow indicates a critical gas residence time for a typical DBD glow vs hybrid glow discharge

## Slide 13: Experimental details
Current and voltage for the 1st and the 3rd discharge with 280 sccm flux
Breakdown on the 3rd electrode occurs later than the one on the 1st electrode
i.e. For a higher applied voltage
Confirms the consumption of NH3 along the gas flow lines
1st
3rd
Ar + 215 ppm

## Slide 14: Consumption of NH3 by the discharge
Penning reaction can be ionization or dissociation of NH3:
42% [1]
58% [1]
Consumption of NH3 by the plasma
[1] J. Balamuta, M. F. Golde, and Y. Ho, J. Chem. Phys., vol. 82, no. 7, pp. 3169–3178, 1983.
1st
3rd
2 mm gap
1 mm layer of quartz
Experimental setup

## Slide 15: Conclusion
Ar + 215 ppm
Quantity of NH3 is a key parameter in the physics driving Ar based homogeneous DBDs
Spacially resolved electrical measurements revealed that NH3 consumption induces :
  Increase of breakdown voltage
  Broadening of the discharge current peak$
Spacially resolved optical measurements revealed that NH3 consumption induces :
  Two distinct discharge regimes  a typical DBD glow and a low density glow (Townsend ?)
  Measurements as a function of space and inlet flow indicates a critical gas residence time for a typical DBD glow vs hybrid glow discharge regime low density glow (Townsend ?)
Once the discharge ignites, NH3 is consumed; if the quantity of NH3 is insufficient, the discharge changes its behavior as the dissociation of NH3 occurs.
This reasoning applies to all discharges with a controlled quantity of molecules in the carrier gas.
Perspectives :
Calculate NH3 consumption as a function of residence time and applied power
Determine the minimum amount of NH3 to inject into a discharge in order to have the same behavior from the entrance to the exit of the discharge

## Slide 16: What is a Plasma ?
Plasmas is the « 4th state of matter »
Composed by neutral, electrons, ions, radicals, photons
Oscilloscope
LF
Ar + 215 ppm NH3
Current probes
Electrodes

## Slide 17: Homogeneous and filamentary discharge at atmospheric pressure
On plane electrode at atmospheric pressure (AP) : 2 regimes of discharge
Filamentary discharge
Homogeneous discharge
Local energy deposit
Statistical treatment
Applied voltage, gas voltage and current as function of time [1]
[1] F. Massines and G. Gouda, J. Phys. D. Appl. Phys., vol. 31, no. 24, pp. 3411–3420, 1998.
[2] N. Naudé, HAL Id : tel-00601053, p. 18, 2011.
Applied voltage, gas voltage and current as function of time [1]
Max power density : 10 W.cm-2
Current density : 1-10 A.cm-2
Max electron density : 1020 m-3
Max power density : 1-5 W.cm-2
Current density : 1 mA.cm-2
Max electron density : 1017 m-3
Energy deposited on the all electrode size

## Slide 18: Atmospheric pressure glow DBD (APGD)
[2] F. Massines, N. Gherardi, N. Naudé, and P. Ségur, “Glow and Townsend dielectric barrier discharge in various atmosphere,” Plasma Phys. Control. Fusion, vol. 47, no. 12 B, 2005.
Power supply voltage, Vps, gas voltage, Vgas, and discharge current, as function of time [1]
DBDs helps prevent arc transition
Homogeneous discharge
LF ignition time ≈ 10 % of the period duration
Electric field
[1] N. Naudé, “Etude électrique de la physique d ’ une décharge de Townsend à la pression atmosphérique et de son interaction avec un générateur : Modèle et Expérience To cite this version : HAL Id : tel-00601053,” p. 18, 2011.
Nemax: 1010-1011 cm-3
Nimax: 1010-1011 cm-3
NArmmax : 1011 cm-3
Current densitymax : 5 à 20 mA.cm-2
Tgaz : 300 K
Electric field along the gap in a APGD [2]

## Slide 19: Influence of NH3 quantity
Low flux  NH3 is consumed at the entrance of the discharge
Current peak indicates abnormal discharge
Optically, entrance of the plasma differs from exit
Measurement of the ligth intensity shows a temporal shift
Ar + 215 ppm
1st discharge
Picture of the 1st discharge cell
Intensity of the visible ligth on one discharge as function of time
One single discharge  Two behaviors