## Slide 1: Surface Relaxation of Vapor Deposited Polystyrene Glasses
Junjie Yin
James Forrest Lab
Physics, University of Waterloo
Outline
Background:
  Glasses and stable glasses
  Physical vapor deposition
Experimental methods:
  Surface perturbations by gold nanoparticles
  AFM measurements
Results and discussions

## Slide 2: Glass and stable glass
S, H, or V
Temperature
source
substrate
glass
substrate
3-5 nm mobile layer
L. Berthier, M. D. Ediger (2016), Physics Today, 69, 1, 40

## Slide 3: Glass and stable glass
glass
substrate
source
S, H, or V
Temperature
3-5 nm mobile layer
L. Berthier, M. D. Ediger (2016), Physics Today, 69, 1, 40

## Slide 4: Glass and stable glass
S, H, or V
Temperature
source
L. Berthier, M. D. Ediger (2016), Physics Today, 69, 1, 40

## Slide 5: Small molecules
Difficulties:
Low vapor pressures
Sensitive to thermal degradation
Possibilities:
Start with small N
Successful distillation of PS (N of 3–17), PEO (N of 7–13) and PMMA (N ~ 7)
Atactic PS:
No crystal ground state
Surface dynamics well studied
A. Raegen, J. Yin, Q. Zhou, & J. A. Forrest (2020). Nature Materials, 19(10), 1110-1113.
Kinetic stability, low and density increase compared to normal glass
Ultrastable: thousands of years in the conventional way
M.D. Ediger (2017), J. Chem. Phys., 147, 210901
S.F. Swallen, et al. (2007), Science, 315 353-356
indomethacin (molecular glass)
Polymers

## Slide 6: Vapor-deposited PS stable glasses
PS glass film prepared by PVD, N = 9
Stable glass compared to regular glass:
Increased density ✓
Bulk kinetic stability ✓
Surface properties ?
glass
mobile surface layer
substrate
Zhang, Y., & Fakhraai, Z. (2017). Physical review letters, 118(6), 066101.

## Slide 7: Experimental methods
stable glass
rejuvenated
glass
Vapor deposition
Prepare stable PS glass films through PVD, and rejuvenate a portion of them
AuNPs
Introduce 20nm size AuNPs on as-deposited and rejuvenated glasses
AFM measurements
At different temperatures, monitor surface relaxation with AFM

## Slide 8: AuNPs on vapor-deposited PS surface
(rejuvenated PVD film of PS, isothermally treated at )
glass
3-5 nm mobile layer
substrate

## Slide 9: Surface evolution in two stages
Embedding is slower for stable glass
Stage 2: embedding
Slower bulk dynamics
Stage 1: material build up

## Slide 10: Quantifying surface properties: peak width/diameter at h=0nm
Stage 1: material build up
Power law relationship with evolution time.
peak width

## Slide 11: t1/4 scaling
Both as-deposited films and rejuvenated films follow t1/4 scaling.

## Slide 12: Characteristic time of relaxation
vapor-deposited
Surface dynamics is independent of bulk stability.
Fakhraai, Z., & Forrest, J. A. (2008). Science, 319(5863), 600-604.
Dhinojwala, et al. (1994). J. Chem. Phys, 100(8), 6046-6054.
spin-cast
Tg
Tg
Short chain, vapor deposited films are similar to long chain, spin-cast films, showing universal behaviours.

## Slide 13: Conclusion
PVD enables us to prepare equilibrated samples in the glassy state.
First measurements on surface relaxation of vapor-deposited PS glasses.
Surface response is similar between stable (equilibrated) and rejuvenated (fresh) PVD films, and both are similar to spin-cast films.
To do
Compare with numerical solutions and learn about the surface mobility.
Characterize stable glass films with varying thicknesses and stabilities to explore their effect on surface properties.