## Slide 1: Characterization of Laser-Driven Photon Emission in Silicon Photomultipliers
Juliette M.J. Martin
TRIUMF, The University of Edinburgh
CAP Congress
June 8th, 2022
1
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 2: Outline
The Silicon Photomultiplier
Cross-Talk
Optical cross-talk studies at TRIUMF
Results
2
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 3: What is a Silicon Photomultiplier (SiPM)?
Solid-state detector
  PMT alternative
  Single photon resolution
  Good photon detection efficiency
Basic unit: single photon avalanche diode (SPAD)
p-n junction biased above breakdown
  Overvoltage:
  Avalanche process: gain is 105-107
3
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 4: SiPM signal detection: SPAD level
Surface coating
Sensor
External cross-talk
Avalanche
Trench
Secondary avalanche
Internal cross-talk
4
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 5: Cross-Talk
Secondary photon by-product of avalanche mechanism
Systematic effect on detector background
Must be quantified for use in rare-event searches (e.g. nEXO)
Is photon emission significant?
5
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 6: MIEL at TRIUMF
SiPM Microscope for Injection and Emission of Light.
Setup developed at TRIUMF
  Study spectral features of SiPM emission
  Geographical location of light emission
Two SiPMs: FBK VUV-HD3.6, HPK VUV4
  nEXO candidate photodetectors
6
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 7: MIEL at TRIUMF
Previous studies explore emission of SiPM in dark conditions
Additions:
  Cryogenic cooling: reduce dark noise, replicate conditions in cryo experiments (nEXO etc)
  Laser injection system: stimulate emission of secondary photons at variety of wavelengths
7
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 8: MIEL laser injection system
SiPM
Collimated laser beam
Dichroic mirror
Longpass filter
8
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022
Microscope objective
Notes: 550 nm longpass filter
was inserted along the IX83 light path to cut any 2nd-order spectrometer features from wavelengths below 550 nm (this combination is hereafter called NIR Spectroscopy mode)

## Slide 9: HPK and FBK photosensors
HPK VUV4
FBK VUV-HD3.6
9
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 10: Laser beam positioning: FBK
Laser: 444nm wavelength
Centre beam on SPAD
Close slit over SiPM for spectra
Open for emission maps.
10
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 11: Emission Microscopy Images: FBK
Polysilicon trenches in FBK – less photon absorbance
Reflection
“Light guiding” effect observed
ADC counts
11
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 12: Emission Microscopy Images: HPK
HPK has tungsten trench
Photon absorption
No distinct ‘cross’ pattern
ADC counts
12
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 13: Spectra: FBK
PRELIMINARY
Raw spectrum
Uncorrected for system efficiency
Rudimentary cosmic removal
550nm longpass filter
Evidence of thin-film interference due to SiO2 coating.
13
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 14: Spectra: HPK
PRELIMINARY
Raw spectrum
Uncorrected for system efficiency
Rudimentary cosmic removal
550nm longpass filter
Fewer oscillation than FBK – thinner coating.
14
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 15: Summary
Stimulated two SiPM with 444nm laser
Obtained raw spectral distributions
Emission maps reflect differences in structure between SiPMs
15
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 16: Ongoing and future work
More effective cosmic removal
Error analysis
Active simulation efforts to model photon transport in SiPM
Correct spectra for system efficiency – intensity calibration
Correct for finite numerical aperture – simulation
Is the level of photon emission a problem for future experiments?
Stay tuned!
D. Minchenko, 8th June, 16:15 in MDCL 1110
16
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 17: Acknowledgements
Supervisor: F. Retière
K. Raymond (SFU, TRIUMF)
PHAAR group at TRIUMF
17
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 18: Thank you! Merci!
juliettem@triumf.ca
Contact
18
Juliette Martin, TRIUMF/The University of Edinburgh
CAP Congress 2022

## Slide 19: Backup

## Slide 20: Efficiency curve
Calibrate spectrometer using PI IntelliCal ® source.
Wavelength and intensity calibrations computed.
Spectra produced treated with efficiency curve
Rudimentary error analysis, potential wavelength miscalibration