## Slide 1
Results – XPS
Different chemical states exhibit energy shifts and structural changes in all main peaks
Complex structure and satellites are observed in Er 4d and Er 3d peaks
Higher energy X-ray’s shift Auger peaks and give rise to stronger photoelectron peaks
Curve-fitting of peak envelopes with constraints should be employed for more accurate speciation
Elemental ratios from survey quantification and counterion peaks must also be considered and compared to the expected chemistry and stoichiometry
All high-resolution spectra are charge corrected to the alkyl-type component of C 1s at 284.8 eV
XPS is used to elucidate the chemical states of REE’s within each ore or material. To accurately identify these chemical states, reference spectra of pure REE compounds are needed. These compounds exhibit complex structures and suffer from various broad overlapping Auger peaks in regions of interest, thus higher energy X-rays (Ag L𝛼) are also being utilized.
Erbium is one of the Rare Earth Elements (REE’s), the only class of critical minerals* common to all member nations of the Minerals Security Partnership.[1] REE’s are essential to support our advancing and increasingly sustainability focused economies with applications in all major energy industries, electric vehicles (EV’s), advanced consumer electronics, catalysts, and many other areas.
Production challenges and geopolitical tensions are creating supply chain risks for REE’s. To maintain responsible resource management and disposal strategies, it is crucial to have a comprehensive understanding of the properties and quality of REE-containing materials.
This work is an effort to advance current methodologies surrounding the analysis and characterization of REE’s, with a focus on erbium. We present preliminary Rutherford Backscattering Spectroscopy (RBS) results on creating ion-implanted calibration standards for erbium Secondary Ion Mass Spectrometry (SIMS) analyses, and in-depth X-ray Photoelectron Spectroscopy (XPS) studies of erbium standards and REE-containing minerals of significance.
*Critical Minerals:[1]
“Have few or no substitutes
Are strategic and somewhat limited commodities; or
Are increasingly concentrated in terms of extraction and, even more, in terms of processing location”
They are important, and there are risks with their supply chains
                Permanent magnets
                Generators, motors, EV’s, MRI’s
          Electronics
              LED’s, cell phones, batteries, IR optics, LCD screens, speakers
          Catalysts
            Catalytic converters
            Energy
            Nuclear control rods, solar cells, wind turbines, fossil fuel refining
Applications of REE’s:
Introduction
By improving our ability to detect and accurately identify REE’s, we support the critical initial and final steps in both streams of the REE supply chain.
Results – Ion Implantation and RBS
A Multimodal Approach Towards Advancing the Characterization and Analysis of Erbium
Sage Buchanan1,2, Dr. Lyudmila Goncharova2,3, Dr. Mark Biesinger1,3
1Surface Science Western, The University of Western Ontario, London N6G 0J3, ON, Canada
2Department of Physics and Astronomy, The University of Western Ontario, London N6G 2V4, ON, Canada
3Department of Chemistry, The University of Western Ontario, London N6A 3K7, ON, Canada
Goal: To enhance the detection, chemical state identification, and recovery capabilities of erbium and other critical rare earth minerals for improved mineral security and economic stability
Rare Earth Element Supply Chains
  This work is supported by Natural Science and Engineering Research Council of Canada (NSERC) Discovery Grants as well as funding from the Canadian Foundation for Innovation and Ontario Research Fund for the Kratos AXIS Supra spectrometer. The mineral samples analyzed in this work were supplied by the Dana Collection, courtesy of the Richard W. Hutchison Geoscience Collaborative Suite. Special thanks to Jack Hendriks for assistance in operating the Tandetron Accelerator, Dr. Todd Simpson and Tim Goldhawk from the Western nanofabrication facility for the implant mask depositions and initial mask removal, and Dr. Jeffrey Henderson for assistance in XPS and EDX analyses and processing.
Acknowledgements
                Improvements on methods of detecting, identifying, and quantifying REE’s such as XPS can inform and enhance recovery procedures to strengthen REE supply chains from both mining and recycling
                Ion implantation with RBS verification could be a promising method to develop custom calibration standards for SIMS analyses in a semi-affordable and efficient fashion – more testing is needed
                Light REE’s were found in interstitial regions between the associated barite (BaSO4) and calcite (CaCO3) mineral grains
                [1] Service Canada. “The Canadian Critical Minerals Strategy.” (2022)
                [2] U.S. Department of the Interior “Mineral Commodity Summaries” (2023)
                [3] S.L. Liu et al. Ore Geology Reviews 157 (2023):
                [4] T. McNulty et al. MRS Bulletin 47, no. 3, 258–266 (2022)
                [5] J.F. Ziegler et al. Nuclear Instruments and Methods in Physics Research Section B: Beam Interactions with Materials and Atoms 268, no. 11, 1818–1823 (2010)
                [6] J.F. Moulder et al. Handbook of X-ray Photoelectron Spectroscopy (1992)
Conclusions and References
Decreased cost
Decreased time
Decreased waste
Increased yield
Increased efficiency
Increased viability
Bastnaesite, (Ce, La, Y)CO3F
Global supply of REE’s is still largely monopolized by China, as shown in Figure 1. While a few other countries are (re)emerging as REE producers, Canada currently produces no REE’s commercially and the U.S. remains >95% reliant on imports for their current REE consumption.[1, 2]
As demand rapidly increases, it is essential to enhance the feasibility and efficiency of REE production through both mining and recycling. Current recovery estimates from mined ores range from 50-80%[4], which we aim to improve upon, alongside strengthened recycling efforts by advancing our abilities to detect and quantify the chemical states of REE’s using calibration standards and analyzing reference materials.
Tandetron accelerator
Implant chamber
High energy magnet
RBS chamber
ERD chamber
Injector
magnet
Duoplasmatron source
Sputter source
(Er2O3)
MEIS chamber
Molecular Beam Epitaxy systems
1 m
Quadrupoles
Raster scanner
Implant
apertures
Figure 1: Global mine production by country of yttrium-containing rare earth oxides. Reprinted with permission from Liu et al. [3]
Ion implantation is being tested as a method to create calibration standards for SIMS analyses as known concentrations can be implanted.
Our method involves:
Using SRIM[5] simulations to inform implant conditions
Implanting Er+ ions into Si wafers shielded by removable masks via the Tandetron accelerator
  Masks are used to achieve desired implant depths
Conducting RBS with He+ ions to analyze the depth profiles of the implanted wafers and to evaluate for beam damage and/or contamination
Figure 2: SRIM[5] simulations of implanting Er+ ions into Au/Ti/Si showing a) the concentration of Er+ ions with target depth and b) Monte-Carlo simulated paths the implanted ions take in the y-z plane.
Figure 3: An exaggerated model of the Er+ into Si implantation layer structure. Au and an adhesive Ti layer were used as a temporary mask to intentionally stop the ions nearer to the surface of the Si substrate.
Figure 4: Curve-fit RBS spectrum of the Si wafer after Er+ implantation and aqua regia etching to remove the Au/Ti masking layer.
Figure 7: a) An optical image of a cross-section of bastnaesite, the red box indicates where Energy Dispersive X-ray maps were taken of b) barium (yellow) and calcium (orange), c) barium (yellow), lanthanum (blue), and cerium (red), and d) fluorine (green) and sulfur (cyan).
Table 1: XPS survey scan atomic percentages from different areas on the bastnaesite surface. Rare earths detected are highlighted in yellow.
C
O
Si
Ti
Er
Au
Er distribution
1 mm
1 mm
1 mm
a)
b)
c)
d)
CaCO3 +
(Ce, La)CO3F
BaSO4
Ba
Ce
La
Ca
S
F
Ba
10 mm
Au and Ti remain trapped
Research Fund
Yield
Energy (keV)
200
300
400
500
600
700
800
900
1000
1000
100
10
1
y
x
z
Au (50 nm)
Ti (10 nm)
Si
Er+
Etched off with aqua regia (3HCI + HNO3) after implanting
Si
a)
(Atoms / cm3 ) / (Atoms / cm2)
Target Depth (Å)
0
5000
x104
10
8
6
4
0
2
Au
Ti
Avg. Depth: 1179 Å
Straggle: 814 Å
b)
Depth vs. Y-axis
Er 3d
Er M4VV
Er 4d
A Multimodal Approach Towards Advancing the Characterization and Analysis of Erbium
Sage Buchanan1,2, Dr. Lyudmila Goncharova2,3, Dr. Mark Biesinger1,3
1Surface Science Western, The University of Western Ontario, London N6G 0J3, ON, Canada
2Department of Physics and Astronomy, The University of Western Ontario, London N6G 2V4, ON, Canada
3Department of Chemistry, The University of Western Ontario, London N6A 3K7, ON, Canada
Figure 5: Normalized spectra of the a) Er 4d, b) Er 3d, and c) Er M4VV peaks from each erbium standard compound measured. Main peak positions are highlighted with the dotted red lines to show the shifts observed with changes in chemical state. *Surface oxide is still observed in Er metal, noted by the presence of the O 1s peak (Figure 6) and rounded Er 4d structure.[6]
a)
b)
c)
Figure 6: Survey scan spectra of Ar500+ sputter-cleaned Er metal taken with Al K𝛼 (blue) and Ag L𝛼 (red)
X-ray sources. Spectra are normalized to the Er 4d peak at 168 eV. Auger peaks are marked in green.
Strong Er 3d peaks visible
Auger peaks ‘shift’ to higher binding energy
With Al K𝛼 X-rays, Er Auger peaks interfere with many peaks of interest, notably the C 1s peak
Al K𝛼 – 1486.6 eV
Ag L𝛼 – 2984.3 eV
Er 3p1/2
Er 3p3/2
Er MNN
O KLL
Er 3d3/2
Er 3d5/2
O 1s
O KLL
Er MNN
Er 4s
Er 4p
Er MNN
Er 4d
Er M5VV
Er M4VV
Er MNN
C 1s
Peaks shift with chemical state
Change in peak structures
Satellites
Notes: Countries with common critical mineral designation:
- Canada
- USA
- The European Union
- United Kingdom
- Japan
- Australia
- India
- South Korea
- South Africa
Bastnaesite enriched in barium, maybe some barium oxides?
Strontium also found in association with barite
Will try aqua regia next to etch out gold and titanium as nitric, sulfuric, and hydrochloric acids and potassium iodide didn’t work