## Slide 1: Simulation of the effects of charge on the kinetics of a triblock copolymer hopping across a membrane
Sylvia Luyben, Rob Wickham
University of Guelph
CAP Congress
May 27, 2024

## Slide 2: Protein Reconstitution → Polymer Hopping
Hydrophilic
Hydrophilic
Hydrophobic
Notes: This work was motivated by protein reconstitution, an experimental process whereby proteins are moved from their native domains into membranes of practical use. We model the protein as a polymer with the same structure as the membrane I’ve shown here: hydrophilic end regions, and hydrophobic centres.

## Slide 3: Protein Reconstitution → Polymer Hopping
To enter a membrane, the polymer must insert and change conformations
From looped
To bridged
The kinetics of hopping can help us understand protein reconstitution.
Conformation affects material strength1.
1. Hua, Kuang, and Liang. J. Am. Chem. Soc. 2011, 133, 2354–2357. dx.doi.org/10.1021/ja109796x
2. Matsen and Thompson. J. Chem. Phys. 111, 7139–7146 (1999) . https://doi.org/10.1063/1.480006
Experimental evidence shows charge can affect both2.
Notes: Now we consider a polymer entering a membrane. To do so the polymer must insert and change configurations
=um distribution

## Slide 4: How does charge affect end block hopping?

## Slide 5: The Model: Triblock Copolymer in Electrolyte Solution
A1
A2
B
Hydrophilic
Charged
Hydrophilic
Charged
Hydrophobic
Neutral
Scaling
Length: b
Rouse Time: 𝜏R =
+
−
+
+
+
+
−
−
−
S
Notes: Highlight solvent (membrane not melt) and charge

## Slide 6: dynamical Self-Consistent Field Theory
Many interacting chains
Single chain in a dynamic mean field
Dynamical partition function
Saddle point approximation
𝜀AA
𝜀BB
𝜀AB
𝜀SS
𝜀AS
𝜀Bs
Notes: “powerful multi-scale approach that allows us to access long time and length scales while maintaining single chain conformations”
“self-assembly”

## Slide 7: Neutral Membrane Formation
Charge | 0.0e
𝜀AA | 0.075
𝜀AB | 0.075
𝜀AS | 0.09
𝜀BB | 0.085
𝜀BS | 0.09
𝜀SS | 0.075
NA1-NB-NA2 | 8-32-8
n | 220
x
y
z
solvent
solvent
Notes: PERIODIC
"first things is to form a stable POLYMER membrane"
Back up slide with equations, and one with force definitions

## Slide 8: Membrane Stress, 𝜎
𝜎xx=𝜎zz
𝜎xx>𝜎zz
n<nequ
n=nequ
𝜎xx<𝜎zz
n>nequ
x
y
z

## Slide 9: Stress vs. Density
Chart: Chains per Unit Area
| 0.2138671875 | 0.1474609375 | 0.13671875
Long Neutral | -0.021563 | 0.00037717 | 0.0035341
Long 0.5 | -0.023451 | -0.026093 | -0.027359
Short 0.5 | 0.00021396 | -0.0022211 | -0.0031899
Short Neutral | 0.0019262 | -9.8648e-05 | -0.00403
Zero | 0 | 0 | 0 | 0 | 0 | 0 | 0
 | NA-NB-NA | Charge /e
● | 16-32-16 | 0.0
● | 16-32-16 | 0.5
◼︎ | 8-32-8 | 0.5
◼︎ | 8-32-8 | 0.0
Debye length = 1b
Notes: Units on axes
"8-32-8 is symmetric"

## Slide 10: Neutral Polymer Insertion
Charge | 0.0e
𝜀AA | 0.075
𝜀AB | 0.075
𝜀AS | 0.09
𝜀BB | 0.085
𝜀BS | 0.09
𝜀SS | 0.075
NA1-NB-NA2 | 8-32-8
n | 220
x
y
z
Notes: put b on axis

## Slide 11: Neutral Polymer Block Centers of Mass
z Position / b
Time / 𝜏R
A1
A2
Charge | 0.0e
𝜀AA | 0.075
𝜀AB | 0.075
𝜀AS | 0.09
𝜀BB | 0.085
𝜀BS | 0.09
𝜀SS | 0.075
NA1-NB-NA2 | 8-32-8
n | 220
Jump time
Notes: emphasize algorithm: back up slide
how long / many simulations

## Slide 12: Neutral Membrane Charged Membrane
Position /b
Density /b-3
Chart: 
Chart: 
Solvent
A Block
B Block
Debye length = 1b
0.5e / bead
0.148 chains/b2
0.0e / bead
0.173 chains/b2

## Slide 13: Jump Time Distribution
Charge | 0.0e 0.5e
Total points | 225 120
𝜀AA | 0.075
𝜀AB | 0.075
𝜀AS | 0.09
𝜀BB | 0.085
𝜀BS | 0.09
𝜀SS | 0.075
NA1-NB-NA2 | 8-32-8
Characteristic decay time
Adding polymer charge?
Increasing forces?
Detergent molecules?
Notes: Intro graph, how did you make it
define blue and red: legend

## Slide 14: Conclusions
Developed dynamical self consistent field theory for polyelectrolyte solutions
Simulated stable membranes in different charge states
Created a routine to categorize polymer conformations
Analyzed jump time distribution for charged and neutral membranes
Questions?

## Slide 15: Categorization: Directional Gating

## Slide 16: Numerical Process
Solvent field
Electric Potential
Mean-field Interparticle force
New solvent field
New particle positions
Number density
Charge density
Particle positions
Time
Poisson-Boltzmann equation
Notes: Introduce any needed symbols

## Slide 17: Mean Field Equations

## Slide 18: Stress:
The stress, 𝜎, in the 𝛽 direction, due to a force in the 𝛼 direction is measured by bond lengths
Stress
𝛽
𝛼
Chain 𝓁
let us quantify the stability of the membrane.
Notes: make this backup