## Slide 1: Superconducting Radiofrequency research and development at TRIUMF and UVic
Tobias Junginger, Aveen Mahon, Daniel Hedji, Lucas Wallace, Noah Gorgichuk, Oliver Kester, Philipp Kolb, Robert Edward Laxdal, Rogério de Sousa, Ryan McFadden, William Stokes, Md Asaduzzman, Edward Thoeng

## Slide 2: Superconductivity for accelerators
Particle accelerators use superconductors to steer and increase the energy of charged particles
Bending Magnets of the LHC
Superconducting Radiofrequency (SRF) cavities of the LHC
Cross section of wire with
NbTi filaments in a copper matrix

## Slide 3: Particle Acceleration with cavities
H
E
beam direction
Particle bunch
H
E
beam direction
Particle bunch
H
E
beam direction
Particle bunch
1. Acceleration with radiofrequency cavities requires synchronization of particles and RF field. Outside of the cavity the approaching particle bunch does not experience the RF field
2. The particle bunch enters the cavity. The electric field is pointing in the direction of the beam axis  The particle is accelerated
3. The particle bunch leaves the cavity. The field direction has changed again
Faraday's law of induction:
Ohm‘s law: =σE
Cavities are used to accelerate particles by an alternating electric field
An oscillating electric field causes an oscillating magnetic field
The cavity confines the electromagnetic fields by surface shielding currents
These currents create losses (heating), which can be reduced by using superconducting materials
Why is niobium the material choice which requires costly helium cooling?

## Slide 4: Two types of superconductors
Material | Lead | Nb | NbTi | Nb3Sn
Bc[T] | 0.07 | 0.2 | 0.2 | 0.52
Bc1[T] | - | 0.17 | 0.01 | 0.05
Bc2[T] | - | 0.24 | 11 | 28
Bsh[T] | 0.08 | 0.24 | 0.16 | 0.44
A type II superconductor can split into normal and superconducting areas to lower its energy
Magnetic fields partially enters into the normal conducting areas in the form of flux tubes
Under DC fields flux tubes can be pinned –> no dissipation
  SC magnets are operated between Bc1 and Bc2
Under RF fields flux tubes oscillate –> strong dissipation
  RF cavities are operated in the Meissner state
  For defect free surfaces the Meissner state can persist metastable up the superheating field Hsh
Bc

## Slide 5: SRF Accelerators in Canada
TRIUMF
Canadian Light Source
ISAC-II
ARIEL e-linac

## Slide 6: TRIUMF ARIEL e-LINAC - Reliable 30MeV Operation
Stable 30MeV operation is critical for Radioactive Ion Beam (RIB) production:
RIB yield is strongly dependent on beam energy
TRIUMF is operating at 30MeV (3 cavities each delivering 10 MV/m) – at the lower end of the yield curve
Field emissions from contaminants in the SRF cavity limit RF performance to lower
Prevention and mitigation critical to keeping performance high, to keep RIB yield high
Field Emission limits performance to
Clean cavity reaches

## Slide 7: TRIUMF ARIEL e-LINAC - Reliable 30MeV Operation
Plasma cleaning
Current cleaning procedures are done ex-situ (2-3 months).
Plasma cleaning allows for an in-situ cleaning, which reduces cleaning time to ~1 week. MSc project D. Hedji
What if we could avoid contamination in the first place?
Emitters are μm to sub μm sized contaminants  dust
Previous studies indicate that dust migrates and is charged:
  A potential barrier could therefore suppress dust migration and tackle field emission problem at its source.
PhD A. Mahon
PI T. Planche
MSc. D. Hedji
P.I. R.E. Laxdal

## Slide 8: SRF materials research
Current material of choice niobium is reaching fundamental limitations
Subtle changes in heat treatments have significant influence
Surface treatments have only been optimized for electron accelerators (elliptical cavities)
  TRIUMF has dedicated program to optimize co-axial cavities for heavy ion accelerators
Accelerating gradients beyond 50 MV/m require new materials potentially as multilayers
Ultimate limitation Hsh
State of the art niobium cavity performance
Co-axial test cavities

## Slide 9: SRF Material of the future

## Slide 10: SRF Material Science
SRF material science is about engineering the outermost ~100nm of the material by coating or diffusion
Our research focuses on detecting flux penetration with nanometer resolution and its correlation to material properties
β-NMR (TRIUMF) enables flux penetration measurements with nanometer depth resolution
Transmission electron microscopy (UVic) and secondary ion mass spectroscopy (Surface Science Western) reveal surface structure and elemental composition
R. Laxdal, R. McFadden, E. Thoeng, Md Assaduzzaman, W. Stokes, L. Wallace

## Slide 11: SRF for Quantum Computing
Main mechanism for quantum decoherence in current quantum hardware are defect two level systems (TLS) in oxides
SRF cavities can increase coherence times and be used as a testbed for theoretical models
Re-analysis of literature data provides evidence that the TLSs present in niobium oxide are “atomic-like” (instead of “glass-like”) . Undergrad Project N Gorgichuk
Replacing the oxide with another material can increase coherence times (recent results from CEA Saclay)
N Gorgichuk, T Junginger, R de Sousa -
Physical Review Applied 19 (2) 2022
Y. Kalboussi et al. APL 124 2024

## Slide 12: Summary
SRF cavities unlike DC magnets need to be operated in a flux free Meissner state
  Current material of choice for SRF cavities is niobium (largest HC1)
    Performance close to fundamental limits in elliptical cavities
  Meissner state can potentially be maintained above Hc1 using heterostructure coatings
SRF technology is interesting for quantum applications

## Slide 13: Backup slides

## Slide 14: Examples of SRF accelerators
KEK, Japan
DESY, Germany
JLAB, USA
CERN, Switzerland+France
XFEL, Germany, 2018
CERN, Switzerland+France
LHC, 2008
Jefferson Lab, USA
TRIUMF+
Canadian Light Source

## Slide 15: Coaxial Research Cavities at TRIUMF
Most SRF research done on high frequency, high beta, elliptical cavities.
Ion accelerators need low frequency, low beta coaxial cavities.
TRIUMF has dedicated coaxial cavities for fundamental SRF research
QWR
HWR
P. Kolb et al.
Phys. Rev. Accel. Beams 23, 122001
QWR: Quarter Wave Resonator
HWR: Half Wave Resonator
QWR
217 MHz
T=2K
PI R. Laxdal, P. Kolb, MSc R. Gregory, MSc. McMullen
  Multiple modes (=multiple frequencies)
New baking procedures tried for the first time on coaxial cavities
Encouraging results but below expectation (P. Kolb et al. SRF2021)

## Slide 16: Coaxial Research Cavities at TRIUMF
Several new baking procedures tried for the first time on coaxial cavities
Unlike for traditional procedures there is no material removal (chemistry) after baking. Very clean environments required.
Material analysis with SEM/EDX shows signs of carbon contamination. (Honors thesis project D. Hedji)
TOF-SIMS depth profile shows that carbon contamination is most pronounced in relevant near surface region
SEM: scanning electron microscopy, EDX: energy dispersive X-Ray spectroscopy, TOF-SIMS: Time-of-Flight Secondary ion mass spectroscopy
400°Cavity Witness Sample
Reference Sample
SEM image before and after furnace cleaning

## Slide 17: When to use Superconducting Cavities
 | Super Conducting | Normal Conducting
RS | ~100nΩ | 3mΩ
Pdiss | 7 W | 200kW
Grid Power | ≈1kW | ≈400kW
Example: Isac-II CW 141 MHz cavity operated in CW Eacc=5 MV/m
Strongest incentive to use SC cavities is for accelerators operated in CW or at high duty factors
Carnot Efficiency of refrigeration cycle:
Dissipated power:
H
E
In case of SRF systems grid power goes mainly to the cryoplant and the beam, for normal conducting machines mainly in the RF power source

## Slide 18: -NMR + SRF @ TRIUMF
High parallel field spectrometer. Successfully commissioned in summer 2021
Low field magnet
New high field magnet
Low energy muon spin rotation is limited to parallel field to about 25mT
SRF cavities operate at 100-200mT
  Steering in higher field difficult due to low muon mass
  Higher mass of 8Li favors betaNMR with 8Li for SRF studies
R. Laxdal, R. McFadden, PhD E. Thoeng (UBC), PhD Md Assaduzzaman
Method is sensitive to changes by surface treatments
(E. Thoeng et al SRF2021)
Next studies will be on multilayer samples prepared by atomic layer deposition at CEA Saclay

## Slide 19: Measurement of the vortex penetration field
β-NMR studies will be coupled with measurements of superconducting bulk and material properties at UVic
Vibrating sample magnetometry can be used to measure the substrate (niobium) vortex penetration field
  Instruments are commercially available but the SRF parameter range (relatively low field at low temperature) favor a dedicated design which can be realized at a fraction of the cost
  Status: Design finalized, construction started (MSc Lucas Wallace)
TEM/EDX map of a NbTiN on Nb sample
BSc Will Stokes

## Slide 20: Backup slide

## Slide 21: UVic/TRIUMF Accelerator Research
There are no particle accelerators at UVic
Accelerator Research does not necessary require accelerators on site. At UVic we focus on
  Cryocooler based fundamental SRF studies
  Surface and Materiel Science Studies at the Electron Microscopy Facility (A. Blackburn)
  Application of SRF technology to quantum computing (R. de Sousa)
  Beam Dynamics studies for polarized beams in SuperKEKB (M. Roney)
Graduate Program
Currently 14 UVic graduate students in accelerator physics based at TRIUMF (11), UVic (2), D-Pace (1)
Seven adjunct professors, six at TRIUMF, one at D-Pace
Education
One graduate lecture course taught by adjunct faculty at TRIUMF each year and broadcasted nationwide
Undergraduate lecture course, graduate + undergraduate projects offered at UVic
Beam Simulations
Accelerator Systems Development
Material Science
Fundamental SRF studies with purpose built instruments

## Slide 22: The superheating field
Niobium:
  Close to Tc Hentry=Hsh
  T<<Tc usually Hentry<Hsh
Nb3Sn:
  Close to Tc Hentry=Hsh
  T<<Tc Hentry<<Hsh
RF heating proportional to H2. Close to Tc less power is dissipated. Flux entry less likely.
Coherence length of Nb3Sn smaller than Nb. Flux entry at defects more likely.
The good news is Hc1 is not a general limitation!
S. Posen et al. PRL 115, 047001 (2015)