## Slide 1: SuperCDMS & Radon
Ray Bunker
Topics in Astroparticle and Underground Physics
July 26, 2017

## Slide 2: Radon Backgrounds
Inner surface
of lead shield
Inner poly surfaces & Interstitial air gaps
Dilution fridge
Cryostat surfaces
SNOLAB Detector Backgrounds
Non-line-of-sight (penetrating) Backgrounds:
Electron recoils:
 210Bi bremsstrahlung
(limit exposure of surfaces to radon)
 214Pb & 214Bi gamma-rays
(purge lead shield with low-Rn gas)
Nuclear Recoils:
 210Po (α,n) on 13C in poly
(limit exposure of surfaces to radon)
Radon Decay Chain
α
α
α
Non-line-of-sight
Radon Background
≈1% of Total Electron Recoil
Photon Background
Non-line-of-sight
Radon Background
<1% of Total Nuclear Recoil
Neutron Background
Solar neutrinos
Neutrons
Photons
Betas
32Si
32P
3H
206Pb
recoils

## Slide 3: Radon Backgrounds
Line-of-sight (non-penetrating) Backgrounds:
Electron recoils:
 210Pb & 210Bi betas and x-rays
Nuclear Recoils:
 206Pb recoils from 210Po decays
Radon Decay Chain
α
α
α
SNOLAB Detector Backgrounds
detector
copper housing
adjacent detector
210Pb
x-ray
210Bi
β
210Po
206Pb
recoil
Detector-surface Backgrounds
Line-of-sight
Radon Background
≈100% of Detector-surface
Electron Recoils
Line-of-sight
Radon Background
≈100% of Detector-surface
Nuclear Recoils
Potentially dominant backgrounds unless:
Detector/copper surfaces clean at start
And protected from radon thereafter
Calls for dedicated background controls:
Limit exposure to radon during payload lifecycle
Dedicated low-radon cleanroom at SNOLAB
Validate cleanliness of critical processes
Solar neutrinos
Neutrons
Photons
Betas
32Si
32P
3H
206Pb
recoils

## Slide 4: Payload Lifecycle & Radon Exposure
#2
#3
#4
#5
#6
#7
#1
Procedure | 210Pb (nBq/cm2)
#1 – storage | <0.1
#2 – polishing | 12–45
#3 – fabrication | 28
#4 – packaging | 4.8
#5 – tower assembly | 0.9
#6 – testing | 1.1
#7 – installation (w/ 1000x Rn mitigation) | <0.1
#7 – installation (w/o Rn mitigation) | 70
210Pb from Rn exposure (conservative plate-out tally):
Detector surfaces: 47–80 nBq/cm2
  Assume worst for sidewalls  80 nBq/cm2
  Sensor fab removes surface area on faces  50 nBq/cm2
Copper surfaces: <10 nBq/cm2
Plate-out ≈2x larger without low-radon cleanroom

## Slide 5: Low-radon Cleanroom @ SNOLAB via Vacuum-Swing Adsorption (VSA)
SNOLAB General
Lab Air ≈130 Bq/m3
Custom-built Radon Mitigation System
Radon-mitigated Air
<0.1 Bq/m3

## Slide 6: Demonstration VSA @ SDSM&T
Input Air
<Rn> = 80 Bq/m3
Cleanroom Radon
Level <0.07 Bq/m3  >1000x reduction!
Simultaneous RAD7 Readings

## Slide 7: Validation of Critical Processes
Bottom-up estimate of 210Pb plate-out from radon exposure in air:
  Detector surfaces: 50/80 nBq/cm2 for faces/sidewalls
  Tower-copper surfaces: <10 nBq/cm2
But doesn’t include:
Initial level of surface contamination
 do surfaces start clean?
Contamination directly from fabrication processes
(e.g., chemical contact)
R&D tests to validate critical processes:
  Detector surfaces  crystal polishing & sensor fabrication
  Copper surfaces  cleaning method
Σ

## Slide 8: Sensor Fabrication Test
Goals:
Validate starting level of 210Pb on detector surfaces
Validate surface contamination from sensor fabrication
Results:
Broad 4–5 MeV peak suggests upper-chain 238U alphas
Precedent from DRIFT  Battat et al., NIM A794 (2015)
Background concern  234Th daughter beta decay
Follow-up measurements:
  Backsides of wafers  no peak
  ICP-MS of wafers  few Bq/kg of 238U in aluminum
210Po
XIA UltraLo-1800 Spectra (SMU)
Background
Sample
210Po
Background
Sample
    Si wafer substrate
600 nm Al (35%)
40 nm pc-Si
40 nm W
Etch wafers
at Stanford
fab facility
Assay in SMU UltraLo-1800
Fab sensor pattern at Stanford
Assay in SMU UltraLo-1800
Not seen on SuperCDMS Soudan detectors
Working with vendor to pre-screen aluminum
uranium
alphas

## Slide 9: Copper Cleaning Test
1st Test Sample
Goal:
Validate method for cleaning tower copper parts
  And thus starting contamination level for detector housings
Methodology:
Fabricate 2 sets of large-area Cu plates: McMaster & Aurubis OFHC (alloy 101)
Mill off >1 mm from all surfaces to simulate parts fabrication
Clean w/ PNNL acidified-peroxide etching recipe
Use SMU UltraLo-1800 to measure surface alphas
210Po
Background
Sample
Anticipate <100 nBq/cm2 210Pb (>10x better than Soudan)
UltraLo-1800 Background not
Subtracted (≈25 nBq/cm2 in 210Po ROI)
McMaster OFHC
Aurubis OFHC
2nd assay of
1st test sample
Po in Cu bulk

## Slide 10: Summary
Radon is an important background
consideration for SuperCDMS SNOLAB
  210Pb within line-of-sight of detectors
  is a potentially dominant background
Estimate of 210Pb from plate-out:
  Detector faces/sidewalls: 50/80 nBq/cm2
  Copper housings: <10 nBq/cm2
Low-radon cleanroom for installation
at SNOLAB mitigates plate-out by ≈2x
  SDSM&T VSA demonstrates >1000x radon reduction
Validation of critical processes:
  Contamination during crystal polishing negligible
  Discovered uranium in detector-sensor aluminum  working with vendor to eliminate
  Demonstrated copper surfaces with <100 nBq/cm2 210Pb via PNNL acidified-peroxide etch
Demonstrated 210Pb at sidewalls:
detector + copper <200 nBq/cm2

## Slide 11: Collaboration

## Slide 12: Crystal Polishing Test
210Po
210Po
Pre-Process
<200 nBq/cm2
clean enough
for test
Post-Process
<100 nBq/cm2
Cleaner!
Mild etch from
slurry solution
XIA UltraLo-1800 Spectra (SMU)
Goal:
Validate 210Pb contamination rate during polishing
Methodology:
Seven 100 mm Si wafers as proxy for detector surfaces
UltraLo-1800 to measure surface alphas
10,000x radon w/ SDSM&T source to boost sensitivity
210Pb surface contamination during
polishing insignificant  <1 nBq/cm2
Background
Sample
Background
Sample