## Slide 1: Electron and X-ray source based on a pyroelectric crystal driven by a periodically varying temperature
Majid Ali
John Adams Institute at Royal Holloway, University of London, Egham, UK.

## Slide 2: Outline
Majid Ali. Electron and X-ray source based on a pyroelectric single crystal driven by a periodically varying temperature
    Pyroelectric effect
    Particle generation and acceleration using pyroelectric effect
    History and development of pyroelectric accelerator
    COOL-X by Amptek Miniature X-Ray source based on Pyroelectric effect
    Study of pyroelectric accelerator in RHUL
    Experimental results
    Further development

## Slide 3: Pyroelectric effect
Wang, W., Li, J., Liu, H., Ge, S., Advancing Versatile Ferroelectric Materials Toward Biomedical Applications. Adv. Sci. 2021, 8, 2003074.
Main three ways to change the
value or direction of spontaneous polarization.
Application of external electric field
Application of mechanical stress
Variation of temperature

## Slide 4: Particles generation and acceleration using pyroelectric effect
Pyroelectric materials used
Lithium Tantalate, Lithium niobate
Temperature variation
10-100 °c
Pressure Range
Up to 100 mTorr
X ray end point energy
Up to 200 keV
Electron current
Up to 10 nA
Positive ion generators
Nitrogen, oxygen, hydrogen, argon ions (max energy up to 150 keV)
Neutron generators
Fast neutrons energy up to 2.45 MeV
Main Scheme of operation

## Slide 5: Electron emission from LiNbO3
B. Rosenblum, P. Bräunlich, and J. P. Carrico, Thermally stimulated field emission from pyroelectric LiNbO3 Appl. Phys. Lett. 25, 17 (1974); https://doi.org/10.1063/1.1655260
Generating of ferroelectric electron emission.
FEE in a crystal during the pyroelectric effect: upon heating
1974 - Stimulated electron emission by change in temperature of pyroelectric material

## Slide 6: X-ray source based on pyroelectric effect
Electron and positive ion acceleration with pyroelectric crystals
Jeffrey A. Geuther and Yaron Danon , Journal of Applied Physics 97, 074109 (2005); https://doi.org/10.1063/1.1884252)
In 1992, Brownridge published the first report about X-ray generation stimulated by change in temperature of the pyroelectric material
Development of x-ray source based on pyroelectric crystal

## Slide 7: COOL-X by Amptek Miniature X-Ray source based on pyroelectric effect
COOL-X shown with the Amptek XR-100CR X-Ray Detector
The x-ray spectrum obtained by COOL-X.
COOL-X
https://www.amptek.com/internal-products/obsolete-products/cool-x-pyroelectric-x-ray-generator

## Slide 8: Amptek COOL-X, Pyroelectric X-ray Source
DISADVANTAGES
The x-ray flux varies vary from cycle to cycle.
Dead time: without x-ray generation, when thermal phase is change.
Interruptions of particle generation by electric breakdowns
Short lifetime: Approximately 200 hours.
ADVANTAGES
Compact pocket-style X-ray source
Low power: < 300 mW
No radioactive sources
Does not required external high voltage source: Runs on standard 9 V battery
Variable end point energy: up to 35 kV
Weight: 185 g

## Slide 9: Periodically varying temperature of LiTaO3
T(t) = T0 + T1sin(Ꙍt)
L. E. Garn and E. J. Sharp, J. Appl. Phys. 53, 8974 (1982)
L. E. Garn and E. J. Sharp, J. Appl. Phys. 53, 8980 (1982)
ipyr= pAT 1Ꙍcos(Ꙍt)
Sinusoidal temperature variation enable us to produce stable, continues and reproduceable temperature variation cycle by cycle through operation. Which is the key to stable x ray generation.
A periodically varying temperature of pyroelectric as a way of stabilizing particle yield

## Slide 10: Experimental setup in RHUL
Current measurement system
0.01 pA – 20 mA
X-Ray detection system
0.5- 150 keV
Vacuum system
Variable pressure from 0.1 mTorr- atmospheric pressure
Changing temperature system
Roughly 5-70 °c (depend on the frequency of temperature variation)
Temperature monitoring
Temperature monitoring of pyroelectric crystal inside vacuum chamber
Majid Ali. Electron and X-ray source based on a pyroelectric single crystal driven by a periodically varying temperature
Pyroelectric sample: Lithium tantalate (LiTaO3)
Thickness: 10 mm
Area: 2020 mm2
Scheme of experimental setup

## Slide 11: Impact of temperature oscillations shift on stability of x-ray generation
An example of the degradation of the X-ray spectrum recorded in one thermal cycle during periodic temperature variation with the frequency of 2mHz.
A stable mode of periodic generation of an electric field of the approximately identical magnitude.
Such conditions should provide the generation of electrons and X-rays in the same amount with almost the same periodicity.
Cooling system without ice
Initial temperature difference 7 °c
Initial temperature difference 1 °c
Without cooling system
Cooling system with ice
Initial temperature difference 0.5 °c
Initial temperature difference 7 °c
Initial temperature difference 1 °c
Cooling system
(a)
(c)
(b)
Cooling system with ice
Without cooling system

## Slide 12: Stable electron and x-ray generation
Cu (Kα=8.05 keV)
Zn (Kα=8.64 keV)
Ta (Lα=80.8 keV)
Ta (Lβ=9.34 keV)
Ta (Lγ=10.89 keV)
Negative Polarity
Heating phase
Positive Polarity
Cooling phase
Parameters of pyroelectric accelerator during temperature variation with frequency of 2mHz, and at pressure range 1-2 mTorr.
Fe (Kα=6.40 keV)
0.3 nA
0.6 nA

## Slide 13: Influence of the gap between the target and the crystal
Temperature variation frequency: 2mHz
Amplitude: 150mVrms ( Amplifier high gain X10)
Pressure range: 1-2 mTorr
(mm)

## Slide 14: Under investigation, two Crystal System
A paired crystal system was explored in which two 10 mm crystals were arranged in series to double the potential difference across the crystal was observed.
We have tested the two crystals system and produce double potential difference in series.
Now we will try to accelerate electrons with the combined electric field of two crystals to double the maximum x-ray energy.
Peltier element
(0.5nA ) – (-0.5nA)
(0.25nA ) – (-0.25nA)

## Slide 15: Further development, multiple Crystal system
Majid Ali. Electron and X-ray source based on a pyroelectric single crystal driven by a periodically varying temperature
Expected potential difference across the crystal will be double, triple and four time in 2, 3 and 4 crystals system respectively.
The X –ray energy can be further increase by stacking more crystal in series as show.
Single Crystal source
Paired-crystal source
Three-Crystals source
Four Crystals source

## Slide 16: THANK YOU!
Majid Ali Electron and X-ray source based on a pyroelectric single crystal driven by a periodically varying temperature