## Slide 1: 3-D Position Sensitive Semiconductor Gamma-Ray Detectors & Applications
Zhong He
NuSec Workshop, London – March 5, 2025
Acknowledgements
DOD DTRA, DOE NA-22 & DHS CWMD
Cleared for Public Release

## Slide 2: Performance Goals E/E  0.5% FWHM (at 662 keV) Real-time  Imaging + isotope I.D.
Eighteen 221.5 cm3 CdZnTe detectors (108 cm3, 648 grams = 1.43 lb)
3-D -Ray Detectors
1
2
3
4
18
97
2033
Number of photons:
E1
E2




## Slide 3: Typical Gamma-Ray Spectrometers
Measured plutonium spectrum

## Slide 4: Perovskite Semiconductor Gamma-Ray Detectors
Goals
Explore alternative room-temperature semiconductor gamma detectors to achieve energy resolution E/E  1.0% FWHM at 662 keV
Thickness  1.0 cm (for required detection sensitivity)
The majority charge carrier (e or h)   10-2 cm2/V (Ref: CdZnTe ()e  410-2 cm2/V )
Wider band-gap than that of CZT (1.6 eV) – to lower noise in hotter temperatures ( 50C)
Lower cost

## Slide 5: 2021 Results on CsPbBr3 #YH-UM-6R (~12mm thick)
(Without near pixel events)
K & K
Summary:
Hole mobility 22 – 65 cm2/Vs on different CsPbBr3 samples
Two-bias (150V & 200V) method  ()h  6.310-2 cm2/V & h  970 s
1.03%
FWHM
137Cs
Bias = 200 V
Notes:   Measurement condition: (1) Gage card sampling rate = 5 MHz, +/-200mV Digital Rail; (2) Preamp decay correction, trapezoidal filtering for amplitude, CR-RC4 for timing; (3) Ran for 14 hours (then the single anode starts breakdown, pixel cathodes are still working.)
  Notes: From: Matthew Petryk <mpetryk@umich.edu>
  Date: Sat, Oct 16, 2021 at 5:49 PM
  Subject: Re: Question on your hole mu-tao estimate on perovskite (slides #4 & 5)
  To: Zhong He <hezhong@umich.edu>
  I don't expect it to be ballistic deficit, since the shaping times should be long enough in both cases.
  The slides may present it a little confusingly. The Cs photopeak did not drop to 1364 ADC at 150V - the 344 keV photopeak is at 1364 ADC at that bias. There is no Cs photopeak in the 150V measurement. Since I did not have a Cs source at the same time, and because the linearity is good, I estimated that 662 would be at 2624 ADC at 150V based on the positions of the 122, 244, and 344 peaks. This is compared to 2725 ADC for 662 keV at 200V. The assumption is that 344 and 662 keV clouds undergo the same trapping mechanisms.
  The drop from 200V to 150V is about 3.7%. There is very little hole trapping at both biases, which does mean more uncertainty in the calculation. For that reason I agree it's better to call 6e-2 a lower limit. I want to take a measurement at 25 - 50V bias, where we should see more clear trapping.

## Slide 6: Depth Corrected 137Cs Spectra from All 9 Pixel Electrodes
Pixel # | FWHM Resolution 662 keV (%)
1 | 1.30
2 | 1.29
3 | 1.68
4 | 1.76
5 | 1.03
6 | 1.72
7 | 1.91
8 | 1.64
9 | 4.21
E/E < 2% FWHM at 662 keV on 8/9 pixel electrodes.
Notes: Notes: Results were from Matthew Patryk’s October 2021 progress report

## Slide 7: Northwestern CsPbBr3 # YH-UM-3VK (2022)
All nine pixel electrodes performed similarly
Thickness ~4 mm

## Slide 8: Northwestern CsPbBr3 #YH-UM-3VK (137Cs)
Best pixel E/E = 0.91% FWHM
Notes: Notes: YH-UM-3VK is a 3.95 mm thick 3x3 pixelated CsPbBr3 with 1.2 mm pixel pitch, refabricated by Vladislav Klepov from old samples grown by Yihui He. This results from Matthew Petryk’s report of August, 2022.

## Slide 9: Diagnostic Measurements on Charge Transport Properties, Material Uniformity and Stability
NW’s CsPbBr3 # YH-UM-3VK (Photopeak amplitude versus hole drift time at 662 keV)
h+ e-
Pixelated
electrodes
Planar
electrode

## Slide 10: Northwestern Univ. & Argonne National Lab. CsPbBr3 in 2024
Det. # QP2304-7-R1(3) Fabricated on 07/16/24
(Operated for more than 4 months under bias)
7.576.8 mm3 CsPbBr3
7.57.06.8 mm3

## Slide 11: Solution Grown Perovskite from Univ. of North Carolina
FA0.9Cs0.1PbBr3 detector UNC #1, ~1 mm pixel pitch, ~ 3 mm thickness
Au planar electrode, Bi pixel electrodes (opposite to that of Northwestern)
Strongly blocking contact (I-V curve ) at the beginning
The blocking contact behavior disappeared a week later?
We are interested in collaborating with you on perovskite semiconductor gamma-ray detectors
Notes: Note: FA
Note #2: Jinsong said on Nov. - Page 7, I remember the device was under continuous bias for two weeks at a high voltage. The corrosion of Bi electrode should be caused by the lacking of encapsulation. Bi is known not to react with perovskites, reported by many research groups.

## Slide 12
Latest 3-cm Thick CZTs at Univ. of Michigan
All Events E/E = 1.00%
Energy (keV)
Counts
0.60 %
FWHM
ASIC: VAD_UM2.2
Cathode: -3kV
Sampling: 5 MHz
Dynamic Range: 700 keV
137Cs
3 cm
2.2 cm
2.2 cm
CZT #11R2
Notes: With subpixel resolution, we will be able to recover some energy resolution loss as shown here.
However, at lower biases, the diffusion will become larger, subpixel resolution will become poorer, and correction will become less and less effective.
Still at -400V, the subpixel calibration can bring lots of improvement.

## Slide 13: Applications through H3D Inc. (https://www.h3dgamma.com)
Chernobyl Arch by Dr. Willy Kaye of H3D
(2019)

## Slide 14: IAEA Demonstrated Gun-Shaped-M400 to Former U.S. Secretary of Energy
H3D M400
September 2021
IAEA, Fall 2024

## Slide 15
Space Applications
Before balloon launch at NASA CSBF in Fort Sumner,
NM (up ~ 24 – 25 miles), Sept.26th, 2021 (UM Eagle)
Kennedy Space Flight Center, Feb. 10, 2025
TERI (Four 4x4x1.5 cm3 CZTs) is scheduled to be launched by SpaceX CRS-32 in April

## Slide 16: Thank you !