## Slide 1
The Development of Hard X-ray Imaging Detectors at STFC
Dr. Matthew C. Veale et al.
11/02/2026

## Slide 2
Group of 16 people
Expertise in:
  High-Z Semiconductors
  DAQ Development
  Electrical Engineering
  Neutron Detectors
  Scintillator-Based Imaging
STFC Detector Development Group
2

## Slide 3
Clear and Bright X-Ray Imaging with Nanophotonic Scintillators
Dr. Issy Braddock et al.
11/02/2026
10:45
3

## Slide 5
DLSR Synchrotrons
DLSR = Diffraction Limited Storage Ring
Increase in the number and quality of bending and focusing magnets
Reduction of the beam size by over an order of magnitude
×100 increase in brightness
Diamond-II increase in average X-ray energy too (> 20 keV)
5

## Slide 6
6
DLSR Synchrotrons
DLSR = Diffraction Limited Storage Ring
Increase in the number and quality of bending and focusing magnets
Reduction of the beam size by over an order of magnitude
×100 increase in brightness
Diamond-II increase in average X-ray energy too (> 20 keV)
Next-Gen Detectors
Hard X-Rays
High Fluxes
Single Photon Resolution
High Spatial Resolution
Temporal Resolution
Large Areas

## Slide 7
Multiple frames
241Am Spectrum
Parameter | HEXITEC
Pixel Pitch (µm) | 250
Array Size | 80×80
Max Frame Rate (kHz) | ~10
Max Spectroscopic Flux (ph s-1 mm-2) | ~104
Digitisation | Off-chip
Detector Type | Peak Track + Hold
Gain stages (keV in CZT) | 200
 | 600
FWHM@100keV (keV) | CdZnTe: 0.79keV Si: 0.59keV
HEXITEC specifications
Fully spectroscopic X-Ray Imaging Detector
80 × 80 pixel array on a 250 μm pitch
Maximum 10 kHz data output (~100 MB s-1)
7
Notes: Here is a basic overview of HEXITEC.I won’t go into any detail but in short it provides spectroscopic X-ray imaging on an 80x80 pixelated array with a 250 µm pitch.
Key to the context of HEXITEC-MHz is that it is a peak track and hold detector, and that analogue voltages are read out each frame to 4 off-chip ADCs at a maximum frame rate of approximately 10 kHz.
The chip has a programmable dynamic range and was designed for electron readout using high-Z materials including CdZnTe and CdTe, and the 250 μm pixel pitch. These attributes have resulted in experimentally measured FWHM at 100 keV of less than 1 keV. In fact, in high-flux CZT sensors, the FWHM of the Am241 59.54 keV photo peak has been reported to be 0.79 keV, whilst it has been measured to be 0.59 keV in 300 μm thick p-type Si.

## Slide 8
Server Computing Nodes
2x 10G UDP Ethernet
Raw Data Frames
ODIN DATA
Spectra per pixel in .hdf5
Speed/latency depends on computing power, processing plug-ins, storing to disk…
2023
2×6 Camera
8

## Slide 9
9

## Slide 10
Spectral X-ray Radiography for Uranium Assay
Andy Gilbert
Pacific Northwest National Laboratory
10

## Slide 11
11
A least-squares fitting algorithm finds the uranium composition that is most consistent with the observed data
  Acquisition times = 30 minutes per sample
Output of algorithm is areal densities (g/cm2) for each element at each detector pixel, which is used to calculate uranium mass
Radiography, energy summed
Transmitted spectra
Estimated uranium mass
Data Analysis
11

## Slide 12
12
12
A least-squares fitting algorithm finds the uranium composition that is most consistent with the observed data
  Acquisition times = 30 minutes per sample
Output of algorithm is areal densities (g/cm2) for each element at each detector pixel, which is used to calculate uranium mass
Radiography, energy summed
Transmitted spectra
Estimated uranium mass
Data Analysis

## Slide 13
Parameter | Value
Pixel Pitch (mm) | 250
Array Size | 80 × 80
Max Frame Rate (MHz) | 1.0
High Gain (keV) | 2 – 100
Medium Gain (keV) | 2 – 200
Low Gain (keV) | 2 – 300
FWHM@100keV (keV) | 1
Key specifications:
  80 × 80 pixels @ 250 mm pitch
  <1 keV FWHM @ 2 – 300 keV
  Static gain
  1 MHz continuous frame rate
  2-side buttable
  13W (~ 2 mW chn-1)
Per pixel spectroscopy @ 2×106 ph s-1 mm-2
  ×100 increase in capability 
https://doi.org/10.1088/1748-0221/18/07/P07048
13

## Slide 14
14
Parameter | Value
Pixel Pitch (mm) | 250
Array Size | 80 × 80
Max Frame Rate (MHz) | 1.0
High Gain (keV) | 2 – 100
Medium Gain (keV) | 2 – 200
Low Gain (keV) | 2 – 300
FWHM@100keV (keV) | 1
Key specifications:
  80 × 80 pixels @ 250 mm pitch
  <1 keV FWHM @ 2 – 300 keV
  Static gain
  1 MHz continuous frame rate
  2-side buttable
  13W (~ 2 mW chn-1)
Per pixel spectroscopy @ 2×106 ph s-1 mm-2
  ×100 increase in capability 
https://doi.org/10.1088/1748-0221/18/07/P07048

## Slide 15
Spectroscopic radiography
  High-Z elements separated by n=1
Dynamic spectroscopic radiography
  Ion drift in solution with dt = 250ms
Radiography, Energy & Angular Diffraction Imaging (READI)
  High-Z powder samples
Application
15

## Slide 16
Spectroscopic radiography
  High-Z elements separated by n=1
Spectroscopic Radiography
8-minutes, 5x5 pixel average
1-minute, single pixel
K-edges
K-edges
16

## Slide 17
Dynamic Measurements
Dynamic spectroscopic radiography
  Ion drift in solution with dt = 250ms
17

## Slide 18
X-ray READI
READI: Radiography, Energy & Angular Diffraction Imaging
  High-Z powder samples (LaB6)
La K-edge
18

## Slide 19
19
Application
Spectroscopic Radiography + ED-XRD + AD-XRD
  High-Z powder samples (LaB6)
La K-edge
HEXITEC User Meeting 2026
Institute of Physics – 27/02/26

## Slide 20
The XIDyn Collaboration
20

## Slide 21
TSMC 65nm process
192×144 pixels, 110mm pitch
>100kHz frame rate
Flux capability > 1011 ph s-1 mm-2
2-stage charge cancelation architecture
Full chip submission March 2026
Quad demonstrator early 2027…
The XIDyn Detector
21

## Slide 22
22
TSMC 65nm process
192×144 pixels, 110mm pitch
>100kHz frame rate
Flux capability > 1011 ph s-1 mm-2
2-stage charge cancelation architecture
Full chip submission March 2026
Quad demonstrator early 2027…
The XIDyn Detector

## Slide 23
Sensor Materials are Critical!

## Slide 24
Notes: The abstract pattern can be removed or repositioned if required. Be careful to ‘Send to Back’ so that it does not obscure any important information.

## Slide 25
X-ray Bay (160kV)
Photocurrent & Imaging
STFC Detector Development Group
Alpha Particle Spectroscopy
(mt Evaluation)
4K Photoluminescence
Optoelectronic Characterisation
25

## Slide 26
ASIC Technology & Hybridisation Capabilities
STFC Detector Development Group
26