## Slide 1
e—cloud, SEY studies and electron induced desorption from cryogenic surfaces.
R. Cimino LNF-INFN
Thanks to F. Ruggiero

## Slide 2
Introduction
e-cloud mitigation methods in a global scenario: compatibility with impedance, vacuum, etc.
Few examples: LASE/LESS – low SEY coatings (a-C)
Conclusions
OUTLINE

## Slide 3: Introduction
1. The beam interacts with the rest gas in the vacuum chamber causing:
  reduced beam lifetime - and/or emittance growth - trigger avalanche multiplication processes
2. The vacuum system plays an important role for beam stability:
  Its material(s) conductivity, shape, coating mainly determine resistive wall impedance of a machine
  Transitions between pipes, bellows, etc. significantly contribute to the global machine impedance
  Total impedance needs to be kept below a certain budget to allow operation at the desired intensity.
3. The vacuum chamber also affects beam stability and lifetime otherwise
  Its inner wall surface properties in particular desorption and electron yields, are critical
  High desorption yields can lead to pressure runaway
  High electron yields can lead to electron cloud formation
  Distributed pumping from surface/design (e.g. NEG coating, pumping holes)
  Shape optimization for photon absorption (antechambers, slits)
The performance reach of accelerators crucially depends on the vacuum system

## Slide 4
Pumping slots
Pumping slots
shields
Cu layer
Cooling tubes
“Saw teeth”
A Functional diagram (here shown for the BS of LHC) must be fulfilled.
EIC (with/without BS) will also have one.
V. Baglin et al. CERN-ATS-2013-006
e- cloud control and mitigation is one (important) aspect in a much more general scenario.
LHC Beam Screen (BS)
Dipole cold bore at 1.9 K

## Slide 5: e- cloud formation
Generation of electrons inside the vacuum chamber
(primary, or seed, electrons)
Photoelectrons from synchrotron radiation
Desorption from the losses on the wall
Residual gas ionization
R. Cimino and T. Demma “Electron cloud in Accelerators” Int. J. Mod. Phys. A 29 (2014) 1430023.

## Slide 6: e- cloud formation
Generation of electrons inside the vacuum chamber
(primary, or seed, electrons)
E
q
secondaries
elastically reflected
Acceleration of primary electrons in the beam field
Secondary electron production when hitting the wall
(F.Zimmermann)
Primary e-
After bunch passage
R. Cimino et al PRL 2004
R. Cimino and T. Demma “Electron cloud in Accelerators” Int. J. Mod. Phys. A 29 (2014) 1430023.

## Slide 7: e- cloud formation
Generation of electrons inside the vacuum chamber
(primary, or seed, electrons)
Acceleration of primary electrons in the beam field
Secondary electron production when hitting the wall
Avalanche electron multiplication
Tx to F. Ruggiero
R. Cimino and T. Demma “Electron cloud in Accelerators” Int. J. Mod. Phys. A 29 (2014) 1430023.

## Slide 8: e- cloud formation
Tx to F. Ruggiero
After the passage of several bunches, the electron distribution inside the chamber reaches a stationary state (electron cloud)
The presence of an e-cloud inside an accelerator has consequences on the machine (pressure rise, outgassing, heat load, etc.) and on the beam (Coherent instability, both single and multi-bunch driven, emittance growth, luminosity and Energy loss, etc.). Needs to be mitigated!
Tx to G. Rumolo

## Slide 9
External solenoid field
Existing and planned accelerator machines base the reaching of their design parameters to the capability of obtaining walls with a SEY ~1.1 or below!
Electrodes in the lattice
Electron and/or photon Scrubbing
Intrinsically low
SEY material
Geometrical modifications
Mitigation Strategies
Active elements
Surface
modification
Run with low e- cloud
filling partners
Machine
operation
Need to be compliant with all specs in the global scenario

## Slide 10
Mitigation Strategies
External solenoid field
Electrodes in the lattice
e- and/or Ph. Scrubbing
Intrinsically low SEY material
Geometrical modifications
Run with low e- cloud
filling partners
Costly and not always applicable
Costly, not always applicable, impedance?
Time consuming, not stable and “asymptotic”
Impedance, stability, adhesion, etc
Impedance, dust, vacuum behavior.
Costs machine performance (reduced n. of bunches)
Issues:

## Slide 11
Mitigation Strategies
External solenoid field
Electrodes in the lattice
e- and/or Ph. Scrubbing
Intrinsically low SEY material
Geometrical modifications
Run with low e- cloud
filling partners
Costly and not always applicable
Costly, not always applicable, impedance?
Time consuming, not stable and “asymptotic”
Impedance, stability, adhesion, etc
Impedance, dust, vacuum behavior.
Costs machine performance (reduced n. of bunches)
Issues:

## Slide 12
Intrinsically low
SEY material
Geometrical modifications
Mitigation Strategies
NEGs, a-C
R. Valizadeh, (2014, 17)
LASE
Not-scrubbed
Cu
a-C
LESS/LASE
Threshold
for e-cloud
In HL- LHC triplets
LESS
Low SEY is a
morphological effect
a-C
Low SEY results from the electronic properties
- Nano -
LASE/LESS

## Slide 13
Mitigation Strategies
External solenoid field
Electrodes in the lattice
Machine Scrubbing
Intrinsically low SEY material
Geometrical modifications
Run with low e- cloud
filling partners
Costly and not always possible
Costly, not always possible, impedence?
Time consuming, not stable and “asymptotic”
Impedance, stability, adhesion, etc
Impedance, dust, vacuum behavior....
Costs machine performance (reduced n. of bunches)
Issues:
But, within the global context:

## Slide 14
R. Valizadeh et al. , Appl. Phys. Lett. (2014)
R. Valizadeh et al. , Appl. Surf. Sci. (2017)
surface morphology of LASE/LESS
Limiting SEY with LASE/LESS -Cu
The structure is expected to have higher impedance (by construction), to be prone of producing dust during formation and to have a much augmented vacuum surface
Very low SEY
R. Valizadeh, et al. Appl. Phys. Lett. 105, 231605 (2014)

## Slide 15
Ongoing LASE/LESS-Cu Impedance studies
Sample | Scan speed [mm/s] | Groove depth [m] | Rs [] | Rs [] |  | 
 |  |  | average | 0 | 45 | 90
Cu | untreated | - | 0.033 |  |  | 
(a) | 180 | 8 | 0.078 | 0.11 | 0.11 | 0.095
(b) | 120 | 20 | 0.13 |  |  | 
(c) | 90 | 35 | 0.14 | 0.15 | 0.19 | 0.20
(d) | 60 | 60 |  |  |  | 
(e) | 30 | 100 |  |  |  | 
See: O. Malyshev et al. e-cloud 2018 Proceeding (2020); R. Valizadeh, et al. Appl. Phys. Lett. 105, 231605 (2014)
SEY and surface resistivity strongly depend on LASE structure (presence and groove directions)

## Slide 16
Ongoing LASE/LESS-Cu Impedance studies
Optimization is in progress!
Impedance and dust production are still open issues
1 µm
Collected particles after Ultrasounds cleaning

## Slide 17
Mitigation Strategies
External solenoid field
Electrodes in the lattice
Machine Scrubbing
Intrinsically low SEY material
Geometrical modifications
Run with low e- cloud
filling partners
Costly and not always possible
Costly, not always possible, impedence?
Time consuming, not stable and “asymptotic”
Impedance, stability, adhesion, etc
Impedance, dust, vacuum behavior.
Costs machine performance (reduced n. of bunches)
Issues:

## Slide 18
Low intrinsic SEY (NEG and a-C)
Typically high surface resistance of impact to impedance.
We know that: - SEY is very surface sensitive
- Surface resistance skin depth ~ 0.1-10 mm
Can the coating be thin enough to reduce SEY without affecting material surface resistance within the skin depth?
(Of course NEG is deposited not only to reduce SEY but its thickness grant pumping reservoir so... It is a different story!)
Coatings:

## Slide 19
We followed the growth of thin a-C layers on Cu with XPS to measure its thickness
Increasing C
How a Coating modify SEY? (the case of a-C on Cu)
XPS
Graphite road
a-C thermal evaporator
M. Angelucci et. al; Rap. Comm in Phys. Rev. Report, in print

## Slide 20
We followed the growth of thin a-C layers on Cu with XPS to measure its thickness
Increasing C
How a Coating modify SEY? (the case of a-C on Cu)
Graphite road
a-C thermal evaporator
M. Angelucci et. al; Phys. Rev. Research Rapid comm. 2, 032030(R) (2020)
C 1s
Cu 2p

## Slide 21
We followed the growth of thin a-C layers on Cu with XPS to measure its thickness
Increasing C
How a Coating modify SEY? (the case of a-C on Cu)
Graphite road
a-C thermal evaporator
C 1s
Cu 2p
In XPS:
where d is the unknown thickness and l is the inelastic mean free path.
{
We can convert
deposition Time in nm (+30%)
M. Angelucci et. al; Phys. Rev. Research Rapid comm. 2, 032030(R) (2020)

## Slide 22
By simultaneously follow SEY changes with a- C thickness we can measure SEY dependence on the actual a-C coverage.
Increasing C
How a Coating modify SEY? (the case of a-C on Cu)
M. Angelucci et. al; Phys. Rev. Research Rapid comm. 2, 032030(R) (2020)

## Slide 23: How a Coating modify SEY? (the case of C on Cu)
 dmax (<1) and Emax are set after 6-8 nm of a-C
dmax, Emax set to their (a-C) final values quite soon, while minor changes still occurs at higher doses in the very low (< ~ 20 eV) and at quite high primary energy (> ~400 eV) part.
dmax vs C coverages
Emax vs C coverages
M. Angelucci et. al; Phys. Rev. Research Rapid comm. 2, 032030(R) (2020)

## Slide 24
L. A. Gonzalez et al., AIP Adv. (2017)
SEY is very surface sensitive:
at LT (10 K) small quantities of contaminants affects it!
SEY is highly sensitive to the presence of adsorbates, even at sub-monolayer coverages
SEY of cold surfaces influenced by gas physisorption

## Slide 25: SEY Surface sensitivity: gases on LT Cu
Kuzucan et al., J. Vac. Sci. Technol. A (2012)
CO thick layer coverage
SEY is an intrinsic material property strongly sensitive to the surface composition and chemical state
L. Spallino, M. Angelucci and R. Cimino, Phys. Rev. Acc.& Beams 23, 063201 (2020)
V . Baglin, et al Proceedings of EPAC 2000, Vienna, Austria
H2O thick layer coverage
Ar thick layer coverage
Element and coverage specific

## Slide 26: gases on Low Temperature surfaces will not only enhance/modify SEY but also electron (and photon, if present) induced desorption.
Studied for 300 eV electrons with (see: H. Tratnik et al., Vacuum 81, 731, 2007)
1) Pure gas 2) Equimolecular mixture of 4 gases 3) Standard LHC gas composition
CO2 @ 300 eV
CO @ 300 eV
Electron Induced desorption increase with coverages and may depend on substrate.
Logarithmic scale!
1 ML

## Slide 27: Conclusions
Specific:
LASE/LESS should be optimized and fully characterized (vacuum, el.desorption etc.)
< 6-8 nm are enough to completely reduce substrate SEY to one of the overlayer.
General:
All new materials should be validated in a global approach.
Material studies in conditions as close as possible to operational ones (preparation, Low Temperature & geometry) is mandatory.
EIC international collaboration:
A diffused community, at INFN (LNF, Rome and Naples) is collaborating since years to develop “state of the art” laboratories and theoretical competence to tackle e-cloud and impedance-related instabilities and is looking forward to define the most efficient involvement in the EIC of mutual interest.

## Slide 28
Tanks to the technical support of DAФNE-L Team:
A. Grilli, M. Pietropaoli, A. Raco, V. Tullio, V. Sciarra and G. Viviani
Thank you for your attention
Thanks to the low temperature team at LNF:
M. Angelucci, A. Liedl, R. Larciprete, A. Novelli e L. Spallino.
Thanks to ARYA supporting project funded by INFN-SNC5

## Slide 29: We thank all the e- cloud community
We planned to reconvene in 2021 but we decided to plan ECLOUD22 from 25 to 29 September 2022 in La Biodola (Elba Island).
We hope to see a numerous participation from the EIC international collaboration.
See:
https://agenda.infn.it/event/13351/