## Slide 1: Superconducting magnet design in Mexico, challenges and opportunities
Daniel Chavez
EIC Workshop – Promoting Collaboration
on the Electron-Ion Collider
Mauro Napsuciale, Giovanni García-Valdivia, Yemby Huamani-Tapia, Arnold Mullisaca and Marco Ortiz
Universidad de Guanajuato, León, Guanajuato, 37150, México.
LABORATORIO DE SUPERCONDUCTIVIDAD
APLICADA

## Slide 2: Outline
Group introduction.
Previous efforts towards the development of 3 and 6 T super-ferric magnets for the JLEIC.
Present projects at the Applied Superconductivity lab of Universidad de Guanajuato, and collaborations with Texas A&M University and Accelerator Technology Corp.
Challenges and opportunities.

## Slide 3
Group introduction

## Slide 4
APPLIED SUPERCONDUCTIVITY LAB
Dr. Daniel Chávez
Dr. Mauro Napsuciale
Yemby Y. Huamani
PhD. Student
Arnold F. Mullisaca
PhD. Student
Giovanni D. Valdivia
PhD. Student
Marco A. Ortiz
PhD. Student
August 2019
Dr. Gustavo Basurto
Neuroscientist
Collaborators
Dr. Alejandro Puga
Dynamical Systems

## Slide 5
Previous efforts towards the development of a 3 and 6 T
super-ferric magnets for the JLEIC, using Cable-in-conduit technology

## Slide 6: Cable-In-Conduits development UG-TAMU
Restrictions on the bend radius and winding capabilities
Current degradation
Some of the problems of previous designs

## Slide 7
Cable-In-Conduit
Technology
Is its own cryogenic-vessel
Features
Full azimuthal contact
between wires.
(Current sharing)
Rigid structure
Allows for precise and complex bends,
in relatively small bend radius (25 mm)
Components
High Strength
Perforated inner tube
High Strength
Outer sheath
Perforations for LHe flow
Superconducting wire
High strength foil
Superconductor is
bathe in LHe, adding
thermal stability
2013-2018
This technology is readily expandable to wind & react superconductors

## Slide 8
How is made?
Cabling
Drawing
High strength foil
foil wrapping
No overlap
Superconductor
Twist-pitch
assessment
In
Out
Core insertion into a
High strength inner tube

## Slide 9: Quality Control
Filament Breakage
FeCl3 solution
Current Degradation
Measurement
Superficial inspection
Compaction
Spacing
Ovalness
Deformations
Chart: Applied Field B (T)
| 6 | 7 | 8 | 9 | 10 | 10.5
Witness_S1 | 901.23 | 651.58 | 416.98 | 212.53
Witness_S2 | 907.78 | 656 | 422.36 | 212.72
Bent_S1 | 895.5 | 654.2 | 418.66 | 209.59 | 56.68 | 14.37
Bent_S2 | 893.41 | 647.22 | 414.13 | 209.89 | 55.11 | 13.87
Bent_S3 | 891.62 | 650.87 | 419.88 | 211.6 | 55.59 | 14.06
Bent_S4 | 898.67 | 658.77 | 423.06 | 211.53 | 56.19 | 13.71
7400 Fil, 9 μm
1.5 Cu:Sc
1.2 mm OD
14 kA CABLE
7600 filaments

## Slide 10: Short sample development
1.745” (44.45 mm) bend radius
(Nb3Sn, MgB2)
1” (25.4 mm)
Bend radius
(Superconductor experienced too much strain!)
No superficial deformation were found at any level: outer tube, superconducting wire,
Or inner tube.
Outer tube tared at various locations
Superconducting wires tare or bottle-necked
No damage to the CIC components
Mechanical behavior (Bends)
QC of samples (Etching, Current degradation)
Wire integrity
Outer sheath
Inner tube
Wind & React
superconductors

## Slide 11: Standard Procedure (quality control) to assess performance of weld line
HLC
As
received
Pressurize at
600 Psi
for 10 min
Thermal shock
from
300 k to 77 k
Bend the samples 180° with weld line facing different directions
<1.0x10-12 atm*cc/s
3x10-3 Torr
Weld line on Nb3Sn CIC

## Slide 12: Complex Winding
3T Superferric CIC dipole
for the Ion Ring of the JLEIC
140 m of NbTi Seamless CIC

## Slide 13
Magnet Lab Team
Texas A&M / ATC Team
We devoted 5 Years of our live towards the development
of a scale prototye for a 3 T superferric dipole
32 kA superconducting cable
Dr. Peter McIntyre
Dr. Akhdiyor Sattarov
Tim Elliot
Ray Blackburn
Joshua N. Kellams
James Gerity
Jeffrey Breitschopf
Karie O’Queen

## Slide 14
Present projects at the Applied Superconductivity lab of Universidad de Guanajuato, and collaborations with Texas A&M University and Accelerator Technology Corp.

## Slide 15
7 T solenoid for material science applications
Superconducting Electron Cyclotron Resonance Ion-Source
5 T Bi2212 CIC research dipole
Magnetic stimulation for Alzheimer deseas
Magentic field for agricultural research (Beans, corn, soy, jalapeño)
Research topics
Yemby Y. Huamani
PhD. Student
7 T solenoid for material science applications
(Patent pending)

## Slide 16
5 T Bi2212 CIC research dipole
Magnetic stimulation for Alzheimer deseas
(Patent pending)
Giovanni D. Valdivia
PhD. Student
More tan 1.8 million diferent configurations for magnetic fields
Arnold F. Mullisaca
PhD. Student

## Slide 17
Marco A. Ortiz
PhD. Student
Dr. Gustavo Basurto
Neuroscientist
Superconducting Electron Cyclotron Resonance Ion-Source
Magnetic stimulation for Alzheimer deseas
(Patent pending)

## Slide 18
Challenges and opportunities

## Slide 19
Challenges
Opportunities
Applied superconductivity is a relatively new area in Mexico, and skepticism is inherited in innovation.
Specialized equipment.
Research Funds.
We are training specialized students in magnet desing and modeling, and production of new technology.
A lot of human resources eager to learn
It’s a new a research topic to Mexico.
Moving towards technology independence.

## Slide 20
Thank you!