## Slide 1: Overview of the thin film SRF programme at Daresbury Laboratory
Daniel Seal
Lancaster University/Cockcroft Institute

## Slide 2: Bulk Nb SRF
Q0
Eacc
Nb : Limits @ 2 K, 1.3 GHz :
Eacc ~ 55 MV/m (± 5 MV/m)
(Geometry : H/Eacc ~ 42 Oe/(MV/m))
Rs = RBCS + Rrés.
High field dissipations
Quench
E Field
B Field
Epeak
Bpeak
0
Max field
Courtesy of C. Antoine (CEA)
Bulk Nb
  Highest Tc and Hc1 of any element
  Large Q0 (1010- 1011)
  CW operation
Some figures of merit
  Eacc  Epeak  Bpeak - limitation = magnetic transition
  Q0  1/RS - limitation = thermal transition
  Duty cycle (=> 100%) - limitation = cryogenic power
However, bulk Nb cavities are close to reaching theoretical limits in Eacc!

## Slide 3: From bulk Nb cavities to thin film cavities
Superconducting films coated on copper:
  Lower production costs!
  Copper substrate  higher thermal conductivity than Nb
  Keeps the SRF properties of the film with the thermal properties of the bulk
Main goals for thin film SRF:
  Improve accelerator performance - higher Q0 and Eacc
  Explore various high Tc materials (Nb3Sn, V3Si, NbN, NbTiN, MgB2, and multilayer structures)
  Reduce cost:
    Copper vs bulk Nb
    Lower cryogenic power consumption (increased Carnot efficiency at higher T)
    Shorter accelerator structures – total cost reduction

## Slide 4: Superconducting thin film development
Thin film deposition
PVD: DC, pulsed, HIPIMS…
Film characterisation
SEM, FIB, AFM,
XPS, XRD, RBS, TEM…
Superconducting RF properties evaluation
Superconducting properties measurement
DC magnetic susceptibility,
QPR at CERN
QPR at HZB
Choke cavity at DL
Nb, NbN, Nb3Sn, MgB2, etc.
Surface preparation
Cleaning, etching,
Polishing, passivating
Field penetration
RRR, Hc, Hfp, Hsh, Tc
Laser treatment of Nb film
Film deposition
SEM image of a NbN thin film
DC magnetisation
QPR
Choke cavity
Mainly planar samples for easier analysis
Key aim: Is there a correlation?

## Slide 5: How is the substrate surface prepared?
At Daresbury Laboratory
Mechanical polishing
Elsewhere
Fine mechanical polishing
  tumbling
  diamond turning
  Metallographic
Chemical polishing:
  SUBU5 solution
  Electropolishing (EP)
Laser polishing for pre- and post-treatment (new technology!)
Combination of different techniques
Surface preparation
Superconducting properties measurement
Superconducting RF properties evaluation
Thin film deposition
Film characterisation
Metallographic polishing at IJCLab courtesy of O. Hryhorenko
SUBU5 polishing at INFN courtesy of E.Chyhyrynets, C. Pira
Would like to develop these at DL

## Slide 6: How is a thin film developed?
Techniques:
  Physical Vapour Deposition (PVD) - DC, pulsed, High-power impulse magnetron (HIPIMS)…
  Chemical Vapour Deposition (CVD)
  Plasma-enhanced CVD (PECVD), plasma-enhanced Atomic Layer Deposition (PEALD) – under development
  Combined: PCVD
Materials:
  Nb
  NbN, Nb3Sn, NbTiN, V3Sn, MgB2, etc.
  Multilayer structures
Deposition facilities at DL
  For planar samples
  For Quadrupole Resonator (QPR) samples
  For cavities
Surface preparation
Superconducting properties measurement
Superconducting RF properties evaluation
Thin film deposition
Film characterisation
A planar sample during the Nb deposition
A QPR sample during Nb TF deposition
Courtesy of R. Valizadeh (STFC)
Cavity prototype deposition

## Slide 7
Physical Vapour Deposition (PVD)
Surface preparation
Superconducting properties measurement
Superconducting RF properties evaluation
Thin film deposition
Film characterisation
Chemical Vapour Deposition (CVD)
Hybrid Physical Chemical Vapour Deposition (HPCVD)
VISTA Laboratory

## Slide 8: How are films characterised?
Films are sensitive to defects
A wide range of techniques:
  Scanning Electron microscope (SEM)
  Focused Ion Beam (FIB)
  Atomic Force Microscope (AFM)
  X-ray Photoelectron Spectroscopy (XPS)
  X-ray Diffraction (XRD)
  Rutherford Backscattering Spectrometry (RBS)
  Transmission Electron Microscopy (TEM)
  Energy-Dispersive X-Ray Spectroscopy (EDX)
FEI inspect S50 SEM
Courtesy of R. Valizadeh (STFC)
Surface preparation
Superconducting properties measurement
Superconducting RF properties evaluation
Thin film deposition
Film characterisation
X-section SEM of Nb3Sn with a Nb underlayer as double structure on Cu

## Slide 9: Magnetic field Penetration
Similar to cavity conditions:
  DC magnetic field parallel to surface
  Field only from one side of sample
Field local to the sample surface:
  Avoid edge effect
  Allow possibility of sample scanning
  Applied and penetrated fields measured by Hall probe sensors
Facility is easy to operate:
  Tmin = 2.5 K, Bmax ~ 612 mT
  LHe free system
  Data acquisition fully automated
  Field of full flux penetration, Bfp vs T
Courtesy of D. Turner (DL/Lancaster)
Surface preparation
Superconducting properties measurement
Superconducting RF properties evaluation
Thin film deposition
Film characterisation
See D. Turner et al. 2022. A facility for the characterisation of planar multilayer structures with preliminary niobium results. Superconductor Science and Technology.
Nb on Cu samples with different substrate treatments

## Slide 10: RRR and Tc
Residual-resistance ratio is essentially a measure of material purity,
Check if material is superconducting and measure Tc
Variable temperature inserts:
  LHe-free cryostat
  Individual vacuum tubes filled with He gas
  Multiple sample tests/day
Surface preparation
Superconducting properties measurement
Superconducting RF properties evaluation
Thin film deposition
Film characterisation

## Slide 11: RF Evaluation
No physical welding between cavity and sample required!
Direct measurements of sample Rs
Surface preparation
Superconducting properties measurement
Superconducting RF properties evaluation
Thin film deposition
Film characterisation
Bulk Nb 3 Choke Cavity
An RF choke is designed to reflect the cavity’s fundamental mode frequency back into the cavity

## Slide 12
Low power measurements of Rs(T,B), of flat samples 90 – 110 mm diameter
Parameters:
  Frequency = 7.8 GHz
  Sample temperatures, T𝑆 > 4 K
  B-fields ≤ 0.8 mT
  RF power ≤ 1 W
Surface preparation
Superconducting properties measurement
Superconducting RF properties evaluation
Thin film deposition
Film characterisation
Simple to operate and change sample (1 PhD student!)
Simple sample design (low cost)
LHe-free system
~ 2-3 sample tests per week (fast turnaround)
Commissioning with bulk Nb (no treatment yet!) and Nb on Cu samples
  More details in poster

## Slide 13: What next?
Thin film deposition
Film characterisation
Superconducting RF properties evaluation
Superconducting properties measurement
Surface preparation
Real cavity measurement
Ultimate Goal: produce a 1.3 GHz thin film coated cavity
1.3 GHz cavity
6 GHz split-cavity

## Slide 14: Conclusions
Significant progress since the programme started in 2014
An ongoing systematic study of correlation between deposition parameters and superconducting properties:
  Small sample depositions, characterisation and testing
  Mastering Nb deposition
  Development in non-Nb films, e.g. Nb3Sn, NbTiN, Mg2B, …
  Depositing multilayer structures, e.g. Cu-Nb-AlN-Nb3Sn
Ultimate goal: beyond Nb coated cavity:
  6 GHz split cavity tests
  Develop a 1.3 GHz deposition and RF testing facility

## Slide 15: Acknowledgements
STFC/CI: O. B. Malyshev, R. Valizadeh, P. Goudket, S. Hitchen, L. Smith, J. Conlon, K. Dumbell, N. Pattalwar, S. Pattalwar, A. May, F. Lockwood-Estrin, A. Hannah, A. Vick, E. Marshall, S. Bibby-Trevor, R. McAllister
Lancaster University/CI: G. Burt, T. Sian, D. Turner, H. Marks
INFN: C. Pira, E. Chyhyrynets
IJCLAB: O. Hryhorenko
CEA: C. Antoine
This work has been supported by: the IFAST collaboration which has received funding from the European Union’s Horizon 2020 Research and Innovation programme under Grant Agreement No 101004730.

## Slide 16: Thank you for listening
Daniel Seal
daniel.seal@cockcroft.ac.uk