## Slide 1: Ion-beam implantation to simulate radiation damage in novel metallic systems for nuclear fusion applications
S. F. Yeates1, A. Gandy2, C. Hofer3, R. Goodall1
1 - The University of Sheffield
2 - UKAEA
3 - The University of Oxford
Particle Accelerator and Beams Conference 2024

## Slide 2
Contents
Challenges for fusion materials
Compositionally complex alloy design approach
Alloy characterisation
Implantation
Post-Implantation characterisation
Conclusions

## Slide 3
Fusion Plasma Facing Components
From - Energy Institute - Statistical Review of World Energy
Deuterium-Tritium – From – Pegasus-III
Operating Conditions
  High 14.1 MeV neutrons
    Ballistic damage
    Transmutation products
  High temperatures
  Thermal cycling & fatigue
  Plasma erosion
  Tritium absorption
Joint European Tokamak– From - UKAEA
Material Shopping List
  High melting temperature
  Phase stability
  Irradiation damage resistance
  Minimal production of long-lived radioactive waste

## Slide 4
Compositionally Complex Alloy Design Approach

## Slide 5
CCAs for Fusion
From - ”Waste implications from minor impurities in European DEMO materials”, Gilbert et al, 2019

## Slide 6
CCA Compositions
Ta30V30Ti30W5Fe5
Ta30V30Ti30W5Cr5
Ta30V30Ti30Fe5Cr5

## Slide 7
Homogenised Alloy Characterisation
Ti
Ti
Ti
Ta30V30Ti30W5Fe5
Ta30V30Ti30W5Cr5
Ta30V30Ti30Fe5Cr5

## Slide 8
Aged Alloy Characterisation
V
V
Ti
V
Ti
V
V
Ti
Ta30V30Ti30W5Fe5
Ta30V30Ti30W5Cr5
Ta30V30Ti30Fe5Cr5

## Slide 9
Aged Alloy Characterisation
C15 Laves
BCC A2
Ti-CON
FIB Lamellar of Ta30V30Ti30W5Fe5
Ta30V30Ti30W5Fe5
Ta30V30Ti30W5Cr5

## Slide 10
Alloy Characterisation
Ta30V30Ti30W5Fe5 XRD Data
Ta30V30Ti30W5Cr5 XRD Data
C15 Laves
BCC
C15 Laves
BCC

## Slide 11
Ti Ion Implantation
Element | Displacement Energy /eV (ASTM E521 2016)
Ta | 90
V | 40
Ti | 30
W | 90
Fe | 40
Ta30V30Ti30W5Fe5 | -WFe
Peak Damage/ dpa | 15.25
Mean Projected Range/ nm | 749
From - Helmholtz-Zentrum Dresden-Rossendorf e.V.

## Slide 12
Homogenised Atom Probe Tomography
Dislocation lines
Dislocation
loops
>15 at% Fe
>37 at% V
Implanted Homogenised Ta30V30Ti30W5Fe5 - 660nm below surface
Linescan of dislocation line
Linescan of dislocation loop
Ta
V
Ti
W
Fe
C
N
O
Notes: C4_M21: 660 nm - 19.5 m

## Slide 13
Homogenised Atom Probe Tomography
V cluster
Dislocation lines
Dislocation
loops
>15 at% Fe
>37 at% V
Implanted Homogenised Ta30V30Ti30W5Fe5 - 660nm below surface
>37 at% V
>15 at% Fe
Isosurface of Fe/V cluster
Line scan of of Fe/V cluster
Notes: C4_M21: 660 nm - 19.5 m

## Slide 14
Aged Atom Probe Tomography
Dislocation lines
Dislocation loops
Implanted matrix phase of aged Ta30V30Ti30W5Fe5 - 300 nm below surface
>33 at% Fe+V
>17 at% Fe
>52 at% V
>33 at% V+Fe
C15 Laves – 650 nm
Matrix – 300 nm
Implanted aged Ta30V30Ti30W5Fe5
 | Matrix |  |  | C15 Laves |  | 
 | Bulk | Cluster | Increase | Bulk | Cluster | Increase
V | 19 at% | 49 at% | 105 % | 47 at% | 60 at% | 33 %
Fe | 2 at% | 5 at% | 150 % | 12 at% | 18 at% | 50 %

## Slide 15
Multi-phase Boundaries
70 at% Ti+C+N+O
27 at% V
20 at% Fe
TiCON | 
Ti | 67.6 at%
N | 18.3 at%
C | 8.6 at%
O | 3.6 at%
Matrix | Concentration
Ta | 28.5 at%
V | 18.8 at%
Ti | 43.3 at%
W | 7.5 at%
Fe | 0.7 at%
C15 Laves Phase | 
Ta | 27.3 at%
V | 44.6 at%
Ti | 14.4 at%
W | 4.0 at%
Fe | 9.2 at%
Implanted aged Ta30V30Ti30W5Fe5 - 210 nm below surface

## Slide 16
Phase Structure Changes
GI-XRD Implanted Homogenised Ta30V30Ti30W5Fe5
GI-XRD Implanted Aged Ta30V30Ti30W5Fe5
BCC
C15 Laves
BCC

## Slide 17
Conclusions
Ion implantation used to produce ballistic damage in Ta30V30Ti30W5Fe5
Ballistic damage drives elemental segregation
Dislocation species demonstrate different segregation behaviors
Bulk phase stability suggested up to 15.3 dpa
Homogenised
Aged

## Slide 18
Acknowledgements
Any Questions?

## Slide 19
Alloy Characterisation
Ta30V30Ti30W5Fe5 XRD Data
Ta30V30Ti30W5Cr5 XRD Data
(110)
(211)
(220)
(310)
(211)
(110)
(211)
(220)
(310)
(211)
Notes: Need to add reflection markers to indicate phases and plane families

## Slide 20
Ti Ion Implantation
Element | Displacement Energy /eV (Ref)
Ta | 90
V | 40
Ti | 30
W | 90
Cr | 28
 | -WCr
Peak Damage/ dpa | 15.3
Mean Projected Range/ nm | 746
From - Helmholtz-Zentrum Dresden-Rossendorf e.V.

## Slide 21
Multi-phase Boundaries
Ta
V
Ti
W
Fe
C
N
O
Ti3(N,C,O)
Matrix
Ti3(N,C,O)
Laves Phase
Matrix
Laves Phase

## Slide 22
Compositionally Complex Alloy Design Approach

## Slide 23
Compositionally Complex Alloy Design Approach

## Slide 24
Compositionally Complex Alloy Design Approach
Notes: We then remove very expensive or non-metallic elements and we end up with…
Rhenium cost - $2000 per kg
Scandium cost – 500000 per kg

## Slide 25
Homogenised Atomic Probe Microscopy
500 nm