## Slide 1: NOMAD - Compact Accelerators for Cultural Heritage
Tessa Charles1,
Adelphine Bonneau2, Pierre Couture3, Jamie Hampson4, Maxim Korostelev5,6, Serge Mathot7, Courtney Nimura8,9, Andy Wolski5,6
1. ANSTO – Australian Synchrotron, 2. Université de Sherbrooke, 3. Surrey Ion Beam Centre, 4. University of Exeter, 5. Cockcroft Institute, 6. University of Liverpool, 7. CERN, 8. University of Oxford, 9. Ashmolean Museum

## Slide 2: Accelerators can be powerful tools, revealing hidden secrets of cultural heritage.
A few examples….

## Slide 3: X-ray Fluorescence (XRF) elemental mapping
D. Thurrowgood et al Scientific Reports | 6:29594 | DOI: 10.1038/srep29594

## Slide 4: X-ray Fluorescence (XRF) elemental mapping to reveal hidden painting
D. Thurrowgood et al Scientific Reports | 6:29594 | DOI: 10.1038/srep29594
Portrait of a Woman
Edgar Degas 1876

## Slide 5: Full spectral XANES imaging revealed the alteration process of chrome yellow pigments in paintings by Vincent van Gogh
L. Monico et al, J. Anal. At. Spectrom., 2015, 30, 613-626, https://doi.org/10.1039/C4JA00419A
The Bedroom (Van Gogh Museum, Amsterdam, The Netherlands)
“…the walls pale lilac, the ﬂoor in a broken and faded red, the chairs and the bed chrome yellow, the pillows and the sheet very pale lemon green, the bedspread blood-red, the dressing-table orange, the washbasin blue, the window green. I had wished to express utter repose with all these very different tones.”
"This time it's just simply my bedroom, but colour is to do everything, and giving by its simplification a grander style to things, is to be suggestive here of rest or of sleep in general. In short, looking at the picture ought to rest the mind, or rather, the imagination"
“This time it’s just simply my bedroom, only here colour is to do everything…” - Van Gogh, in a letter to his brother Theo.
This study used:
the beamline ID21 at ESRF,
the XFM beamline of the Australian Synchrotron, and
the hard X-ray micro/nano-probe beamline at DESY

## Slide 6: Accélérateur Grand Louvre d’analyse élémentaire (AGLAE) at the Louvre
C. Pacheco, Technè, 43 | 2016, 26-31. https://doi.org/10.4000/techne.591
Claire Pacheco, Head of the C2RMF-New AGLAE facility (Paris, France) Image credit: C. Hargoues/C2RMF

## Slide 7: PIXE mapping revealing locations of trace elements
Earthenware depicting a human face, discovered at the ruins of the Miyagi Kamikawana shell mound. Approximately 7,000 years ago.
It is believed that Ancient Japanese people (Jomon) had the custom of painting eyes with red iron oxide.
K. Ishii (2019) “PIXE and Its Applications to Elemental Analysis” Quantum Beam Sci. 2019, 3(2), 12

## Slide 8: Looking at any of these examples…
Benefits:
  Non-invasive ✓
  Non-destructive ✓
  Elemental specificity ✓
  Rapid ✓
  Sensitive ✓
Disadvantage:
  Requires travel to a synchrotron or ion beam accelerator

## Slide 9
The problem:
Museum curators are often hesitant to risk moving valuable artworks. The insurance and security costs of transporting artworks can be prohibitively expensive. Taking samples of the artworks is done sparingly and prohibits the artworks being analysed as a whole.
Often cultural heritage objects and artefacts cannot be taken outside of their country of origin due to legal restrictions, or burdensome bureaucracy.
A solution?
NOMAD directly addresses these issues, with the portable accelerator becoming a self-contained mobile laboratory.
Being able to fit in a container, NOMAD could be taken to countries and regions that don’t have local access to accelerator facilities, allowing local researchers to examine and characterise artefacts.
As a compact, more affordable accelerator, the NOMAD accelerator could be housed in museums and universities.

## Slide 10: We can’t bring the rock to the accelerator. But we might be able to bring the accelerator to the rock.
With so few artworks and artefacts being analysed, what could be discovered if we had greater access to accelerator facilities …
10
With so few artworks and artefacts being analysed, what could be discovered if we had greater access to accelerator facilities …

## Slide 11
NOMAD (Non-destructive Movable Analysis Device) aims towards a conceptual design of a portable 2 MeV proton accelerator for Ion Beam Analysis.
Two technologies being considered.

## Slide 12: Comparison of size
CERN 750 MHz RFQ structure. Credit: Maximilien Brice/CERN
Photo credit: Jean-Pierre Dalbéra.
2 MeV in ~16 m
Conventional Ion Beam Accelerators
CERN’s 750 MHz RFQ structure
Image credit, L. Leay et al "Development of irradiation capabilities to address the challenges of the nuclear industry“, NIM B 343 (2015) 62–69.
ELISA (Experimental Linac for Surface Analysis) on the same scale as figure to left:
Photo credit: Maximilien Brice/CERN
2 MeV in 1 m
Dalton Cumbrian Facility layout
AGLAE (Accélérateur Grand Louvre d'analyse élémentaire)
12

## Slide 13
High-frequency RFQ accelerators could provide a more compact and affordable accelerator, delivering short pulses of protons, ~180 s long.
However a question remains: how does the damage induced by a lower current continuous stream of protons, compare with short pulses with higher peak current?

## Slide 14: Experiment at ELISA (Experimental Linac for Surface Analysis), CERN
2 MeV proton beam
Image credit: CERN
2 MeV proton beam

## Slide 15: Experiment at ELISA (Experimental Linac for Surface Analysis), CERN
SDD detectors
Sample
Exit window
Faraday cup
Top view:
Side view:
Sample:
Samples prepared by Dr Adelphine Bonneau, Université de Sherbrooke

## Slide 16: Experiment at ELISA (Experimental Linac for Surface Analysis), CERN
Samples prepared by Dr Adelphine Bonneau, Université de Sherbrooke.
Paint samples made with:
ochre derived from different ground sedimentary rocks in South Africa (Eastern Cape Drakensberg and Stormberg region) and commercial ochre
water, egg yolk, blood or oil binder
Shown here painted on Kapton. Also painted on paper.
Many thanks to Andy Wolski and Adel Bonneau for sorting out the ethics approval required!

## Slide 17: Analysing colour variation
1. Rotate original image to ensure line is vertical
2. Find keypoints using OpenCV modules
3. Match keypoints, dischard bad keypoints
4. Rotate and shift images to align with each other
5. CIELab evaluation
6. Fit gaussian to signal
Rotate original
1. Rotate original image to ensure reference line is vertical
Find keypoints
2. Find keypoints using OpenCV modules
Match keypoints
3. Match keypoints, discard bad keypoint matches
Rotate and shift
4. Rotate and shift images to align with each other
CIELab evaluation
5. CIELab evaluation

## Slide 18: CIELab is a colour model for quantifying colour variation
L* represents lightness.
a* represents the red–green axis.
b* represents the yellow–blue axis.
ΔE is standardised metric for quantifying the difference between two colours.

## Slide 19
Image cropped to 300 px width around reference line.
CIELab parameters evaluated.
Impact of proton beam

## Slide 20: CIELab parameters from 10 minute exposures at various current values, at ELISA
Sample 16 - South Africa ochre with oil binder
All samples currently being processed

## Slide 21
Add paper results

## Slide 22: Surrey Ion Beam Centre
Parameter | Range available | Experimental parameters
Energy | 100 eV – 12 MeV | 2 MeV
Beam current | fA - mA | 0.2 – 2.0 nA
External beamline, irradiation in air.
Many thanks to Pierre Couture (Surrey) and Maxim Korostelev for conducing this portion of the experiment.

## Slide 23
The next slides are a sneak peek at some preliminary results…

## Slide 24: Preliminary results: Finnish Rock art analysed on XFM beamline at the Australian Synchrotron
Slide from: Uine Kailamäki & Antti Lahelma, University of Helsinki , ‘CONTROLLING CHRONOLOGY’ talk, 2019
Samples taken with permission by: Uine Kailamäki & Antti Lahelma, University of Helsinki

## Slide 25: Preliminary results: Finnish Rock art analysed on XFM beamline at the Australian Synchrotron
Many thanks to the XFM beamline scientists Daryl Howard and Andrew Langenham

## Slide 26
Fe concentration
Fe, Rb, K as RBG
Vari 1

## Slide 27
Vari 3 (long)
Fe concentration
Fe, Rb, K as RBG

## Slide 28
Fe concentration
Fe, Rb, K as RBG
Vari 3
Notes: Silica, paint, silica, paint.

## Slide 29
Syrja
Fe concentration
Fe, Rb, K as RBG

## Slide 30: Conclusion
Work is underway to developing a conceptual design of a compact, portable 2MeV accelerator for Ion Beam Analysis. NOMAD (Non-destructive Movable Analysis Device)
Experiments conducted at CERN and Surrey Ion Beam Centre aim to determine damage thresholds for short pulse compared to continuous beam irradiation.
…

## Slide 31: Backup slides

## Slide 32
Image credit: Taccetti, F., et al. MACHINA, the Movable Accelerator for Cultural Heritage In-situ Non-destructive Analysis: project overview. Rend. Fis. Acc. Lincei 34, 427–445 (2023)
CERN and INFN collaboration, MACHINA (Movable Accelerator for Cultural Heritage In-situ Non-destructive Analysis), has already demonstrated proton acceleration in a compact 750 MHz RFQ.
March 2022 - first extracted 2 MeV beam.
Notes: “A view of the MACHINA system during the tests at CERN. From left: the half rack holding the signal and waveform generators and hosting the module in charge of limiting the power injected into the cavities in case of exceedingly high pressure (higher than 10–5 mbar) in the accelerator; the two racks (blue frames) of the amplifers of the RF PS from which the copper waveguide connects the RF PSs to the cavities; the accelerator assembly (foreground the metal cage of the source and the HV power supplies switched on). In the background: the chillers for the cavities and for the RF PSs”