## Slide 1: Study of surface contamination on ultralow background (ULB) materials
Maria Laura di Vacri
Low Radioactivity Techniques 2019

## Slide 2
Detector components and surrounding materials:
a significant background source
SuperCDMS SNOLAB detector

## Slide 3
Uranium-238
Thorium-232
The usual suspects

## Slide 4
Validation of all materials: a challenging task
For reference:
1 ppt Th = 4.1 mBq 232Th/kg
1 ppt U =12.4 mBq 238U/kg
mBq/kg
range or lower
 Extremely stringent radiopurity requirements
Ultra sensitive analytical techniques
Dedicated facilities
Meticulously clean analytical procedure specifically developed
R&D to develop ultrapure materials (i.e., electroformed copper)

## Slide 5
Surface contamination!
After validation, will materials remain “ultraclean” forever?
Machining
Handling for assembly
Moving and storage
Manufacturing and processing
Exposure to dust, even in clean rooms!

## Slide 6
ICP-MS: a powerful tool
Understanding
Identifying rather than observing (too late!)
Direct, fast, quantitative
Surface and bulk
Quantifying and controlling

## Slide 7
Machining, handling, exposure to dust
Block of HDPE:
1850 g
1600 cm2
2845 ng, or 2.8 mg, of 232Th to account for


22.6 ng
<204 ng
2868 ng
< upper limit

## Slide 8
Flex cable
Polyimide (PI)/Cu laminate
Finished cable
 | 232Th | 238U
 | ppt | ppt
PI/Cu laminate | 8.06 ± 6.30 | 8.72 ± 3.43
Finished cable (whole sample analysis) | 62.8 ±5.2 | 6164 ± 112
Manufacturing and processing
 | 232Th | 238U
 | ppt | ppt
From leach 1 | 40.4 ± 3.0 | 7071 ± 1065
From leach 2 | 2.29 ± 0.13 | 40.2 ± 12.9
From leach 3 | 1.34 ± 0.58 | 16.5 ± 5.8
Leachate analysis, normalized to sample mass
 | 232Th | 238U
 | ppt | ppt
Leached sample | 35.4 ± 2.9 | 55.1 ± 16.6
2% HNO3 solution, 30 sec

## Slide 9
PFA (Perfluoroalkoxy alkane)
Surface exposure
Surface leaching
Quantitative analysis
Silicon
Exposure to dust: direct measurement of dust activity

## Slide 10
Class 10000 clean room at PNNL, 29 day exposure
For reference
1 fg = 10-15 g
[fg day-1 cm2]
Measured accumulation rate on PFA and Si surfaces

## Slide 11
Source: https://pubs.usgs.gov/of/2005/1413/maps.htm
PNNL
K ~ 1.4 E+4 ppm
Th ~ 7.2 ppm
U ~ 1.2 ppm
K ~ 99.94 %
Th ~ 0.051%
U ~ 0.009%
Notes: US Geological Survey.

## Slide 12
K, Th and U relative content in dust (%)
Notes: In this plot I have reported a comparison between the measured content of K Th and U in the dust of a 10000 Class clean room (PFA and Si) and the content in the soil of that geographic area reported by the USGS.

## Slide 13
Room air – Class 10000 clean room comparison
PFA surface, 30 day exposure
Accumulation rate scaling of 100X, as expected
Exposure in a Class 10 area (30 days) : instrumental background level
Notes: I have also compared data obtained from PFA surface exposure in a 10000 Class clean room.

## Slide 14
Summary
2.8 mg of 232Th ( ~1g dust???) on HDPE block surface
  Removed with specific cleaning procedure
  ICP-MS  material assay at ppt levels, not an upper limit
~6 ng g-1 of 238U measured in a flex cable
  Leaching + ICP-MS:
    Identification: 238U localized on the surface
    Reduction: 1st 30 sec mild leaching pulled out all 238U surface contamination
ICP-MS: first direct measurement of dust activity
  Relative contribution from K, Th and U
  Deposition rate

## Slide 15
In conclusion
Surface contamination: a potentially limiting source of background
How can we support ULB detectors?
ICP-MS: a very powerful technique
  Rapid, direct identification and quantitation
  Developing procedures to control and reduce:
    Cleaning
    Working with manufacturer
Dust activity measurement
  Contribution to contamination from exposure to dust (even in clean rooms!)
  Study of contribution in significant locations
    Valuable for planning assembly and installation of detectors
    Collaboration with underground labs, work in progress for a publication

## Slide 16
DOE Detector R&D for High Energy Physics (KA-25)
Sonia Alcantar
Khadouja Harouaka
Notes: More funding source to thank?

## Slide 17
BACK UP SLIDES

## Slide 18
Si wafer
Surface ~ 700 cm2
Thickness 0.77 mm
Density 2.33 g cm-3
https://www.svmi.com/silicon-wafers/300mm-wafers/
1 year exposure in a Class 10000 clean room