## Slide 1
X
Jornada de Transferencia de Conocimiento y Tecnología para la Creación de Nuevas Actividades
Programa FTEC 2016
Málaga 15 de Febrero de 2018
Alejandra Pérez Rodríguez
Technology department– Vacuum group- Surfaces, coatings and chemistry section
Optimisation of the current process.
Performance of fluid dynamic and electrochemical simulations.
Definition and optimisation of the tools used in the surface treatments.
Project coordination.
Definition of the hydraulic circuit and dimensioning of the main equipment.
Creation of Technical specifications for the control system and facility assembly.
Generation of the documentation related to machine safety ( risk analysis, measures to put in place, etc.)
Identification of a correlation between the etching rate and a fluid dynamic parameter:
Design of an installation of electrochemical polishing
R&D OF SURFACE FINISHING IN SUPERCONDUCTING RF CAVITIES
Cavity processing with the best technological process available (Electropolishing) to fulfil particle acceleration requirements.
Supply data for the Future Circullar Collider (FCC) study.
Complete facility definition and equipment purchasing.
Coordination of the facility assembly at CERN.
Work performed
Characterisation of the surface treatment used in the processing of HIE-ISOLDE cavities
Results achieved
Chart: Tasa erosión material [µm/min]
| 2.2329000000000001E-4 | 3.7492999999999999E-4 | 6.6925999999999997E-4 | 1.7003999999999999E-4 | 3.9121000000000002E-4 | 4.5274999999999997E-4 | 2.4096000000000001E-5 | 5.2547999999999999E-5 | 8.2550000000000001E-5 | 2.6811999999999999E-3 | 3.1267000000000001E-3 | 2.6243E-3 | 3.1459999999999999E-3 | 2.833E-3 | 3.3354000000000001E-3 | 3.2073000000000002E-3 | 8.2550000000000001E-5 | 1.5461000000000001E-4 | 3.6772999999999998E-4 | 6.1032999999999997E-4 | 1.0897999999999999E-3 | 2.7902E-4 | 6.4172000000000003E-4 | 7.3382000000000005E-4 | 4.0281999999999998E-5 | 8.5836999999999998E-5 | 1.3531E-4 | 4.4641999999999998E-3 | 5.2475999999999998E-3 | 4.3990000000000001E-3 | 5.3842999999999999E-3 | 4.7733000000000003E-3 | 5.6778000000000002E-3 | 1.7894E-3 | 5.4860999999999998E-3 | 1.3531E-4 | 2.5501000000000001E-4 | 5.0712000000000001E-4 | 8.3389E-4 | 1.4858E-3 | 3.8315000000000002E-4 | 8.8144999999999999E-4 | 1.005E-3 | 5.5822000000000002E-5 | 1.1767E-4 | 1.8532999999999999E-4 | 6.4168000000000003E-3 | 7.5281000000000002E-3 | 6.3159000000000002E-3 | 7.7302999999999998E-3 | 6.8167999999999996E-3 | 8.1530000000000005E-3 | 7.8826999999999994E-3 | 1.8532999999999999E-4 | 3.5100000000000002E-4
6 m3/h | 0.44 | 0.40261 | 0.73995 | 0.41624 | 0.65555 | 0.6939 | 0.27518 | 0.29426 | 0.26505 | 2.4377 | 2.277 | 2.615 | 2.651 | 2.7822 | 2.788 | 2.845 | 0.30997 | 0.31556 | 0.42429 | 0.51531 | 0.93468 | 0.45649 | 0.718 | 0.95555 | 0.31934 | 0.30906 | 0.26443 | 2.5235 | 2.5916 | 2.4951 | 2.5434 | 2.6909 | 2.5916 | 2.079 | 2.5439 | 0.31574 | 0.3408 | 0.73512 | 0.63424 | 1.3099 | 0.52637 | 0.90425 | 1.0896 | 0.40993 | 0.43971 | 0.40511 | 3.3686 | 3.4579 | 3.5764 | 4.0863 | 3.4545 | 3.2273 | 3.7686 | 0.48949 | 0.44109
Process optimisation
Foresee the quantity of material removed
Alejandra Pérez Rodríguez
alejandra90pr@gmail.com
Energía cinética de turbulencia [m2/s2 ]
Optimisation of the tool geometry used in the chemical polishing and definition of the working conditions.

## Slide 2
Jornada de Transferencia de Conocimiento y Tecnología para la Creación de Nuevas Actividades
Programa FTEC 2016
Málaga 15 de Febrero de 2018
PROFESIONAL MOTIVATION
Work experience
2011-2014 MSc Industrial Engineering, specialized in power and fluids engineering (University of Oviedo)
2008-2011 BSc Industrial Chemistry Engineering Intensified on Environmental Technology (University of Oviedo)
Jun. 2016- Present Industrial Engineer at CERNT. FTEC program, Geneva (Switzerland)
Sept. 2015- May. 2016 R&D Engineer in the department of patterned glass products development, Saint-Gobain, Avilés (Asturias)
Nov. 2014-Ago. 2015 Engineer in the department of Energy Saving and Efficiency in the Industry (Institute for the Diversification and Saving of Energy), Madrid
Education
Languages
Mother tongue
Level C1
Level B2
Level A2
Computing skills
• Microsoft Office
• COMSOL Multiphysics
• SolidWorks
• AutoCAD
• Visio
• SketchUp
• Matlab
R&D
Alejandra Pérez Rodríguez
alejandra90pr@gmail.com
Process optimisation
International character
Team work
Goals achievement
Industrial field
Profesional developement
New challenges