## Slide 1: Mechanical Engineering for beam intercepting devices (target, collimators and dumps)
(FTEC2019-17)
Álvaro Romero Francia
STI (Sources, Targets and Interactions)
TCD (Targets Collimators Dumps)

## Slide 2: Overview
Alvaro Romero Francia, EN-STI-TCD
Date: 10/12/2020
The HL-LHC (High Luminosity Large Hadron Collider) and LIU (LHC Injector Upgrade) era are presenting unprecedent challenges. This includes the upgrade of the Target Internal Dump Vertical Graphite (TIDVG) located in the SPS.
TIDVG#4
TIDVG#5
Average Beam Thermal Power 60kW
Average Beam Thermal Power 235kW
LSS1
LSS5
Move from LSS1 to LSS5
Problem Definition
Fig.1 LSS1 and LSS5 location in SPS

## Slide 3: Index
Cooling Pipes CFD/Thermal Coupling
Cooling Pipes Thermal/Structural Coupling
CFD Cooling Air around the Vacuum Chamber
Interlocks and Alarms
Cooling TIDVG#5 after Interlock
Number of Particles/Time
TZM Fatigue Test Campaign
Cooling TIDVG#5
Interlock
Fatigue
Alvaro Romero Francia, EN-STI-TCD
Date: 10/12/2020

## Slide 4
Cooling Pipes CFD/Thermal Coupling
Cooling Pipes Thermal/Structural Coupling
CFD Cooling Air around the Vacuum Chamber
Work Completed
Alvaro Romero Francia, EN-STI-TCD
Date: 10/12/2020

## Slide 5: Overview
Problem Definition, Previous Work and Current Work
Beam Direction
Beam Direction
Vacuum Chamber
Absorbing Blocks
CuCr1Zr core
Air Extraction
Cooling Pipes
Particle Beam
Particle Beam
Simulations Completed:
CFD-Thermal Simulations Coupled for the cooling pipes.
Thermal-Structural Simulations Coupling for the cooling pipes.
Full CFD analysis for the Vacuum Chamber new design.
Von Mises Stress- [Pa]
Temperature [K]
Velocity [m/s]
Fig.2 LSS1 a) CuCr1Zr Core. B) Vacuum Chamber
Fig.3 a) CFD-Thermal Coupling b) Thermal-Structural Coupling. c) Cooling air behavior around Vacuum Chamber
Alvaro Romero Francia, EN-STI-TCD
Date: 10/12/2020

## Slide 6
Interlocks and Alarms
Cooling TIDVG#5
Number of Particles/Time
Work Completed
Alvaro Romero Francia, EN-STI-TCD
Date: 10/12/2020

## Slide 7: Interlocks and Alarms
CFD and FEA simulations
Interlocks
CuCr1Zr water flow < 10
( Possible problem with the water cooling)
Chamber Air flow < 500
( Possible problem with the air cooling)
More than 5 consecutive full SPS-FT SHiP super-cycles dumps after LHC filling steady state
(To be confirmed and defined in terms of particles/unit of time)
New: due to constrained displacements
Alvaro Romero Francia, EN-STI-TCD
Date: 10/12/2020

## Slide 8: FEA Transient Thermal
7.2 s - SPS-FT SHiP pulse period
3.6 s - MD
21.6 s - LIU-SPS 80b pulse period
3.6 s - MD
BP=1.2s
LHC Filling SuperCycle
Repeated until Steady State
44.12 K
Max.Difference
1st Pulse
2nd Pulse
3rd Pulse
4th Pulse
5th Pulse
54
50
40
30
20
10
0
351
360
370
380
390
395
(s)
5 FT-SHiP Pulses
(C)
Fig.4 Temperature increase after LHC Filling Steady State and 5 FT-SHiP Pulses
Alvaro Romero Francia, EN-STI-TCD
Date: 10/12/2020

## Slide 9: FEA Transient Structural
Stresses seem acceptable in the CuCr1Zr core and Vacuum Chamber for the normal operational scenario structural dynamic response. Both remain in the elastic domain.
Fig.5 Vacuum Chamber FEA Transient Structural after LHC Filling + 5 SHiP Pulses
Fig.6 Vacuum Chamber FEA Transient Structural after LHC Filling + 5 SHiP Pulses
Alvaro Romero Francia, EN-STI-TCD
Date: 10/12/2020

## Slide 10
Number of Particles / Unit time
The Number of Particles / Unit time indicates a limiting value for operators controlling the TIDVG#5. If this value is reached or exceeded, it is a signal that the machine shall stop and the causes investigated.
The goal is to avoid dumping more than 5 Full SHiP pulses after reaching steady state with LHC filling super-cycle.
Buffer Time – 54 Seconds
Interlock Activated if… 3.1868e12 p+/s
Alvaro Romero Francia, EN-STI-TCD
Date: 10/12/2020

## Slide 11: Cool Down Phase Max.Temperature
Baseline Cooling Time 20 minutes
Waiting Time for Continuous Operation 5 minutes
Alvaro Romero Francia, EN-STI-TCD
Date: 22/09/2020
Fig.7 TIDVG#5 Cooling after LHC Filling + 5 SHiP Pulses
Alvaro Romero Francia, EN-STI-TCD
Date: 10/12/2020

## Slide 12
TZM Fatigue Test Campaign
Work to be Completed
Alvaro Romero Francia, EN-STI-TCD
Date: 10/12/2020

## Slide 13: TZM Absorbing Block
During Worst-Case Scenario, Christensen failure criterion demonstrated how prompt is the first TZM block to fail. A deeper study is required. This includes a fatigue analysis.
Fig.8 a) TZM temperature after worst-case scenario. b) Christensen Criterion after worst-case scenario.
Alvaro Romero Francia, EN-STI-TCD
Date: 10/12/2020

## Slide 14: Failure Criterion
Non-Constant Amplitude, Non-Proportional Loading
Critical Plane Method
Fatemi Socie Criterion, Crossland Criterion, Sines Criterion, Dan Van Criterion
Plane at 0º X rotation
Plane at 10º X rotation
Plane at 20º X rotation
Plane at 30º X rotation
Plane at 40º X rotation
Plane at 50º X rotation
Fig.9 Critical Planes Shear Stresses
Alvaro Romero Francia, EN-STI-TCD
Date: 10/12/2020

## Slide 15: TZM Fatigue Campaign
APDL command in ANSYS Records stress history during Dump.
Two Python Codes Defines Lifetime based on Criterions.
Torsion Fatigue Properties are required:
Very limited experimental data.
Most of the experimental data cover uniaxial fatigue tests.
Non experimental data relating Uniaxial and Torsion properties for Non-Ferrous alloys.
Problem
Alvaro Romero Francia, EN-STI-TCD
Date: 10/12/2020

## Slide 16: Future Steps
Perform Torsion Fatigue Tests with TZM specimens.
Commissioning TIDVG#5
Torsion fatigue parameters are required to solve the failure criterions.
During Commissioning, temperature in TIDVG#5 will be recorded. Experimental results are to be compared with Numerical results.
Alvaro Romero Francia, EN-STI-TCD
Date: 10/12/2020

## Slide 17
Questions?
Thank you,