## Slide 1
1/15
sonia.garcia.scheifler@cern.ch
07/12/2020
FTEC Workshop December 2020
Mechanical Engineer for the design and constuction of high power
Radio Frequency devices RF

## Slide 2
sonia.garcia.scheifler@cern.ch
07/12/2020
2/15
Drop test background
·· Series Cryomodules ··
The main objectives are to validate:
The non-rupture of ceramic
The absence of plastic deformation
The 25 ohm-design
50Ω
25Ω

·· Frida Eriksson & Sonia García ··

## Slide 3: Ceramic testing
sonia.garcia.scheifler@cern.ch
07/12/2020
3/15
LHCACFHC0246
OLD design
Cracks already appear when we closed the flange
Steps for validation
1st thermal test
Penetrant testing
2nd thermal test
Penetrant testing
·· Thermal test ··
21
23
18
17
Leak test
Leak test
Leak test

## Slide 4: Ceramic testing
sonia.garcia.scheifler@cern.ch
07/12/2020
4/15
LHCACFHC0292
We finished the tests, now we wait for the vacuum official validation.
No cracks!
Final assembly for ceramic testing
We added the purple piece
When we mount the ceramic in the vacuum chamber and we tight the screws we don’t break the ceramic
FINAL design

## Slide 5: Ceramic testing
sonia.garcia.scheifler@cern.ch
07/12/2020
5/15
Departement / groupe | EN/MME |  | BE/RF |  | EN/MME |  | BE/RF | EN/CV | BE/RF |  | 
contact | Simon | Fritz | Seb | Seb | Simon | Thomas | Seb | 40/30 | Seb | Seb | 
N ceramique |  |  |  |  |  |  |  |  |  |  | 
34 |  |  |  |  |  |  |  |  |  |  | support de ceramique collé sur brasage sortie de four
35 |  |  |  |  |  |  |  |  |  |  | les 3 passages ont été posé sur support dans le cryostat du SM18 pour test cryo des ceramiques
36 |  |  |  |  |  |  |  |  |  |  | 
37 |  |  |  |  |  |  |  |  |  |  | 
38 |  |  |  |  |  |  |  |  |  |  | 
39 |  |  |  |  |  |  |  |  |  |  | 
40 |  |  |  |  |  |  |  |  |  |  | 
41 |  |  |  |  |  |  |  |  |  |  | 
42 |  |  |  |  |  |  |  |  |  |  | 
43 |  |  |  |  |  |  |  |  |  |  | 
44 |  |  |  |  |  |  |  |  |  |  | 
45 |  |  |  |  |  |  |  |  |  |  | 
Titanium flange machining
Metrology
Brazing
Visual Control
Assembly test
Leak test
Penetrant testing
Visual inspection
FE weld
Metrology
Leak test official validation
STEPS FOR VALIDATION
Vacuum chamber assembly
Clean room preparation
Cavity mounting



Pending

## Slide 6: Tooling for transport under vacuum
H-HOM
sonia.garcia.scheifler@cern.ch
07/12/2020
6/15
Boxes for transport
Protection pieces
Chassis anti-vibration
V-HOM
H-HOM Feedthrough
Field antenna
V-HOM
H-HOM Feedthrough
Field antenna
V-HOM
H-HOM Feedthrough
Field antenna

## Slide 7: Clean room tooling
sonia.garcia.scheifler@cern.ch
07/12/2020
7/15
Participation in the design and mounting of the tooling for clean room
·· Courtesy of Nicolas Villanti ··

## Slide 8: Crab cavity RFD and DQW coaxial lines
sonia.garcia.scheifler@cern.ch
07/12/2020
8/15
Design of the coaxial lines for DQW and RFD cryomodules:
These lines extract the power from the HOMS
The lines are special because they pass from 2 K to 300 K
Difficult task has been to find a cable suppliers for 25 ohm
They need to be changed because we need to pass from 50 ohm to 25 ohm

## Slide 9: Crab cavity RFD coaxial line
sonia.garcia.scheifler@cern.ch
07/12/2020
9/15
Sent for study

## Slide 10: Coax line pieces for testing
sonia.garcia.scheifler@cern.ch
07/12/2020
10/14
We tested 5 pieces with different type of welding.
TIG Welding: good quality
EBW: deformation, expensive
Laser: deformation
Different surface treatment
(stainless steel copper plated)
TIG
EBW
LASER
TIG


## Slide 11: HL-HLC crab cavity Cryomodule RFD
sonia.garcia.scheifler@cern.ch
07/12/2020
11/15

## Slide 12: HL-HLC crab cavity Cryomodule RFD with coax lines
sonia.garcia.scheifler@cern.ch
07/12/2020
12/15

## Slide 13: Collaboration with BE-RF-SRF in QA/QC
In progress
Assemblies
Material Certificates
Single Parts
sonia.garcia.scheifler@cern.ch
07/12/2020
13/15
Manufacturing Inspection Plan (MIP)
Steps
Fundamental Power Coupler (FPC)

## Slide 14: Collaboration with BE-RF-SRF in QA/QC
1. Production tracking (RI company)
DQW cavity
2. Documentation and contract requirements
3. EDMS & MTF platforms and MIP (Manufacturing Inspection Plan)
sonia.garcia.scheifler@cern.ch
07/12/2020
14/15

## Slide 15
sonia.garcia.scheifler@cern.ch
07/12/2020
15/15
Sonia Garcia
BE/RF/PM
Thanks to all colleagues from the BE-RF-PM team involved with the HOMC and Field Antenna devices, specially to Eric, Seb, Nicolas, Jamie and Frida.
Thanks to Fritz (EN-MME-FW), Nuria (BE-RF-SRF) and Teddy (EN-MME-EDM) for their help and collaboration.
Thank you