## Slide 1: Ultra-high light yield solutions (from IHEP)
Low temperature CsI+SiPM+TPB solution
CsI, LY >100000 photons/MeV, 2.5 times better than CsI(Na)
SiPM, PDE 50%-60%, 2 times better than PMT
Expected ~50-60 p.e./keVee
TPB（WLS）
SiPM
CsI
Low temperature

## Slide 2: Pure CsI crystals
LY be significantly improved at LT
The brightest scintillator, 310-340 nm
QF>100% for alpha/gamma
QF for nuclear recoil/gamma 10%, 20%???
LY of CsI(Na), CsI(Tl) is reduced at LT
New Physics: Sae Mulli,Vol. 71, No. 5, May 2021, pp. 469475
IEEE TRANSACTIONS ON NUCLEAR SCIENCE, VOL. 37, NO. 2, APRIL 1990
RDTM (2018) 2:15

## Slide 3: TPB wavelength shifter
Shift 340nm to 420 nm, match the SiPMs sensitive spectrum
Performance is enhanced at LT
Widely used in liquid argon detectors
R Francini et al 2013 JINST 8 P09006

## Slide 4: SiPMs Performance
PDE 50-60% at 420 nm
DCR reduced by 7 orders, < 0.01 CPS/mm2 at 77K
Optical cross talk, acts as a photon amplifier
AFBR-S4N66P014M NUV-MT Silicon Photomultiplier
Alberto Gola FBK

## Slide 5: Prototype detector
CsI crystal 5x5x5 cm, 0.56kg, polished
Packaging with Teflon reflective film without TPB
SiPMs array, 5x5 cm, two end readout, with TPB
Cooling to 77 K with liquid nitrogen
Low temperature front-end amplifier circuit

## Slide 6: SiPMs array performance
SiPM and preamplifier run stably at low temperatures
Single photoelectron resolution is very good
Consistency of the two arrays is very good
DCR ~0.1 Hz/mm2 @35V bisa
arXiv:2212.11515

## Slide 7: Waveform performance
Decay time ~1 µs, Pulse Width ~3 µs
Baseline width <5 mV

## Slide 8: Energy spectrum
Test with 241Am and 55Fe
Excellent energy resolution,fine structures are clearly visible
arXiv:2212.11515

## Slide 9: Luminescence linearity
Excellent luminescence linearity, no drop down below 10keV
Significantly better than LaBr3, NaI:Tl
Nuclear Science and Techniques (2024) 35:23
arXiv:2212.11515

## Slide 10: Influence of SiPMs Cross Talk and After Pulse
arXiv:2212.11515
CT, AP significantly increasing the measured p.e. number
Internal CT, AP triples the number of p.e. at 37 Vbias
External CT 1.4 times the number of p.e. at 37 Vbias

## Slide 11: Influence of TPB
Photoelectrons number is doubled with TPB
arXiv:2212.11515

## Slide 12: Light yield
arXiv:2212.11515
The measured p.e. number increases significantly with increasing bias voltage, 30 to 122 p.e. /keVee
122.7 p.e./keVee, a world record
30.1 p.e./keVee, after CT subtract (50% PDE at LT?)

## Slide 13: Potentials in the CEvNS detection
35 m distance to a 4.6 GWth reactor
QF=0.06, DCR= 0.1 CPS/mm2, DCR dominant background,
Threshold 2 p.e., good chance for reactor CEvNS observation
If QF ~15%?, DCR~0.01?, better sensitivity
arXiv:2212.11515

## Slide 14: Issue of SiPMs eCT coincidence events
Events rate of eCT coincidence is very high
5 orders larger than accidental coincidence of DCR
Big issue for low threshold detectors
Need do further study, single-ended readout, correlation with iCT
arXiv:2212.11515

## Slide 15: Summary
Ultra-high light yield solution is proposed by IHEP
The prototype detector works well
Good chance for reactor CEvNS detection
eCT issue need further study