## Slide 1
High Order Modes in Superconducting Cavities
HOMSC16, 22 – 23 August, 2016
HOM considerations for Energy Recovery Linacs and other high-current, CW SRF accelerators
Georg Hoffstaetter (Cornell) for the SRF and CBETA team
Cavity design and construction for high BBU current
Beam-pipe HOM absorber design and construction
HOM testing with and without beam
Beam limits from HOM heating
BBU limits for multi-turn ERLs with realistic HOM

## Slide 2: Cornell’s ERL for eRHIC prototyping and beam experiments
6 MeV
6 MeV
Cornell DC gun
100mA, 6MeV SRF injector (ICM)
600kW beam dump
100mA, 6-cavity SRF CW Linac (MLC)
+/- 36 MeV
Electron Current up to 320mA in the linac
Bunch charge Q of up to 2nC
Bunch repetition rate 1.3GHz/N
Beams of 100mA for 1 turn and 40mA for 4 turns
42, 78, 114, 150 MeV
Existing components at Cornell

## Slide 3
1.7 × 1033 cm-2 s-1 for √s = 127 GeV (15.9 GeV e↑on 255 GeV p↑)
× 10 luminosity with modest improvements (coating of RHIC vacuum chamber)
× 100 luminosity with shorter bunch spacing (ultimate capability)
ePHENIX
eSTAR
BeAST
courtesy Thomas Roser
eRHIC Design – need for an ERL

## Slide 4
E=18.3 GeV
E=6.7 GeV
E=5.0 GeV
E=1.7 GeV
QF
BD
eRHIC uses two FFAG beamlines to do multiple recirculations. (FFAG-I: 1.7-5.0 GeV, FFAG-II: 6.7-18.3 GeV, 20 GeV)
All sections of a FFAG beamline is formed using a same FODO cell. Required bending in different sections is arranged by proper selection of the offsets between cell magnets (or, alternatively, with dipole field correctors).
Permanent magnets can be used for the FFAG beamline magnets (no need for power supplies/cables and cooling).
Orbits in Transition section
Each of two eRHIC FFAGs contain 1066 FFAG cells
Orbits in Detector bypass section
Quad offsets evolve adiabatically
@S.Brooks, D.Trbojevic
eRHIC ERL – 12 turns in only 2 NS-FFAG arcs

## Slide 5: CBETA for risk drivers of eRHIC
Some of the most important risk items for eRHIC:
FFAG loops with a factor of 4 in momentum aperture.
  Precision, reproducibility, alignment during magnet and girder production.
  Stability of magnetic fields in a radiation environment.
  Matching and correction of multiple simultaneous orbits.
  Matching and correction of multiple simultaneous optics.
  Path length control for all orbits.
Multi-turn ERL operation with a large number of turns.
  HOM damping.
  BBU limits.
  LLRF control and microphonics.
  ERL startup from low-power beam.

## Slide 6: ERL injector at Cornell
Cavities, couplers,
HOM absorbers
Source
SC injector
Dump
Diagnostics

## Slide 7: The CBETA CDR
Background for CDR
Wrote PDDR for hard X-ray ERL at Cornell in 2012.
Start of CBETA July 2014 White paper December 2014
CDR scheduled for magnet prototypes.
Planed for completion of optics and layout for CDR.
Scheduled this Review to include advise on CDR.
Plan to include committee advise by the end of July.

## Slide 8: Why is CBETA at Cornell
Track Record:
ERL injector with world-record current (10 times more than the next)
ERL injector with world-record emittance (5 times less than the next)
SRF cavity shape for high current (30 times more than the next)
SRF R&D for ERL Light Sources with world-record low energy loss
High Brightness Beam Physics (first full hard x-ray ERL design)
Facilities and Capabilities:
About 120 accelerator-related employees with decades of experience in accelerator building and operation at the worlds forefront.
Facilities and experience for building full SRF accelerators and DC guns.
Space for a 100mA, > 36MeV per turn ERL.

## Slide 9
L0E contained approximately 7,000 square feet of Lab and Shop space
Hall L0E before CBETA

## Slide 10
70% of the existing technical-use space was removed for the initial phase
Spring 2015

## Slide 11
The initial installation was completed for the MLC and ERL beamline
Fall 2015

## Slide 12
The second phase will accommodate the new loop-layout
Spring 2016

## Slide 13
The second phase is almost complete
Summer 2016

## Slide 14
Cavity string and Rad monitor notes
JT-valve
Cavity#1
Cavity#5
Cavity#2
Cavity#3
Cavity#4
Cavity#6
JT-valve
Pre-cool
Prototype Main Linac Cryomodule
MLC
HGRP
2K-2phase
the chimney on 2K2P line to HGRP
six packages of 7-cell cavity/Coupler/tuner
a SC magnets/BPMs package (magnet not installed)
five regular HOMs/two taper HOMs
nominal length: 9.8 m
Beamline HOM absorber
7-cell cavity
SC magnets & BPMs
Intermodule unit

## Slide 15: Main linac cryomodule assembly for CW beams
MLC assembly was completed
Cooled down fall 2015, field, Q, and microphonics tested.
Further cold studies will start August 2016

## Slide 16: High Current Cavity Design Strategy
Central focus: Maximize threshold current through ERL
Optimization over ~100 degrees of freedom
  Center cell geometry
  End cell geometry
  Beam line HOM absorbers
Simulate ERL performance with realistically shaped cavities
Notes: Say what realistic shapes mean

## Slide 17: Accelerating Structure Overview
Center cells
  Geometries are (nominally) identical
  Responsible for general properties of HOM spectrum
    Controls frequencies of HOM passbands and dispersion relations
    Determines cell-to-cell coupling and how sensitive HOM spectrum is to variation in cell shape
Goal: Maximize Ith > 100 mA (under constraints)

## Slide 18
Center cells
  Geometries are (nominally) identical
  Responsible for general properties of HOM spectrum
    Controls frequencies of HOM passbands and dispersion relations
    Determines cell-to-cell coupling and how sensitive HOM spectrum is to variation in cell shape
End cells
  Asymmetric design helps prevent trapped modes
  Responsible for coupling HOMs to HOM absorber
    Directly controls quality factors of HOMs
Goal: Maximize Ith > 100 mA (under constraints)
Accelerating Structure Overview

## Slide 19: Accelerating Structure Overview
Center cells
  Geometries are (nominally) identical
  Responsible for general properties of HOM spectrum
    Controls frequencies of HOM passbands and dispersion relations
    Determines cell-to-cell coupling and how sensitive HOM spectrum is to variation in cell shape
End cells
  Asymmetric design helps prevent trapped modes
  Responsible for coupling HOMs to HOM absorber
    Directly controls quality factors of HOMs
Beam Pipe
  Should be short to improve linac fill factor but long enough to avoid dissipating too much power from the fundamental mode
Goal: Maximize Ith > 100 mA (under constraints)

## Slide 20: Accelerating Structure Overview
Center cells
  Geometries are (nominally) identical
  Responsible for general properties of HOM spectrum
    Controls frequencies of HOM passbands and dispersion relations
    Determines cell-to-cell coupling and how sensitive HOM spectrum is to variation in cell shape
End cells
  Asymmetric design helps prevent trapped modes
  Responsible for coupling HOMs to HOM absorber
    Directly controls quality factors of HOMs
Beam Pipe
  Should be short to improve linac fill factor but long enough to avoid dissipating too much power from the fundamental mode
HOM load
  Absorber material properties determine specific mode losses.
Goal: Maximize Ith > 100 mA (under constraints)

## Slide 21
Center Cell Optimization
Baseline Center Cells
Enhanced cell-to-cell coupling
BBU Parameter
BBU Parameter
o HOM properties with no fabrication variation
x HOM properties with 1/16 mm variation

## Slide 22
Cornell HOM Beamline Absorbers
Cooling Passage Configuration of 80K Cooling Jacket
Absorbing Material:
Doped SiC (SC-35 from Coorstek
The HOMSC workshop series started in 2010 with a call to discuss development of this HOM absorber.

## Slide 23: Horizontal Test Cryostat (HTC) with 1st ERL cavity
cavity
HOM load
HOM load
HGRP
80K shield
Gate valve
Horizontal Test Cryostat:
16MV/m, 1.8K: Q0 = 2.E10 (reached with coupler)
Q0 = 3.5E10 without coupler
Q0 = 6E10 with coupler and HOM absorbers (held the world record)
Much better Q0 than the ERL spec.
Increased state of the art expectations for other projects, e.g. LCLS-II.
Became essential for high-Q cavity research, incl. for N-doped cavities.

## Slide 24
HTC-2: No HOM Absorbers
HTC-3: With HOM Absorbers
Beamline HOM absorbers strongly damp dipole HOMs to under Q ~ 104
5K intercept
40 to 80K intercept
SiC absorber ring
Shielded bellow
Flange for disassembly
Flange to cavity
Ralf Eichhorn | CLASSE | Cornell University ERL Workshop 2015 | Stony Brook| 06/10/15 24
HTC HOM damping

## Slide 25: HOM measurements with beam
BPM
7-cell cavity in cryostat
gun
No charge-up of the HOM absorber observed.
HOM heating was less than expected, limits to 400mA total ERL current.
This establishes the current limit of 40mA for the 4-turn CBETA ERL

## Slide 26: Main linac cryomodule (MLC) achieved accelerating gradients
Chart: cavity#
 | 16.2 | 16.2 | 16.2 | 12 | 7.8 | 14
 | 16.2 | 16.2 | 16.2 | 13.7 | 16.2 | 16
 | 16.2 | 16.2 | 16.2 | 13.7 | 16.2 | 16.2
Quench
Admin.
Admin.
Admin.
Admin.
Limit.
*FE processed out.
FE
5 of 6 cavities had achieved design gradient of 16.2MV/m at 1.8K in MLC.
Cavity#4 is limited by quench so far, no detectable radiation during test.
Enough Voltage for 76MeV per ERL turn (where 36MeV are needed)

## Slide 27: Main linac cryomodule (MLC) achieved surface losses (Q0)
4 of 6 cavities had achieved design Q0 of 2.0E+10 at 1.8K.
Q0 of Cavity#6 had severe FE at 16MV/m.
Enough cooling for 73MV per ERL turn (where 36MeV are needed)
Chart: cavity#
| 1.0 | 2.0 | 3.0 | 4.0 | 5.0 | 6.0
initial cool down | 18800000000 | 14800000000 | 18100000000 | 10000000000 | 15100000000 | 12400000000
1st thermal cycle w/ fast cool | 18390032552.6968 | 13900000000 | 18400000000 | 14000000000 | 20400000000 | 11700000000
 | 21682077081.2831 | 19973515235.523 | 20111830881.2101 | 13004498069.4695 | 17527367813.0144 | 8910000000 | 13400000000
*Q0 at 16.2MV/m with severe FE.
*Q0 after many quench.
*Q0 after FE processed out.
1.8K
*Q0 at 14MV/m, FE started.
Target Qo 2.0e10 at 1.8K

## Slide 28
Current limits from HOMs
Dipole HOMs on MLC were strongly damped below Q~104.
Consistent with HTC and simulation results.
HTC results were:
HOM heating: currents are limited to < 40mA in CBETA
BBU no HOM limits BBU to below 100mA in one turn

## Slide 29: BBU for 1 pass in CBETA
100% of simulations have > 100mA
CBETA 1-pass
Cavity shape error: 125 μm

## Slide 30: BBU for 4 passes in CBETA
100% of simulations have > 100mA
CBETA 4-pass
Cavity shape error: 125 μm
x/y coupling is simulated to increase the threshold significantly
86% of simulations have > 40mA

## Slide 31
CBETA: FFAG-ERL
6 MeV
6 MeV
Cornell DC gun
100mA, 6MeV SRF injector (ICM)
600kW beam dump
100mA, 6-cavity SRF CW Linac (MLC)
+/- 36 MeV
Electron Current up to 320mA in the linac
Bunch charge Q of up to 2nC
Bunch repetition rate 1.3GHz/N
Beams of 100mA for 1 turn and 40mA for 4 turns
42, 78, 114, 150 MeV
Existing components at Cornell

## Slide 32: Summary
Cornell is building a 4-turn Energy Recovery Linac (ERL) with a beam current limited by HOMs through
HOM heating
The Beam-Breakup (BBU) instability
Cornell has already built the Injector Cryomodule (ICM) and the Main Linac Cryomodule (MLC) with beam-pipe HOM absorbers.
The ICM has accelerated 75mA CW without HOM-heating problems.
The cavity arrangement of the MLC with HOM absorbers has been tested with beam.
HOM-absorber heating limits to 320mA in the MLC, or 40mA for a 4-turn ERL beam.
HOM measurements with and without beam indicate the a 1-turn ERL with 100mA should be possible.
BBU calculations: 100mA one-turn ERL is possible, 40mA, 4-turn ERL may be possible
To operate accelerators CW linacs with larger
currents, HOM absorption at room temperature
become advisable. Designs for this should be
developed.

## Slide 33: The END
Questions
Discussion
?