## Slide 1: Radiation Detectors, Imaging What You Cannot See: Silicon and Advanced Techniques
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025
Cinzia Da Vià
The University of Manchester, UK & Stony Brook University USA

## Slide 2: Some Information about myself
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025
Professor at The University of Manchester (UK)
Visiting Professor at the University of Stony Brook, New York, USA
Member of the ATLAS Collaboration at CERN – LHC
Chief editor Frontiers in Physics, Radiation Detectors and Imaging
Co-Chair of the EU-ATTRACT Independent Committee
IEEE WIE International Committee Member 2017-2022
Chair of the IEEE SusTech Innovation, Engagement & Collaboration sub-committee
Distinguished Lecturer of IEEE NPSS Instrumentation Schools
Scientific Interests:
Radiation Detector development : silicon pixels, 3D silicon detectors, fast timing
Radiation effects in silicon, “Lazarus effect”
3D printed detectors, Vertical integrated microsystems
Quantum Imaging at X-Ray energies
Sustainable Technology

## Slide 3: This lecture
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025
Brief reminder: Radiation, Radiation interaction with Matter and Radiation Detectors
Imaging Radiation with Silicon Detectors:
Pixel sensors �➔Monolithic and Hybrid
Basics of Signal formation in silicon sensors
Basics of radiation effects in silicon sensors
Examples of applications in High Energy Physics, medicine, Environmental Monitoring and Energy Harvesting
A brief look at the future
3

## Slide 4: Imaging radiation
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025
Web cams Smart phones photo cameras machine vision, automotive, security etc…
HEP
x-ray crystallography
cosmology
Medical imaging
Quantum Imaging…..

## Slide 5: What is Radiation and its interaction with matter - recap
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025
Ionizing
has enough energy
to knock an electron from
an atom
Radiation can be defined as the propagation of energy through space or matter in the form of electromagnetic waves or energetic particles.
charged
neutral
Non-ionizing does not have enough energy to ionize atoms but generate heat in the material it interacts with.
5
See talk from T. Trojek
2n + 2p = He2+ nucleus

## Slide 6: Particle “signatures” with the Timepix readout electronics
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025
241Am alpha source gives clusters of ~5x5 pixels measured with the MEDIPIX-USB device and a 300 μm thick silicon sensor. The clusters are shown in detail in the inlet. The cluster sizes depend on particle energy and threshold setting.
Signature of X-rays from a 55Fe X-ray source. Photons yield single pixel hits or hits on 2 adjacent pixels due to charge sharing.
A 90Sr beta source produces “tracks” in the silicon detector.
A pixel counter is used just to say “YES” if individual quantum of radiation generates in the pixel a charge above the pre-selected threshold
a
5 keV X-rays
2MeV electrons
See talk from B. Bergmann

## Slide 7: The semiconductor revolution 1947
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025
First transistor invented 1947 by William B. Shockley, John Bardeen and Walter Brattain (Nobel Prize 1956)
First semiconductor particle sensor: Pieter Jacobus Van Heerden, The Crystalcounter: A New Instrument in Nuclear Physics. University Math Naturwiss, Fak (1945).
CCD Nobel prize Boyle Smith 2009
Semiconductor a material that has a conductivity between a conductor and an insulator; electricity can pass through it, but not very easily
The point contact germanium transistor

## Slide 8: SILICON: from sand to wafer
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025
a) The sand is cleaned and further purified by chemical processes. It is then melted. Then a tiny concentration of phosphorus (boron) dopant is added to make n (p) type poly-crystalline ingots
b) Single-crystal silicon is obtained by melting the vertically oriented poly-silicon cylinder
onto a single crystal “seed” --- called “Float Zone-➔ FZ”
c) Wafers of thickness 200- 500μm are cut with diamond encrusted wire or disc saws.
Note: the crystal orientation matters!
<111> and <100> crystals can influence the detector properties eg. capacitance
10
Silicon (silicates) makes up 27.7% of the Earth's crust by mass and is the second most abundant element (oxygen is the first)

## Slide 9: Interaction of radiation with silicon- recap
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025
11
Photons:
-Photoelectric, Compton, pair production
Charged pion in Silicon
Ionizing particles:
Bethe-Bloch equation:
average/mean amount of energy lost due to
ionization per unit of distance in the media)
silicon
Neutrons: Alpha Bragg peak
-Ek = hv -EB
Quantum mechanics in action!!!!
Si bandgap=1.12 eV

## Slide 10: Photons quick recap
12
Eph = hn = hc / l
Photons are the quantum particles carrying “electromagnetic energy”
They have zero mass energy
They travel at the speed of light
Their energy is:
(where h is the Planck’s constant, 6.62×10-34 J·s)
The most important forms of interaction with matter include:
  Absorption
  Refraction
  Transmission/Reflection
  Diffraction
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 11: X-rays absorption efficiency in Si
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025
13
100
90
80
70
60
50
40
30
20
10
0
0 10 20 30 40 50 60 70
Energy (keV)
Efficiency (%)
300um 500um 1000um 1500um

## Slide 12
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025
14
At low energy the most important parameter is the absorption coefficient a, that determines the probability of the photon to be absorbed
a is strongly dependent on the atomic number of the absorbing medium Z
The attenuation of a light beam in the semiconductor is described by the Lambert-Beer’s law:
-ax
I ( x) = I0 × e
Absorption coefficient

## Slide 13: Charged particles
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025
Charged particles continuously interact with electrons and protons in the nucleus via the long-range Coulomb force.
Most interactions are elastic (Rutherford) scattering with atomic electrons.
The basic theory was developed by N. Bohr using classical arguments, and later quantum mechanics was used by Bethe (1930), Bloch (1933) and Landau (1944).
Since the time that the electrostatic force acts on the traveling electron is inversely proportional to its velocity, the energy loss is inversely proportional to the square of the particle velocity.
Minimum Ionizing Particle Energy Loss in Si: 3.87 MeV/cm.
Ionizing Energy for e-h pair creation= 3.62eV
15

## Slide 14: Problem: Getting a Signal from “pure” Silicon
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025
-
16-
n = p = ni
Intrinsic semiconductor:
Pure (undoped) semiconductor the electron density n and hole density p are equal.
For Silicon: ni = 1.45×1010 cm-3
Ef
E
conduction band e
300 µm
1 cm
1 cm
,
Signal generated by an Ionizing particle passing through 300 um intrinsic Silicon
Ionization energy I0 = 3.62 eV ,
mean energy loss for a mip dE/dx = 3.87 MeV/cm [dE/dx x d ] /I0 =[ 3.87 x 0.03]/3.62 = 3.2 x 10 4 e-h pairs
  4.5×108 free charge carriers in 1cm x 1cm x 300um volume but only 3.2×104 e-h pairs produced by a M.I.P.
Need to reduce number of free carriers, hence deplete the detector
Solution: Make use of reverse biased p-n junction (reverse-biased diode)!!
E=3.62eV
h
valence band

## Slide 15: Doping and p-n Junction
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025
Doping: n-type Silicon
  add elements from Vth group
    donors (P, As,..)
  electrons are majority carriers
Doping: p-type Silicon
  add elements from IIIrd group
    acceptors (B,..)
  holes are majority carriers
-17-
Resistivity
carrier concentrations e, h
carrier mobility µ , µ
e h
r = 1q (µ e + µ h)
0 e h
 | detector grade | electronics grade
doping | � 1012 cm-3 | � 1017 cm-3
resistivity r | � 5 k·Wcm | �1 W·cm
p-n junction
The P atom donated its 5th valence electron which becomes a free charge carrier
A free place in a B atom is filled with an electron therefore a new hole is generated
B=Boron
P=Phosphorus

## Slide 16: The depletion region
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025
-
18-
p-n junction with reverse bias
At the interface of an n-type and p-type semiconductor the difference in the Fermi Levels (EF) which is the energy level with a 50% probability of being occupied by an electron at any given time cause diffusion of surplus carries to the other material until thermal equilibrium is reached. At this point the fermi level is equal. The remaining ions create a space charge and an electric field stopping further diffusion.
Operation with reverse bias
  applying an external voltage V with the cathode to p and the anode to n
  e and h are pulled out of the depletion zone. The depletion zone becomes larger.
  The potential barrier becomes higher and diffusion across the junction is suppressed. The current across the junction is very small “leakage current”.
Et voilà, that’s the way we operate our semiconductor detectors!

## Slide 17: p-n junction detector basic working principle
W
Vbias
~ +100V
photon x-ray
PE electron
+ + +
- - -
charged particle
n , K , p , µ , e
p++(n++ ) (~1µm)
n++ (p++) (~1µm)
n (p) - type
- +
- +
- +
- +
- +
- +
- +
- +
- +
Junction side
Ohmic side
thick ~300µm
E-field [V/cm]
Depth [µm]
fully-
over-depleted
under-
Ex-ray
Q sensitive amplifier
n+ and p+ electrodes are implanted on the wafer’s surfaces to form a p-i-n junction
Vbias is the applied reverse bias voltage, W is the depletion region
e-h pairs are created by the energy released by the impinging particle
e-h drift towards the positive and negative electrode “inducing “ a current pulse
Charge collection time depends on the carrier mobility, bias voltage and carrier polarity
signal
0 Si
eff
2
2ε ε
W q N
Vbias =
E= permittivity

## Slide 18: Segmented Silicon Sensors for better position sensitivity ..“imaging”
Vbias
~ +100V
photon x-ray
charged particle
n , K , p , µ , e
PE electron
+
+
+
+
+
+
+
-
- +
- +
- +
-
-
-
-
-
-
Ex-ray
n-type
p++
n++
signal
signal
signal
signal
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 19: Leakage Current
Generation Current:
From “thermal” generation in the depleted region
It’s minimal if the bulk is high resistivity and with low impurities
Diffusion Current:
Carriers from the ‘un-depleted’ region Diffusing into the depleted region
21
Doubles every 8oC
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 20: Signal to Noise and Landau distribution
SIGNAL if there is a PARTICLE
Signal formed no matter what
Detection efficiency
NO SIGNAL if NO PARTICLE
Noise under control
Discrimination
Mean (dE/dx) Si = 3.88 MeV/cm
⇒116 keV for 300 μm thick Si (~75e/um)
Most probable loss = 81 keV for 300μm Si Since 3.6eV needed to make e-h pair
⇒ charge in 300 μm= 22500 e- (=3.6 fC)
(75e/um)
Mean charge = Most probable charge ≈ 0.7× mean
23
Width depends on Substrate thickness
High energy tail From delta rays
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 21: Two-dimensional segmentation. Pixel Detectors “Hybrid”
ATLAS FE-I4~4cm2
50 microns (25um In, <10um Au)
solder
FE-I4 80x336
=26 880 pixels
125 x 50 um2
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 22: Pixel detectors “Monolithic”
Readout circuit
Collection electrode
Sensitive layer
High energy particle
IEEE TNS Vol: 56, Issue: 3, 2009
MAPS
Pixel size :
20 x 20 micron
Thickness 20-50 um
Used in the
EUDET telescope And at
STAR at RICH
CCD
Charge coupled
Device Various dimensions
Many uses in Different fields
Integrate the readout circuitry together with the detector in ‘one piece ’ of silicon
The charge generated by a particle is collected on a defined collection electrode either by diffusion or by the application of an E-field
Small pixel size and thin effective detection thickness
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 23: Pixels detectors
deepNwell
diamond
CMOS
Pixel Sensor
LePiX
DEPFET
n-in-n, n-in-p- planar
PWELL
PMOS
DEEP PWELL
SUBSTRATE
- +
+ +
- -
- -
+
+ +
EPITAXIAL LAYER
INMAPS
NWELL SUB NWELL DIODE CONT NMOS CONT
HV-MAPS
CCD
Mimosa
0.18mm
SOI
Radiation Hardness
3D sensors
Granularity, low mass
Hybrid
Monolithic
26
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 24: ALICE ITS3: a bent stitched MAPS-based vertex detector
27
Using special properties of silicon
Wafer-scale sensor ASICs – Fabricated with stitching
All electrical signals and power routed on-chip
Ultra-thin and bendable: 50 µm
266 mm (Z) x variable width* (rφ)
CMOS MAPS • 65 nm technology
Open-cell carbon foam spacers
Key benefits
Extremely lightweight
Material budget: 0.35% X0* => 0.05% X0
Uniformly distributed material
Closer to interaction point
Beam pipe radius: 18.2 mm => 16 mm
Radial position: 24 mm => 18 mm
*X0 (radiation length)=the mean length (in cm) into the material at which the energy of an electron is reduced by the factor 1/e
Slide from From Ola Groettvik
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 25: High Precision Imaging in space and time
Fundamental Science
Medical Imaging
Biology
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 26: LGAD Basics. Low Gain Detector
G. Pellegrini, Low Gain Avalanche Detectors
Core Region
  Uniform electric field,
high enough to activate mechanism of impact ionization (multiplication)
Termination
High electric field confined in the core region
Periphery
Dead region.
Charges should not be collected. Reduction of the surface leakage currents
Electric Field @ 400 V
N+
P
π
Centro Nacional del Microelectrónica
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 27: Silicon Photomultipliers (SiPm)
pixel
pixels
pixels
APD
Quench resistor
1 mm
SiPm requires a special doping profile to allow a high internal field (>105 V/cm) which generates avalanche multiplication
APD cell operates in Geiger mode (= full discharge), however with (passive/active) quenching.
The avalanche formation is intrinsically very fast (100ps), because confined to a small space.
High Gain G ~ 105 -106 at rel. low bias voltage (<100 V)
G is Sensitive to temperature and voltage variations
Fill factor still low due to quench resistor on the surface (but work in progress to solve this)
30
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 28: 40 x 40 Metalens Array for Improved Hamamatzu Silicon
31
Photomultiplier Performance
Soh Uenoyama* and Ryosuke Ota ACS Photonics 2021, 8, 1548−1555
circular transmission nanopillar varies the locally effective index by changing the diameter of the metasurface and does not depend on incident polarization.
Focal Point
~14.5um Outside focal point
Hafnium oxide (HfO2) nanopillars on a 300 μm thick glass substrate to minimise absorption in the Near UV
3x3mm2 75um
~82%
Fill factor (~50%)
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 29: 3D radiation sensors
3D silicon detectors were proposed in 1995 by S. Parker, and active edges in 1997 by C. Kenney.
Combine traditional electronics processing and MEMS (Micro Electro Mechanical Systems)
technology.
Electrodes are processed inside the detector bulk instead of being implanted on the Wafer's surface.
The edge is an electrode! Dead volume at the Edge < 5 microns!
The electric field is parallel to wafer’s surface: and smaller inter-electrode spacing: low bias voltage, low power, reduced charge sharing and high speed – for the same wafer thickness
particle
300 um
n+
p+
50 mm
-
+ +
- --
n+
Active edge
50 um
+ -
V=7V
Before
irradiation
Drift lines parallel to the surface
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 30: Precision in space and time Developments in Bulk Micro-Fabrication
11:1
1997
24:1
today
40-60:1
110:1!!!
34
NATURE https://doi.org/10.1038/s41598-020-79560-z
Deep Reative Ion Etching Cryo-etching Atomic Level Etching (ALE)
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 31
Van Lint 1980
Primary Knock on Atom
Displacement thresholds in Si:
Frenkel pair E~25eV
Defect cluster E~5keV
For X-Rays E~250KeV
Vacancy (V)
V, I MIGRATE UNTIL THEY MEET IMPURITIES AND DOPANTS TO FORM STABLE DEFECTS
What happens during irradiation to silicon detectors?
Defects formation in irradiated silicon
particle
Interstitial (I)
Ec
Ev
Ei
V2(-/0)+Vn Ec-0.40eV
V2(=/-)+Vn Ec-0.22eV
VO- Ec - 0.17eV
V6
CIOI(0/+) EV+0.36eV
V2O
Defects position in the bandgap
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 32
2E = 103um
L=IES [um] | 103 | 71 | 56 | 47 | 35
SE 1x1016ncm-2 [%] | 45 | 51 | 66 | 68 | 78
SE 2x1016ncm-2 [%] |  | 38 |  | 50 | 60
Signal Efficiency at different IES of 3D sensors
C. Da Via et al Nucl. Instrum. Meth. A 603 (2009) 319–324
71 um IBL
56 um
47 um
35um-PH2
PH2 pixel design
50x50 um2
80% signal after
1x1016ncm-2
60% signal after
2x1016ncm-2
For a 150 um sensor this means
11.250 e most probable signal before irradiation
9000 e after 1016 and 6750 e after 2x1016 ncm-2
I. Haughton et al. Nucl. Instrum Meth.A806(2016)425–431
GF Dalla Betta
IWORID 2017
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 33
3D sensors
285 microns
FE-I4 ROC 100 microns
Micro-channels
Si 450 microns
90Sr
C. Da Via, F. Munoz-Sanchez, N. Dann,
D. Hellesmidht, P. Petagna, G. Romagnoli
Paper in preparation
3D silicon : CNM double side 285 um thick IBL qualification batch
FE-I4A: thinned to 100um at IZM
Si-Si micro-channels
designed by CERN PH-DT,
  produced by PH-DT in EPFL CMi cleanroom,
  direct bonding CSEM
Glue: 2-components
Masterbond EP37-3FLFAO
3D Vertically Integrated Module
with CO2 internal cooling
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 34: Fast response and Radiation hardness
35
of 3D sensors
1×1017n!"/cm2at
250 V (T= −16◦C)
with top IR illumination
M. Manna et al. NIMA 979 (2020) 164468
IES
35um
3D Trench
180 GeV/c π+beam
Timing resolution Before irradiation
Timing resolution after irradiation
A. Lampis 23rd International Workshop on Radiation Imaging Detectors Riva del Garda, June30th 2022
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 35: Example: Tracking Identification of Event Vertices
primary event vertex reconstruction crucial in multiple collision events
secondary vertices for live time tagging
b- jet tagging
36
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 36
TOMSK talk
37
CERN-LHC
27 Km tunnel
~100m underground
CMS
ATLAS
LHCb
ALICE
LHCf
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 37: ATLAS and CMS use alone more that 250m2 of Silicon Strips to “image” charged particles
Strips
198 m2 of silicon,
9.3 million channels
Inner : 4 barrel layers, 3 end-cap disks Outer: 6 barrel layers, 9 weels
22cm < R < 120cm
Strips
61m2 of silicon.
6.2million channels 4 barrel
layers + 9 disks per endcap 30cm < R < 52cm
ATLAS
CMS
Pixels
3 Barrel layers
(r=5,9,12 cm)
2 end caps each with
3 disks
80Mpixels 50x400um2
Digital I/O
Pixels
3 barrel layers 2 end caps each with 2 disks
66 Mpixels 150 x 100um2
Analog I/O
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 38
AMS (Alpha Magnetic Spectrometer)
on ISS particle physics experiment in space
to measure antimatter in cosmic rays
FERMI Large Area
Telescope
Gamma-ray
detector
Detectors in Space
Roger Romani
Cycle of pulsed gamma rays from the Vela pulsar. Constructed from photons detected by Fermi's Large Area Telescope.
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 39: X-ray energy of the most common medical and biological applications
10
20
30
40
50
60
70
80 90 100
Energy [keV]
Protein crystallography
Mammography
Angiography
PET SPECT
Radiology
Dental imaging
0
50
10
[%] 0
100
101
102
300 um Si
500 um Si
700 um Si
1000 um Si
L. Tlustos
Absorption efficiency
C. Da Via’ 2007
Synchrotron sources
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 40: Direct/indirect conversion
Contrast
Resolution
pixel dimension-x
Signal to noise ratio S/N
Dose to the patient
Sampled image
X-rays
electronics
Direct conversion Si, Ge, CdTe, GaAs, Se
electronics
Sampled image
Photodiode/ CCD
Scintillator
Gadox, YAG CsI
(high Z)
IA/IB
Organ
Thorax, face Lumbar region Urography Brain scan
Whole Body scan Mammography
dose skin mGy
0,2 - 0,5
4 – 28
40 – 60
7 – 78
30 – 60
7 – 25
effective dose mSv
0,015 - 0,15
1,5
3
1
4 – 10
0,5 - 1
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 41: Comparison of different image qualities
This image has high spatial
resolution but very high noise
level which destroyed the image contrast
Optimum image quality has adequate
resolution and
contrast, and a low
noise level
This image has high spatial
resolution and low noise, but it has
almost zero contrast.
This mage has low noise and high contrast, but very poor spatial resolution.
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 42: Synchrotron Radiation: Diffraction Protein crystallography 12 KeV
X-ray diffracted Photographic image of the double helix taken in 1952 by Rosalind Franklin and Raymond Gosling. The DNA sample was fibrous DNA
Bragg Law
X-rays
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 43: Ghost Imaging of undetected photons
https://doi.org/10.1364/QIM.2014.QTu1A.1
Uses Quantum Entanglement – Non-local correlation, superposition states
Entangled Photons generated in Non –Linear medium
SPDC=Spontaneous Parametric Down Conversion
Bucket detector=No-segmentation placed on the line of the object. Just detects the arrival of a photon, but without position information
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 44: Ghost Imaging with Xrays
Direct
Ghost
.
15 keV
7.5 keV
L ≈ 70 cm
2r = 24.2 mm
Δ
°
°
Diamond (111)
θ
Lynx T3 Detector
2α ≈ 1.99°
The effect of parametric down conversion (PDC) is the spontaneous decay of a photon of frequency wp into two of frequencies wi and ws in an optically non-linear medium
Energy conservation, wp = wi + ws
Momentum conservation
kp = ki + ks
Quantum enhanced microscope collaboration
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 45: Environmental Radiation Monitoring
U. Stöhlker
European established networks cold war improved networks
countries
GDR
during the
period and
these
after the
Chernobyl accident in 1986.
Monitoring of: nuclear facilities
atomic bomb scenarios
terroristic attacs
Gamma Dose Rate (GDR) networks in Europe
German Network 1800 GDR stations to perform gamma Spectrometry and
Create contamination
Map for long -lived radionuclides
1cm3 coplanar grid (Cd,Zn)Te detector
Broken mountain
Inter-calibration facility (INTERCAL) on Schauinsland mountain (1200 m) since 2007
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 46: Detecting Solar Radiation for Energy Harvesting Photovoltaic
The Earth receives 174 petawatts (1015) (PW) of incoming solar radiation (insolation) at the upper atmosphere.
About 30% is reflected back to space while the rest, 122 PW, is absorbed by clouds, oceans and land masses.
In 2022 solar photovoltaic PV generated 4.5% (1284 TWh) of the world's electricity compared to 1% (253 TWh) in 2015. Wind and solar generated over 12% of the world's electricity in 2022
A solar cell is basically a p-n-diode where current, voltage and resistance
– vary when exposed to light
Land Coverage
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 47: Harvesting UV Radiation from the Sun in 2023
The
Sustainable
City in Dubai, United Arab
Emirates
Produce 87% of its needed energy over 114-acre
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 48: Solar Photovoltaic Technologies
Efficiency
Cost
Generations
Evolution
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 49: Conclusions
The development of radiation detectors and imaging technologies has always been a crucial component in scientific discoveries. Silicon being one of the most abundant element on earth still has a great potential in being a big player in sustainable solutions for the future.
By making the unseen “visible”, these detectors not only expand our understanding of the natural world but also pave the way for innovations that improve and advance human life.
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 50: References
Daniela Bortoletto, CERN Summer Student Lectures 2012 Patrick Le Du, EDIT School 2013
Helmut Spieler, Lecture notes (IBL)
Hartmut Sadrozinski, GianLuigi Casse, Vienna Instrumentation Conference 2013
Michael Moll, PhD Thesis
Steve Watts, CERN Academic Training Harris Kagan,TIPP 2009
Roland Horisberger, Silicon Detector WorkshopSplit, Croatia 2012 Marco Povoli, PhD thesis 2013
Gregor Kramberger
Andrea Castoldi, course given at the Advanced School and Workshop on nuclear signal processing, Acireale Italy, November 2011
Chris Damerell, Sherwood Parker, Erik Heijne, Ariella Cattai
53
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025

## Slide 51: Books on silicon detectors
Rossi, Fisher, Rohe and Wermes. Pixel Detectors from fundamentals to applications. Springer
Helmut Spieler. Semiconductor detector systems. OUP Oxford
Gerard Lutz. Semiconductor Radiation Detectors. Springer
W. R. Leo. Techniques for Nuclear and Particle Physics Experiments. Springer- Verlag
C. DaVia, GF. Dalla Betta, S. Parker, Radiation Sensors with 3D electrodes, CRC Press
54
Cinzia Da Via, Stony Brook USA and The University of Manchester, UK– 2025