## Slide 1: Measurements of a LYSO Crystal Array for a Rare Pion Decay Experiment (PIONEER)
David Hertzog; University of Washington
Lepton Flavor Universality (e vs m to <10-4 in BR)
Cabibbo Angle Anomaly (Vud) pion beta decay)
Sterile neutrinos and exotic decays:
10 x Improvements in precision
All of these involve high-resolution calorimetry in the (unusual) “below 100 MeV” range
Physics Goals
illustrate challenge with this channel
2D cartoon of experiment
x 10-4
What is this?
LXe?
LYSO?
Interested in growing PIONEER Collaboration? Contact me: hertzog@uw.edu

## Slide 2: How the Calorimeter is used in a pi-e-nu measurement
tm = 2197 ns
tp = 26 ns
70 MeV
The key is to minimize the fraction of p  e events that hide below the Michel spectrum: “The Tail”, and determine that fraction well
Must measure (and model) the full line shape
Resolution makes Hi / Lo boundaries more distinct
20 X0 deep calorimeter: Tail fraction <0.5%
Use a highly segmented, 5D tracking pion stopping detector to reject Michel and other low-energy events
(subject of a separate talk)
Tail fraction uncertainty <0.01%
Tail
The Tail
p  e
p  m  e
See Y. Zhang; Pioneer presentation
Room 121 at 3 PM today
Resolution and Depth are important

## Slide 3: What material might work?
Lutetium–yttrium oxyorthosilicate (LYSO):
By weight: 72% Lutetium, 17% Oxygen, 6% Silicon, 3% Cerium (dopant), 2% Yttrium
X0 = 1.14 cm , RM = 2.07 cm
Decay time = 40 ns
Light yield 30,000 g/MeV
lpeak 420 nm -> conventional PMTs
Radioactive (< 1 MeV constant rumble)
Non hygroscopic
No Temp dependence
n = 1.82
Not so cheap … 
LXe (used in MEG II) has excellent properties, but cannot be segmented
LYSO crystals look promising, but no one has yet achieved needed resolution
Goal of this R&D: Test newer LYSO formulation with attention to details to achieve the resolution promised by the intrinsic properties.
History: Some arrays tested, obtained 4.5% @70 MeV, which met their goals
  Can we do better?
A test by Mu2e

## Slide 4: LYSO Intrinsic Light Properties
Absorption
Emission
300 350 400 450 500 550 600
Wavelength (nm)
Can extend transmission by using Wrattan 3E yellow filters at the cost of light
An interesting fact, LYSO intrinsic radioactivity.
Built in calibration!
Slight concern when seeking best resolution at low energies from an array
 From the beta decay of Lu-176
0.1 0.6 1.2 MeV
Alva-Sánchez et al. Understanding the intrinsic radioactivity energy spectrum from 176Lu in LYSO/LSO scintillation crystals. Sci Rep 8, 17310 (2018).
Notes: Emission spectra is measured by excitation with a UV LED (spectra shown). The ‘spectral density’ scale is intensity (counts in 180 ms) divided by the crystal length.
Transmission is the percentage of light that passes through the crystal. A pulsed xenon light source was used
Because of the high index of refraction, the light spreads out less in LYSO than in air, so the reference spectrum of air has to be rescaled. Using Snell’s Law, the corrected reference is the original reference spectrum times the LYSO index of refraction squared.
Absorbance is defined as the negative (base 10) log of transmission. The result is also scaled by crystal length.
Absorption and emission are consistent across all SICCAS crystals, transmission varies more widely

## Slide 5: Single crystal tests of recent SICCAS* formulation
2.5 × 2.5 × 18 cm3 (15.7 X0)
Co-60 tomography to measure longitudinal uniformity / attenuation
ESR-wrapped LYSO crystal
Measure Peak Positions vs Impact along crystal
60Co
(The Trigger)
Distance from PMT
red
*Shanghai Institute of Ceramics (made our PbF2 crystals for g-2)

## Slide 6: Energy resolution with “bench” sources
Na22
Co-60
Na-24*
  1.38, 2.76 MeV
*Short lived (15 hr half life); emits a series of g
Source made by bombarding 18 MeV deuterons, produces neutrons that strike an Al button (done at CENPA Van de Graaff)
(2g sum)
(2g sum)
(Resolution is sigma of a Gaussian)
(2g sum)
2g implies coincidences of lower energy lines
(this is why they are used in most PET scanners now)
511 keV
2.76 MeV
1.17 & 1.33 MeV

## Slide 7: Measurements with 10 crystals
Read out with R1450 Hamamatsu 19-mm PMTs using a customized, tapered voltage divider
p-Li calibration following L3 @ LEP and MEG-II.
We use a 1.4 MeV proton beam degraded and impinging on a LiF foil. @440 keV it excites a resonance, which decays with a 17.6 MeV gamma (and other lower energy lines)
1.4 MeV p
LiF
2.6% at 17.6 MeV
This is state-of-the art resolution

## Slide 8: Next, p/m/e beam at PSI
PMT
PMT
PMT
PiM1 is ideal up to a few hundred MeV/c
  DP/P measured to be <0.6% for range of measurements
  Positrons energy scan: 30 – 100 MeV
  Muons @ 210 MeV/c used for transverse tomography
Expt
Scint
T0
3%
m
Distance from PMT
1 4 7 10 13 16 cm

## Slide 9: Timing Resolution vs Positron Energy
Use T0 vs fitted Crystal waveform time
  Plot is Xtal to Xtal time diff
e+
X-Y
Hodoscope
NaI border
LYSO array
T0
Time Difference between adjacent crystals
Easily meets our goal
Divide by root(2) for individual timing

## Slide 10: Uniformity across Crystal Boundary at 70 MeV
Used X-Y hodoscope and moving table to scan front of array

## Slide 11: Energy Resolution vs Positron Energy
Fits using Crystal Ball function
Resolution is sigma of high-side Gaussian
Notes: Many configurations were tested. Yellow filters (out/in); PMT dividers (built-in vs tapered);
Only 7 tapered dviders were available at PSI; later made 10 made for follow-up run with p-Li source @CENPA
Electronics / PMT non-linearity at PSI
0
The 17.6 g measured after the PMT dividers were upgraded
50 MeV
66 MeV
70 MeV
MEETs GOAL

## Slide 12: Next: Test 3 tapered crystals in a realistic final geometry for the experiment (concepts shown)

## Slide 13: Summary
Grad students
Undergrad
The Team
LYSO tests of single crystals and array of 10 confirm performance expectations
  Fast, Dense, Uniform, Bright
Timing resolution <200 ps
Energy resolution <2% at 70 MeV
  Meets our target for p->e decay
A paper is being written
Next Steps: Explore tapered crystals

## Slide 14: Pulse shape

## Slide 15: MEG resolution with p-Li
3.6% Energy Resolution
MEG 1
MEG 2

## Slide 16: Details of the p-Li method
A 440 keV proton excites the 17.6 MeV level which decays to both the ground state and to a 3 MeV level with a 14.6 MeV gamma.
We use a 1.4 MeV proton beam, which is appropriate degraded through theta foil and the LiF crystal itself to the resonance energy

## Slide 17
Ren-yuan Zhu, Caltec

## Slide 18: LYSO Intrinsic radioacivity