## Slide 1: <10 meV MTE from Cu
- Siddharth Karkare (Department of Physics - ASU)
What does MTE depend on?
  Excess energy, roughness, band-structure
Demonstration of sub-10 meV MTE
  Can be obtained from Cu(100) surface cooled to 30 K
How to translate low MTE to high brightness?
  Defeat electron heating

## Slide 2: MTE, Brightness and Emittance
I. Bazarov et al., Phys. Rev. Lett. 102, 104801 (2009)
Cathodes Used Today
Brightness
MTE (meV)
1000
1
10
100

## Slide 3: MTE limiting factors (1) – Excess energy
Energy
Fermi level
Vacuum level
Work
Function
W
Lower photon energy to the work function
Cool to low temperature
Limited by kT at threshold
Penalty for operation is low QE
J. Feng, S Karkare et al. APL 107, 134101 (2015)

## Slide 4: MTE limiting factors (2) -Surface non-uniformities
Physical Roughness
Chemical Roughness
S. Karkare and I. Bazarov, Phys. Rev Applied, 4, 024015 (2015)
J. Feng, S. Karkare et al, J. Appl. Phys. 121, 044904 (2017)
G. Gevorkyan et al. Phys. Rev. ST- Accel and Beams, 21, 093401(2018)
Need single crystal ordered surfaces to minimize MTE

## Slide 5: MTE limiting factors (3) – Band structure
S. Karkare et al. Phys. Rev. B 95, 075439 (2017)
S. Karkare et al. Phys. Rev. Lett. 118, 164802 (2017)
Effect surface state of Ag(111)

## Slide 6: Measuring Low MTE
Delay Line
Detector
Cryostat
Electrostatic shield
Sample
Sample
Incident laser pulse (fs-ps)
Electrons drift towards detector
MCP stack
X, Y Delay lines
(x, y, t) of electron hitting the MCP
Has sub-meV energy resolution!!!
Can obtain complete energy/momentum distribution
MTE = 28 meV
4.5 eV at RT
8 V
acceleration
4 V
acceleration
MTE = 6 meV,
4.43 eV at 30 K

## Slide 7: Cu(100) – Ideal for low MTE
X (100)
Photoemission threshold at ~4.5 eV – can be accessed by our laser
Cooled to LHe (30K)
Projected band-structure
Atomically ordered flat surface
0 Transverse
momentum
direction
Work function

## Slide 8: Cu(100) – Smallest MTE measured
6 meV MTE measured from Cu(100)
Previous record was 22 meV from Cs3Sb at 90K
Issue – Very low QE (~10-8) …
Still suitable for single electron/ bunch applications
For large charge densities – electron heating/multi-photon emission – Jai Kwan Bae’s talk
Room Temperature
30K
6 meV!!
Work function reduced!!! – first measurement of work function of Cu(100) at LHe temp ??
Andreas Schroeder’s talk on Wednesday for theory description

## Slide 9: Beat Electron Heating – CBB efforts
Small effective masses yield smaller for a given excess energy,
Predictions from band-structure
Measurement
Does not work for PbTe(111)!!!
Use single crystals with small effective masses
Kevin Nangoi’s talk on Wednesday
Use Low Electron Affinity semiconductor cathodes – Alkali-antimonides, GaAs(Cs/O)
Electron heating is mitigated
Have higher QE even at threshold
However, roughness is an issue
Will DeBenedetti’s talk in next session
Gevork Gevorkyan’s talk in next session
Howard Padmore’s talk tomorrow
New low effective mass materials:
Joshua Paul’s talk this session
Chris Pierce’s talk next session

## Slide 10: Acknowledgements
LBNL
Howard Padmore
Siddharth Karkare (now at ASU)
Cornell
Jared Maxson
UIC
Gowri Adhikari
Andreas Schroeder
NSF and DOE
for funding

## Slide 11: Basic setup and equations
DLD
Sample
Shield
d
d1
V=0
Vshield-Voff1
Vsam-Voff
Red  known/can be varied and measured
Green  unknown but constant for one sample
d+d1
S
1.
2.
x, y, t are recorded for each electron hitting the DLD
MTE is calculated by averaging over all detected electrons

## Slide 12: Obtaining Flat equipotential lines
DLD
Sample
Shield
d1
V=0
Vshield-Voff1
Vsam-Voff
DLD
Sample
Shield
d1
V=0
Vshield-Voff1
Vsam-Voff
DLD
Sample
Shield
d1
V=0
Vshield-Voff1
Vsam-Voff
DLD
Sample
Shield
d1
V=0
Vshield-Voff1
Vsam-Voff
A
A
A
A
A’
If fields are not flat, the shield electrode acts like an non-linear electron lens and the electron spot on the DLD moves when the manipulator (sample+shield) position is changed w.r.t the DLD, keeping the incident laser spot fixed w.r.t DLD
e-
e-
e-
e-
FLAT EQUIPOTENTIAL LINES
CURVED EQUIPOTENTIAL LINES
Manipulator shifted w.r.t DLD