## Slide 1: Requirements and Challenges of Photocathodes for Free Electron Laser Applications
Oct 15, 2018
Bruce Dunham
DRAFT

## Slide 2
SACLA 2011
8.5 GeV,
60Hz NC
European XFEL 2017
17.5 GeV, 2800 x 10 Hz SC
PAL XFEL2016
10 GeV
60Hz NC
SWISS FEL 2018 5.8 GeV
100 Hz NC
2
Shanghai SHINE 2025 8 GeV
1 MHz SC
LCLS-II 2020 4 GeV
1 MHz SC
LCLS-II-HE 2025 8 GeV
1 MHz SC
Hard X-ray FELs
Notes: SACLA thermionic
PAL copper
LCLS-II, CsTe
LCLS-I Copper
XFEL – CsTe
SwissFEL copper
Shanghai – CsTe

## Slide 3
Other FELs
Jlab IR/UV FEL
88-135 MeV
74.85 MHz
Novosibirsk THz FEL
40 MeV
90 MHz
HZDR FEL
12-34 MeV
13 MHz
Notes: Boeing FEL used CsKSb
Only metal, CsTe and thermionic cathodes in regular use – what are we doing wrong???
Industrial FEL, EUV
CHALLENGE!! How to justify all the work we have and want to do
QW GaAs only real advance in memory

## Slide 4
SASE FEL Electron Beam Requirements
eN < 0.5 µm at 1 Å, 15 GeV
<0.04% at Ipk = 3 kA, K  3, lu  3 cm, …
18LG ≈ 60 m for eN  0.5 µm
P(z) = P0 ∙ exp(z/LG)
relative energy spread:
Notes: We must increase peak current, preserve emittance, and maintain small energy spread so that power grows exponentially with undulator distance, z,
P(z) = P0 ∙ exp(z/LG)
FEL power reaches saturation at ~18LG
SASE depends exponentially on e- beam quality (to be exploited)

## Slide 5: Example: FEL output vs. Injector emittance
LCLS peak FEL performance
LCLS hard X-ray (> 6.5 keV) energy loss data w/ nominal injector charge

## Slide 6
Motivation for lower thermal emittance (LCLS-II-HE)
Chart: Maximum Wavelength for 100 uJ
| 7 | 7.25 | 7.5 | 7.75 | 8 | 8.25 | 8.5 | 8.75 | 9
Nominal Emitt | 10.92 | 11.34 | 11.76 | 12.18 | 12.6 | 13.02 | 13.44 | 13.8075 | 14.175
75% Nominal Emitt | 12.6 | 13.23 | 13.86 | 14.4375 | 15.015 | 15.5925 | 16.17 | 16.7475 | 17.2725
50% Nominal emitt | 14.49 | 15.33 | 16.17 | 17.0625 | 17.9025 | 18.7425 | 19.5825 | 20.4225 | 21.2625
125% Nominal Emit | 9.45 | 9.765 | 10.1325 | 10.4475 | 10.71 | 11.025 | 11.2875 | 11.55 | 11.8125
Photon Energy (keV)
Electron Energy (GeV)
Emittance at Undulator
The emittance at the injector will need to be at least 4X lower than we can generate now to reach 20 kV (< 0.1 um needed)
LCLS-II Injector

## Slide 7: Beam transport limitations from 100 MeV  8 GeV
Nominal Slice Emittance Evolution
Slice e: 0.22/0.22  0.26/0.30 um
High Brightness Slice Emittance Evolution
Slice e: 0.08/0.07  0.19/0.24 um
Better cathodes do not solve everything …

## Slide 8: System Level Knobs for FEL Performance
How to achieve better emittance at the undulators?
  Cathodes with lower εth and improved laser shaping
  Wavelength dependence of εth
  Temperature dependence of εth
  Laser shaping
  Cathode heating, other effects
  Low Frequency Guns
  Longer initial pulse (lower Ipeak)
  Less RF curvature
  Gun gradient
  Gun energy
System Design and Optimization
Cathodes and Lasers
  Injector and FEL optimizations
  Layout optimized for lower Ipeak
  Controlling instabilities
  Emittance compensation
  Start-to-end simulations
  Laser shaping
Gun Design
Notes: U bunching instabilities driven by laser modulations

## Slide 9: MTE Ranges available today
Metals
  25-40 meV near threshold
  Very low QE<10-6.
Alkali-antimonides
  25-40 meV near threshold
  Low QE <10-4.
GaAs/(Cs,O)
  25-40 meV near threshold
  long response time
1 eV
100 meV
1 meV
10 meV
Practically used MTE’s
MTE limited by disorder induced heating (DIH)
emittance
0.44 um / mm-rms
0.14 um / mm-rms
0.04 um / mm-rms
1.4 um / mm-rms
Log-scale

## Slide 10: Average Current and Bunch Charge
Average currents for FELs are in the range of ~10 nA up to ~10 mA with bunch charges of ~10 pC up to ~500 pC
The rep rate is the biggest driver for average current, with ‘industrial’ applications at the high end. CW systems more in use.
The majority of machines are <100 uA and ~100 pC
  Much less demanding for cathodes (QE not a big concern)
  Opens up opportunities for: metals, near threshold emission, etc
  Cathode lifetime is less of a concern (2 week lifetime desired)
The relatively modest demands on current/bunch charge open up possibilities for big reductions in thermal emittance.

## Slide 11: Example: Improvements for LCLS-II
Na2KSb
CsTe is the baseline cathode for LCLS-II. An easy win for lower emittance:
change to a better cathode with visible/IR excitation
Initial simulations indicate that ~0.20 um (95%) can be obtained:
This cathode is desired because:
It can run ‘hot’, and the LBL gun operates at >50C
Has already demonstrated 65 mA with reasonable lifetime in a DC gun
Improved emittance control with laser shaping in the green/IR
Full characterization of a NaKSb photocathode in the APEX gun to prove out feasibility for LCLS-II/HE

## Slide 12: Example: Metal Cathodes
J. Teichert ERL17 workshop
Theoretical understanding and full characterization of the thermal emittance and QE versus wavelength of Mg/Pb cathodes for use in an SRF gun, material properties, roughness, …
Magnesium has the highest QE of a (machinable) metal – 0.2% at 260 nm
Can be cleaned in-situ
Low dark current
Cathodes can be machined then cleaned and prepared to be particle-free
Bunch charges up to 300 pC and current of 30 uA have been demonstrated
One measurement (BNL) indicates that it has lower thermal emittance than predicted
Mg plugs for an SRF gun

## Slide 13: Example: SRF Gun with a lead cathode (DESY)
Pb is a superconductor
QE of ~0.05%
100 pC operation feasible
Vertical tests underway at DESY
Waiting for results from DESY

## Slide 14: Properties of Alkali Photocathodes
Cs3Sb
Na2KSb
QE drops near threshold and with decreasing temperature.
Not a big concern for most FELs
Operation at cold temperatures a good match for CW SRF guns
Need a better understanding of properties at < 80K
Cultrera et al, APL 108, 134105 (2016)
Longer laser wavelengths
Colder temperatures
Notes: These plots show some recent measurements on alkali cathodes. Each have emittance on the left axis and laser spot size on the bottom. The slope gives the thermal emittance per mm of laser spot size, our usual way to describe cathodes a low current. The left shows what happens as the laser wavelength is changed from green to infrared – the emittance drops > 2X. Cooling it down drops in even further.
Note that the QE drops for longer wavelengths, and for colder temperatures
The could be the first step in a staged approach to harder x-rays – a new cathode and laser.
R&D: full characterization over 4K-300K, operation in an SRF gun, dark current/multipacting, particle free growth and transport,surface roughness

## Slide 15: Other Topics to Consider
Induced heating
Longitudinal non-linearities that reduce compression efficiency
Longitudinal non-linearities that drive instabilities
Optimizing laser shaping for emittance and/or FEL performance

## Slide 16: Final Example: Path forward for LCLS-II-HE and 20 keV
Lower intrinsic emittance allows improved beam brightness
Intrinsic emittance (um/mm rms) | Total intrinsic emittance (um) | 100% emit. at zrms = 1 mm (um) 200K MP
1.0 | 0.114 | 0.142 (0.116, 95%)
0.4 | 0.065 | 0.093 (0.075, 95%)
0.2 | 0.042 | 0.075 (0.061, 95%)
Comparison of WiFEL-type gun (40 MV/m) performances for different cathode εintrinsic

## Slide 17
Summary
Challenges
Requirements