## Slide 1
Spin polarized low energy electron microscopy:
3D vector-magnetometry
and workfunction mapping
Andreas Schmid, LBNL

## Slide 2
light
photocathode
electron beam
P3
acceleration

## Slide 3
Sample
electron beam
Spin polarized low energy electron microscopy
Deceleration

## Slide 4
Sample
Spin polarized low energy electron microscopy
accelerate reflected e-
photocathode
image screen
decelerate primary beam
dipole
beam
splitter

## Slide 5
Electrically driven domain-wall motion
Pt/Co/Ni/Co/Pt
CoFe/Pt or Ta
K.-S. Ryu, Nature Nanotech. 8, 527 (2013)
S. Emori, Nature Mater. 12, 611 (2013)
A. Brataas Nat. Nanotech. 8, 485 (2013)
Propagation of domain wall using spin-orbit torque:
Very high velocity [Thiaville, A. et al. Europhys. Lett. 100, 57002 (2012)]
Suppressed critical current [Tretiakov, O. A. et al. Phys. Rev. Lett. 105, 157201 (2010)]
Chirality-dependent direction of motion [Khvalkovskiy, A. V. et al. Phys. Rev. B 87, 020402(R) (2013)]

## Slide 6
Spirals,
Skyrmions,
Chiral domain walls, …
Bode, et al. Nature 447, 190 (2007)
Ferriani et al. PRL 101, 027201 (2008)
Meckler et al. PRL 103, 157201 (2009)
Sessi, et al. PRL 103, 167201 (2009)
Muhlbauer et al., Science 323, 915 (2009)
Yu et al., Nature 465, 901 (2010)
Yu et. al., Nature Mat. 10, 106 (2011)
Heinze, et al. Nat Phys. 7, 713 (2011)
Yoshida et al. PRL 108, 087205 (2012)
Menzel et al. PRL 108, 197204 (2012)
Seki, et. al., Science 336, 198 (2012)
Bauer et al., PRL 110, 177207 (2013)
Romming et al. Science 341, 636 (2013)
Ryu, et al. Nat. Nanotech. 8, 527 (2013)
…
STM, TEM, Moke, etc.
Magnets with broken inversion symmetry:
image, understand, control chiral magnetism

## Slide 7
Spin polarized low energy electron microscopy image of Fe/Ni thin film
MX
Pixel brightness
=
x-component of magnetization vector.
Field of view: 10 μm diameter in images in this talk, unless mentioned.
3ML Fe
Cu (001)
2ML Ni

## Slide 8
SPLEEM: imaging 3D magnetization vector
MX
“A compact electron-spin-polarization manipulator”
T. Duden, E. Bauer, Rev. Sci. Inst. 66, 2861 (1995)

## Slide 9
3 SPLEEM images,
3 cartesian components of magnetization
MX MY MZ

## Slide 10
SPLEEM: 3D vector-map of magnetization

## Slide 11
Directly identify right-handed and left-handed spin textures
SPLEEM: 3D vector-map of magnetization

## Slide 12
Spirals,
Skyrmions,
Chiral domain walls, …
SPLEEM
G. Chen et al. PRL 110, 177204 (2013)
G. Chen et al. Nat. Comm. 4, 2671 (2013)
G. Chen et al. APL 106, 062402 (2015)
G. Chen et al. APL 106, 242404 (2015)
G. Chen et al. Adv. Mater. 27, 5738 (2015)
G. Chen et al. Nat. Comm. 6, 6598 (2015)
G. Chen et al. Nat. Comm. 8, 15302 (2017)
H. Yang et al. Nature Mat. 17, 605 (2018)
…
Magnets with broken inversion symmetry:
image, understand, control chiral magnetism

## Slide 13
Work function mapping:
(i) Hall thrusters
(ii) Thermionic power generation

## Slide 14
Hall thrusters: electrically powered rocket engines
Tyson C Back, AKS, Steven B Fairchild, John J Boeckl, Marc Cahay, Floor Derkink, Chen Gong, Ali Sayir

## Slide 15
Solar powered rocket engine.
NASA probe “Dawn” (now visiting Ceres)
Xe ion beam: High efficiency because exhaust velocity is high.

## Slide 16
Solar powered rocket engine.
NASA probe “Dawn” (now visiting Ceres)
Xe ion beam: High efficiency because exhaust velocity is high.
Propulsion system depends on
e-beam to neutralize the Xe+ beam.

## Slide 17
M.S. McDonald et al., IEPC-2017-253
Cathode materials: poor fracture toughness

## Slide 18
A. Taran et al., Functional Materials 20, 485 (2013)
High strength and low workfunction:
directionally solidified LaB6-MeB2 compounds

## Slide 19
Functional imaging: heat sample, image thermionic emission
LaB6-VB2: high strength, low workfunction
LaB6-matrix:
dark
VB2-nanorods:
bright
T. Back et al., Ultramicroscopy 183, 67 (2017)

## Slide 20
Functional imaging: heat sample, image thermionic emission
LaB6-VB2: high strength, low workfunction
LaB6-matrix:
dark
VB2-nanorods:
bright
T. Back et al., Ultramicroscopy 183, 67 (2017)

## Slide 21
10
5
0
-5
-10
-15
Sample band structure and density of states
Energy
EF
work
function
Electric field between column and sample
above work function: transmission/reflection ≈ DOS
below work function: 100% reflection

## Slide 22
10
5
0
-5
-10
-15
Sample band structure and density of states
Energy
EF
work
function
Electric field between column and sample
Imaging Workfunction

## Slide 23
Work function measurements from energy dependence of electron reflectivity: LaB6
Chart: 
Reflectivity [%]
Voltage between cathode & sample

## Slide 24
Work function measurements from energy dependence of electron reflectivity: LaB6
Chart: 
Reflectivity [%]
Voltage between cathode & sample
Φsample – Φcathode = 0.8 eV
Φcathode = 1.6 eV
=> Φsample = 2.4 eV

## Slide 25
T. Back et al., Ultramicroscopy 183, 67 (2017)
LEEM workfunction mapping: LaB6-VB2
1 μm

## Slide 26
LEEM workfunction mapping,
in-situ deposition onto LaB6-VB2
1 monolayer boron
1 monolayer lanthanum
1 monolayer vanadium
1 μm
T. Back et al., Ultramicroscopy 183, 67 (2017)

## Slide 27
Directionally solidified LaB6-VB2:
High strength under extreme conditions
Workfunction can be significantly lower than LaB6 host compound

## Slide 28
Work function mapping:
(ii) Electrical power generation
Andre Cauduro, Lucas Hess, Frank Ogletree, Jared Schwede, AKS

## Slide 29: Acknowledgement
Dan Riley
en.wikipedia.org/wiki/Steam_turbine#mediaviewer/File:Turbine_Philippsburg-1.jpg

## Slide 30: Power generation landscape

## Slide 31
EF
low work
function
high work
function
Energy

## Slide 32
EF
low work
function
high work
function
Energy
space charge

## Slide 33
Thermionic energy conversion
GE Research, 1963 (PCE ~4.5%).

## Slide 34: Efficiency potential, thermoelectrics and thermionics
Jared W. Schwede, Spark Thermionics
Thermionics
Thermoelectrics
WF =
WF =
WF =

## Slide 35: Optimizing thermionics anode for:
I. T. Lim, S. A. Lambert, J.-L. Vay, J. W. Schwede, APL 112, 073906 (2018)
low workfunction
low reflectivity

## Slide 36: Thermionic converter: “black box”
Low workfunction
anode
Thermionic
cathode
Heat

## Slide 37: Opening the “black box”: Low energy electron microscopy as a model thermionic converter
sample
accelerate reflected e-
photocathode
image screen
decelerate primary beam
dipole
beam
splitter

## Slide 38: In-situ cesium deposition on Cr(110)
Φ (Cr110)=4.9eV
Φ (CsMin)=1.6eV
Φ (CsCr110)=2.0eV
Cr [110]
Reflectivity

## Slide 39: Current absorption
60 % absorption

## Slide 40: Polycrystalline anode materials (W)
1
2
3
3μm
Different grains: different workfunction, different reflectivities
BF-LEEM
IV-LEEM
Reflectivity
Landing Energy/eV

## Slide 41: Polycrystalline anode materials (W)
1
2
3
3μm
Different grains: different workfunction, different reflectivities
BF-LEEM
IV-LEEM
Reflectivity
Landing Energy/eV

## Slide 42: Polycrystalline anode materials (W)
1
2
3
3μm
Different grains: different workfunction, different reflectivities
BF-LEEM
IV-LEEM
Reflectivity
Landing Energy/eV
Hunch: what if we suppress grain growth?

## Slide 43: Vapor deposition Cr on cold Si: ‘nanograined’ Cr anodes
Φ (CrNano)=4.4eV
Φ (CsMin)=1.6eV
Φ (CsCrNano)=1.8eV
Φ (Cr110)=4.9eV
Φ (CsMin)=1.6eV
Φ (CsCr110)=2.0eV
Cr ‘nano’
Cr [110]
Reflectivity
A. Cauduro et al., to be published
Cr(110)
Cr(‘nano’)

## Slide 44: Current absorption
60 % absorption
As-deposited Cr films lead to enhanced current absorption
specular and diffuse reflection is quenched
78 % absorption

## Slide 45: Using LEEM for thermionics anodes development:
 | Crystalline Cr [110] | Nanograined Cr/W | Nanograined Mo/Si
IAbsorbed % a | 60 | 78 | 80
Φcesiated eV | 2.0 | 1.8 | 1.7
a Integrated current absorption from 0-2 eV.
Identify low-workfunction systems
Identify low-reflectivity systems

## Slide 46: Using LEEM for anodes & cathodes discovery:
Quantitative characterization of low-workfunction
and/or low-reflectivity systems
In-situ thermionic emission imaging
Photoemission electron microscopy (just add light)
Workfunction mapping at high resolution
In-situ MBE sample growth
In-situ cesiation
In-situ negative electron affinity preparation

## Slide 47
Tyson Back
Steven B. Fairchild
John J. Boeckl
Marc Cahay
Ali Sayir
Jared Schwede
Lucas Hess
Frank Ogletree
Gong Chen
Andre Cauduro
Roberto Lo Conte
McCallum Robertson
Floor Derkink
Thanks!

## Slide 48: Research Made Possible By the Molecular Foundry
A knowledge-based user facility for nanoscale science at Lawrence Berkeley National Laboratory
Provides free access to multidisciplinary expertise and instrumentation
Proposal calls in March and September
foundry.lbl.gov