## Slide 1
Space-Charge Dominated Photoemission in the Photocathode RF Gun at PITZ
Ye Chen and Mikhail Krasilnikov for the DESY-PITZ team
The 5th Photocathode Physics for Photoinjectors (P3) Conference
Santa Fe, New Mexico USA, October 15-17, 2018
Acknowledgements to
D. H. Dowell, SLAC, C. Hernandez-Garcia, J-lab, R. Ganter, PSI, C. Hessler, CERN
F. Brinker, M. Dohlus, K. Floettmann, W. Hillert, S. Lederer, S. Schreiber, DESY
P. Michelato, L. Monaco, C. Pagani, D. Sertore, INFN, H. Chen, Y.-Ch. Du, W.-H. Huang, Ch.-X. Tang, Q.-L. Tian, L.-X. Yan, Tsinghua University
A. Arnold, J. Teichert, R. Xiang, HZDR, H. De Gersem, E. Gjonaj, T. Weiland, TEMF
for kind support and useful discussions on photocathode and photoemission
Photo Injector Test facility at DESY in Zeuthen

## Slide 2: Outline
PITZ facility
Observation & characterization of SCDPE
Summary
SCDPE: Space-Charge Dominated PhotoEmission

## Slide 3
The PITZ Facility
DESY Zeuthen Campus nearby Berlin
PITZ
Zeuthener See
http://www.desy.de/

## Slide 4
Development, test and optimization of high brightness electron sources
for SC linac driven FELs + applications
RF Gun
L-band (1.3 GHz) 1.6-cell copper cavity
Ecath ≥ 60 MV/m  7 MeV/c e-beams
650 µs ×10 Hz  up to 45 kW av. RF power
Cs2Te PC (QE~5-15%)  up to 5 nC/bunch
Solenoids for emittance compensation
LLRF control for amp and phase stability
The DESY-PITZ guns are in use at the European X-ray Free Electron Laser (European-XFEL) and the Free electron LASer in Hamburg (FLASH).
<7MeV
<25MeV
PITZ Beam Line 3.0
UV
Laser
 Details: https://pitz.desy.de/

## Slide 5: PITZ evolution 2002-2017
Highlights of the Evolution:
Increasing the brightness (decreasing the emittance)
Improving gun stability and reliability
Extending beam diagnostics
Use high brightness beam capability
Photocathode and cathode laser

## Slide 6: Flexible Photocathode Laser pulse shaping system
MBI Pulse Shaper
Pulse Train Time Structure
PITZ and EXFEL run bunch trains with up to 600 (2700) laser pulses
Comb
Towards ultimately low emittance beams
 3D ellipsoidal pulses (under development)
Proof of principle demonstrated with IAP (JINR) system at PITZ (2016-2017)
Comparison with simulated e- beam shapes (500pC): similarity in shape
Gaussian laser
Flattop laser
Ellipsoidal laser
Details in J. Good et al., Proc. 38th FEL Conf., WEP006 (2017)
First Measurement
@EMSY1
@PST.Scr1

## Slide 7: Photocathode in the gun: Cs2Te
Visual inspection
QE measurement
QE map
Cs2Te produced at DESY and INFN-LASA
QE: 5~15% @ 257 nm
Up to 5 nC/single bunch possible
Vacuum level in the gun: ~10-9 mbar
For nominal operation (~6.5MW×650µs) dark current < 100µA (for different guns)
Dark current measurement
YAG Screen
Faraday cup
insertable
Dark current
on Screen
~0.8m
~ 1 month
~ 4 months
Max. dark current vs. RF power during gun conditioning
 ≈ 92
IF: current [A], E: field [V/m]

## Slide 8
Operation: Working Points at European-XFEL, FLASH & PITZ
Representative cathode drive laser intensity
At European-XFEL and
FLASH working points, the
beam extraction at cathode
strongly influenced by space-
charge effects
Best emittance measured at
the working points, e.g. for
1nC beam at European-XFEL
320pC
0.45
0.40
0.35
0.30
0.25
0.20
0.15
0.10
0.05
0.00
Laser pulse energy [µJ]
0 0.02 0.04 0.06 0.08
1nC
0 0.5 1.0 1.5 2.0 2.5 3.0 3.5 4.0
Qbunch [nC]
1.6
1.4
1.2
1.0
0.8
0.6
0.4
0.2
0
Q [nC], emitted bunch charge
experiment
experiment
RF@~6.5MW×650µs | RF@~4.8MW×600µs
1nC  European XFEL, PITZ ~320pC  FLASH, PITZ

## Slide 9
σrms=0.4mm
σrms≈0.3mm
measured
simulated
σrms=0.3mm
Uniform
Uniform
C+H
Charge vs. Laser Energy
Core(C)+Halo(H) model:
fits for Gaussian temporal
distribution (see backup slide)
but not for flattop case
NIM A 871, 97-104 (2017)
Operation: Discrepancies of Emitted Charge in simulation vs. measurement
E-XFEL
case
Representative cathode drive laser intensity
320pC
0.45
0.40
0.35
0.30
0.25
0.20
0.15
0.10
0.05
0.00
Laser pulse energy [µJ]
0 0.02 0.04 0.06 0.08
1nC
0 0.5 1.0 1.5 2.0 2.5 3.0 3.5 4.0
Qbunch [nC]
1.6
1.4
1.2
1.0
0.8
0.6
0.4
0.2
0
Q [nC], emitted bunch charge
experiment
experiment
RF@~6.5MW×650µs | RF@~4.8MW×600µs
1nC  European XFEL, PITZ ~320pC  FLASH, PITZ

## Slide 10
Operation: Discrepancies of Emittance in simulation vs. measurement
Emittance vs. Cathode Laser Spot Size
Lager discrepancies for stronger space-charge dominated e-beams
Problems may (partially) originate from photocathode already?
20pC
100pC
250pC
1nC
Stronger
effects
PRST-AB 15, 100701 (2012)
Representative cathode drive laser intensity
320pC
0.45
0.40
0.35
0.30
0.25
0.20
0.15
0.10
0.05
0.00
Laser pulse energy [µJ]
0 0.02 0.04 0.06 0.08
1nC
0 0.5 1.0 1.5 2.0 2.5 3.0 3.5 4.0
Qbunch [nC]
1.6
1.4
1.2
1.0
0.8
0.6
0.4
0.2
0
Q [nC], emitted bunch charge
experiment
experiment
RF@~6.5MW×650µs | RF@~4.8MW×600µs
1nC  European XFEL, PITZ ~320pC  FLASH, PITZ

## Slide 11
time
QE
Map, f2
Laser
Spot Map, f1
Temporal laser profile
intensity
(f1
f2)
(r, t)
y
x
Convolution
Modeling: Some Treatments in simulations
Treatment 3  modeling field(RF + space-charge) effects during emission through well-known Schottky effect
K. Jensen et al., J. Appl. Phys104, 044907 (2008)
Treatment 2  Bridging beam dynamics in vacuum with simplified effective cathode QE
for metals:
: effective cathode work function
: intrinsic work function
: Schottky term
: photon energy
: Fermi energy
: characteristic parameter
for semiconductors:
: electron affinity
: characteristic parameter
: reflection coefficient
: band gap
during emission, determined according to the RF field & the self-field of the beam at extraction, but, the latter is NOT prior known.
Treatment 1  Generating more "realistic" photoemission distribution according to cathode laser (and QE map)
*D. Dowell et al., PRST-AB 12 074201 (2009)

## Slide 12
time
QE
Map, f2
Laser
Spot Map, f1
Temporal laser profile
intensity
(f1
f2)
(r, t)
y
x
Convolution
Modeling: Some Treatments in simulations
Treatment 2  Bridging beam dynamics in vacuum with simplified effective cathode QE
for metals:
: effective cathode work function
: intrinsic work function
: Schottky term
: photon energy
: Fermi energy
: characteristic parameter
for semiconductors:
: electron affinity
: characteristic parameter
: reflection coefficient
: band gap
Treatment 1  Generating more "realistic" photoemission distribution according to cathode laser (and QE map)
Treatment 4  determining temporal emission profile based on a space-charge iteration approach (See poster for details)
Can self-consistently determine temporal emission profile according to local fields at cathode surface
For very high space-charge densities numerical convergence tricky
 Another relevant work: photoemission modeling based on a 3D Lienard-Wiechert approach [see details in NIM A 889, 129-137 (2018)]
K. Jensen et al., J. Appl. Phys104, 044907 (2008)
*D. Dowell et al., PRST-AB 12 074201 (2009)
Treatment 3  modeling field(RF + space-charge) effects during emission through well-known Schottky effect
during emission, determined according to the RF field & the self-field of the beam at extraction, but, the latter is NOT prior known.

## Slide 13
Modeling (Cont'd): Space-Charge Cooling Effect
At cathode
Space-charge fields cooling down cathode surface through an increased cathode work function
K. Flöttmann, TESLA-FEL report 1997-01, DESY, 1997
QE and intrinsic emittance:
Dump
Emittance @~5.277m
Simulation setup
Time-dependent photoemission effects influence downstream slice emittance
For higher charges the effect will be stronger
  Simulations in progress
Downstream at 5.277m
500pC
K. Jensen et al., J. Appl. Phys104, 044907 (2008)

## Slide 14
Modeling (Cont'd): "Emission Curve"
"Emission curve" (Q vs. Elas)
"Schottky scan" (Q vs. gun)
Characteristic emission measurements
18.3µJ
49.7µJ
76.5µJ
93.1µJ
113.3µJ
Conventional
Measured
Measured
Improved
Conventional
pancake
pancake
Improved
129.5µJ
Measured trans. laser distributions used for simulations at different laser pulse energies
Improved agreements with measurements
Machine parameters
In collaboration with Tsinghua University (H. Chen, Y.-Ch. Du, Ch.-X. Tang, et al.)
Emission curves measured for a copper cathode in an S-band NC RF gun
(Proceedings of LINACʹ18 , THPO116)

## Slide 15
Observation and analysis of a photocathode effect
Spiky photo-emitted electron bunch trains (Q-train) from a fresh Cs2Te photocathode
Observation at FLASH (S. Lederer & S. Schreiber)
Cathode drive UV laser
Cathode #73.3
in fresh state
∆Q ~10%
~tens of µs
1 MHz repetition rate

Charge measured at gun exit
A flat energy distribution of the laser pulse train produces a "spike" at the head of the electron bunch train emitted from a fresh cathode
The spike depends on laser energy density and accelerating field on cathode
The spike "vanishes" over long operation time (year)
S. Lederer, et al., European Workshop on Photocathodes for Particle Accelerator Applications (EWPAA), Daresbury, 2016
S. Lederer, S. Schreiber, et al., FEL’15

## Slide 16
Observation and analysis of a photocathode effect
Spiky photo-emitted electron bunch trains (Q-train) from a fresh Cs2Te photocathode
Observation at FLASH (S. Lederer & S. Schreiber)
Cathode drive UV laser
S. Lederer, et al., European Workshop on Photocathodes for Particle Accelerator Applications (EWPAA), Daresbury, 2016
two laser operation to explore the effect
Laser 2
Laser 1
L1 only (red) as reference
Q-train effect "restarted" as delay time increases
S. Lederer, S. Schreiber, et al., FEL’15
A flat energy distribution of the laser pulse train produces a "spike" at the head of the electron bunch train emitted from a fresh cathode
The spike depends on laser energy density and accelerating field on cathode
The spike "vanishes" over long operation time (year)
delay
Cathode #73.3
in fresh state
∆Q ~10%
~tens of µs
1 MHz repetition rate

Charge measured at gun exit

## Slide 17
Observation and analysis of a photocathode effect
Spiky photo-emitted electron bunch trains (Q-train) from a fresh Cs2Te photocathode
Observation at FLASH (S. Lederer & S. Schreiber)
Cathode drive UV laser
long-term average QE not really changing
average
S. Lederer, et al., European Workshop on Photocathodes for Particle Accelerator Applications (EWPAA), Daresbury, 2016
S. Lederer, et al., EWPAA, Helmholtz-Zentrum Berlin, Germany, 2017
A flat energy distribution of the laser pulse train produces a "spike" at the head of the electron bunch train emitted from a fresh cathode
The spike depends on laser energy density and accelerating field on cathode
The spike "vanishes" over long operation time (year)
Cathode #73.3
in fresh state
∆Q ~10%
~tens of µs
1 MHz repetition rate

Charge measured at gun exit

## Slide 18
Observation and analysis of a photocathode effect
Spiky photo-emitted electron bunch trains (Q-train) from a fresh Cs2Te photocathode
Observation at FLASH (S. Lederer & S. Schreiber)
Cathode drive UV laser
One hypothesis
temporal variation of cathode band bending potential
Extracted photoelectrons recombine with the holes (e.g., from defects) at the surface state dynamically changing the band bending level, and therefore, the cathode work function, QE[(t)]  Q(t)
  0.4 eV change of bending potential (green) over ~90µs may result in spiky Q-train effect (red)
Microscopic modeling of dEband(t) needed
Photoemission model
measurement
simulation
Vac. level from bulk
e-
Surface
states
dEband
p-type semiconductor
Experimental studies reveal cathode effects
A flat energy distribution of the laser pulse train produces a "spike" at the head of the electron bunch train emitted from a fresh cathode
The spike depends on laser energy density and accelerating field on cathode
The spike "vanishes" over long operation time (year)
Cathode #73.3
in fresh state
∆Q ~10%
~tens of µs
1 MHz repetition rate

Charge measured at gun exit

## Slide 19: Summary
The PITZ facility is used to characterize and study space-charge dominated photoemission
  Important for clarifying discrepancies between measurement and simulation at the working points of European XFEL and FLASH
  Essential for
    Understanding slice emittance formation at cathode (including "green" photocathodes R&D for CW upgrade of European-XFEL)
    Advanced (e.g. ellipsoidal) cathode laser pulse shaping (benefiting high charge beams or CW guns)
Space-charge iteration approach used to take into accounts space-charge contributions onto photoemission through well-known Schottky effect
   Emission curve simulated with improved agreement to measurement
   Space-charge can COOL the intrinsic (surface) emittance
Microseconds level "Q-train" effect observed at FLASH and analyzed at PITZ: spiky photo-emitted electron bunch trains from a fresh Cs2Te photocathode may originate from the change of band bending potential
Outlook: more detailed PE modeling
  Modeling of possible field penetrating effects (e.g. on
  electron mobility)
  Open for new joint work!
PITZ Group 2015
PITZ Collaboration Meeting 2018

## Slide 20: Backup Slide on "Core + Halo" model
"Core + Halo" model
measurement
simulation
Temp. Gaussian case fairly explained
  Trans. emission profile does play a role

## Slide 21: Development of Green cathodes on INFN LASA plug design
Goal: grow reliable “green” cathodes (K-Cs-Sb compound) on INFN plugs and test them in the PITZ RF-Gun (high cathode gradient + fairly high duty cycle)
  First sequential deposition on test sample in week 47/2017 (“proof of principle”)
    Sb 10 nm
    K until max QE
    Cs until max QE
    Repeated on 1 Dec 2017
  Long term measurement
    Total extracted charge over more than 3 months
    QE versus time
      Base system pressure: low 10-10 mbar
      QE decrease depends on light power density (fatigue effect?)
     still reasonable QE
  Next: Design new source layout in view of co-evaporation in the near future
View into the prep chamber
Aim:  better beam quality,  simplified photo cathode laser.  especially needed for CW operation
(full light spectrum)
No light
        broad band LED power density ()
        Laser Driven Light Source power density ()
F. Stephan, 18th Advanced Accelerator Concepts Workshop (AACʹ18)