## Slide 1: Towards adaptive, automated growth of photocathodes
Vitaly Pavlenko, Alexander Scheinker, Mark A. Hoffbauer, Fangze Liu, and Nathan A. Moody
Los Alamos National Laboratory
Photocathode Physics for Photoinjectors (P3) 2018
October 16th, 2018

## Slide 2
Definitions
Slide 2
Photocathodes = Alkali Antimonide Photocathodes
  Cs3Sb = Single parameter system
  K2CsSb = Two-parameter system
Growth = Co-evaporation at a low substrate temperature
  Co-evaporation = True co-evaporation
  Low = Temperature at which cathode is stable
Automated = Feedback-based process control
Towards = Ultimate goal is stoichiometric single crystal
Notes: 2

## Slide 3
Benefits of Automation
Slide 3
Reproducibility: you always get the same thing
Accuracy & Flexibility: you can specify exactly what you want
Cost: you can do something more important instead
Notes: 3

## Slide 4
How Important is Flux Control?
Slide 4
Intuitive adjustment
Notes: 4

## Slide 5
Rudimentary Model for Single Parameter System
Slide 5
Assumption: Extremum
Consequences:
(local) minimum
Oscillations vanish at extremum
Frequency doubles at extremum
Phase shift by p at extremum
Notes: 5

## Slide 6
Choice of Thickness-Independent Quality Parameter
Slide 6
Data from:
L. Cultrera et al., Applied Physics Letters, 99, 152110, 2011.
Chart: Photon Energy (eV)
QE | 0.001 | 0.01 | 0.1 | 1
QE | 0.001 | 0.01 | 0.1 | 1
QE | 0.001 | 0.01 | 0.1 | 1
QE | 0.001 | 0.01 | 0.1 | 1
QE | 0.001 | 0.01 | 0.1 | 1
QE405nm/QE532nm
1.8
5.2
Ethreshold(eV)
2.2
2.0
Physically significant parameter, lower is better
Engineering parameter, lower is better
Cs3Sb
≥50 nm thick
Non-stoichiometric Cs3Sb
<50 nm thick
Notes: 6

## Slide 7
Flux Control and Calibration
Slide 7
Notes: 7

## Slide 8
Towards Automated Growth
Slide 8
Observations:
+ (local) minimum
+/- Oscillations vanish at extremum
- Frequency doubles at extremum
- Phase shift by p at extremum
GOAL
Notes: 8

## Slide 9
Choice of Thickness-Independent Quality Parameter: Experiment
Slide 9
QE Ratio
Easy to implement
No ambiguity
Advantages
Work Function
Physically significant
Potentially universal metric
Notes: 9

## Slide 10
Conclusions / Future Plans
Slide 10
Precise flux control is critical for low substrate temperature co-evaporation of alkali antimonides
Thickness-independent real-time quality parameter can be based on photoemissive properties
Response of the growing cathode system to flux ratio modulation indicates potential for feedback-based control methods
Next step: integration of adaptive control algorithm into growth procedure
Notes: 10