## Slide 1: Computational Screening for New Photocathode Materials
Joshua T. Paul, Alice Galdi, Siddharth Karkare, Howard Padmore, Ivan Bazarov, Richard G. Hennig

## Slide 2: Motivation
Common photocathode materials: GaAs, InGaAs, CsTe, CsI, SbCs, Sb-K-Cs, Na-K-Sb
New photocathodes are typically identify based on trial and error efforts on what photocathodes already exist

## Slide 3: Motivation
Computational resources have the ability to improve the search for photocathode materials
  Materials databases (MaterialsProject, AFlowLib, OQMD)
  Density functional theory (DFT)
  High-throughput techniques
  Supercomputers (HiPerGator, XSEDE)
  Materials science software (Pymatgen, MPInterfaces)

## Slide 4: Computational Path to Find Photocathodes
Screen MaterialsProject database
Identify surface states
Match candidates to commercial substrates
Calculate effective mass
Estimate MTE
Validating
Software Complete Validating
Calculating
Software Complete

## Slide 5: MaterialsProject Database
Using materials databases, we can search for photocathodes never before considered
Jain, PRL 115 036402 (2015)

## Slide 6: Initial Screening Criteria
Need to reduce the number of materials considered for calculations to a more reasonable number
Total number of starting materials | 69,640
No radioactive elements | 66,119
Hull distance 50 meV/atom | 43,087
Contains band gap 4 eV | 38,019
Effective mass 0.2me | 517
Total number of starting materials | 69,640
No radioactive elements | 66,119
 | 43,087
 | 38,019
 | 517
Hull distance: Sun et al. Sci. Adv. 2016; 2, 11, e1600225

## Slide 7: Approximating the Effective Mass
By fitting the points near an extrema to a parabola, a second derivative gives one an approximation of the effective mass
Performed for select systems in Kim et al. PHYS. REV. B. 80, 035203

## Slide 8: Approximating the Effective Mass: Convergence
The default k-point density in MaterialsProject is sufficient for their purposes, but fairly low for fitting to equations. Thus, we re-calculate the effective mass using higher density meshes.
Potentially low m* materials
GaAs | BaLiAs | GeSe
Cs3BiN | Na3As | NaZnAs

## Slide 9: Approximating the Effective Mass: Convergence
Using MaterialsProject data to estimate m* is insufficient for screening, but it does allow for narrowing the scope of the investigation

## Slide 10: Estimating MTE: Probability of Optical Excitation
When calculating dielectric response in VASP, the optical excitation probability is calculated. This can be explicitly written out to obtain the strength of transition from one band to another at a given k-point
M. Gajdoš, PHYS. REV. B 73, 045112 (2006)

## Slide 11: Estimating MTE: Relevant Optical Transitions
Emission if
For a more detailed derivation, refer to Karakare et al., PHYS. REV. B 95, 075439 (2017)

## Slide 12: Estimating MTE: Relevant Optical Transitions
(100)
(010)
(001)

## Slide 13: Matching Photocathodes to Substrates
Using MPInterfaces software package, we can epitaxially match potential photocathodes to other materials
With our database of commercial substrates, we can match the screened photocathodes to easily obtained substrates to optimize growth conditions
Cs3Sb on (100) MgO

## Slide 14: Summary
Using a computational approach, we can identify photocathodes that have not been considered before
Effective masses can be estimated from band curvatures, which is currently being validated for over 500 materials
Using transition rates and focusing on relevant transitions for emission, we can approximate MTE for emission
Using MPInterfaces, we can epitaxially match candidate photocathodes to a variety of commercially available materials to help optimize growth conditions

## Slide 15: Acknowledgments
Center for Bright Beams and the National Science Foundation for funding this project
The HiPerGator supercomputer, where these calculations are being performed
The MaterialsProject database for providing the initial database of structures