## Slide 1
Advanced XRF Tools and Methodologies for the Revisualization of Vanished Ancient Polychrome
Eva Eleftheriou, MSc Student INPP Annual Meeting, 2021

## Slide 2
Introduction
The two research projects
XRF experimental equipment and methodologies
Results
Conclusions

## Slide 3
Research Projects Aim of the research
The marble throne at the tomb of Queen Eurydice I at Aigai
Cycladic Figurines (National Archaeological Museum, Museum of Cycladic Art)
Identification of the pigments used on the throne
Characterization of the throne’s gold leafs
NAM 6165
NG252, MCA
Investigation of the existence of patterned polychrome on Early Cycladic marble figurines
Characterization of the pigments’ chemical composition

## Slide 4
Methods Handheld XRF Spot Analysis of the marble throne
HH-XRF analyzer (Niton XL3t GOLDD+)
29 selected spots of interest (dark blue area at the front bottom, right side & painted panel)
Two measurement conditions: 50 kV, 40 μA (Main) 8 kV, 200 μA (Light)
About 20 sec per measurement
Ag-target X-ray transmission tube
50 kV max voltage & 200 μA max current
SDD 30 mm2 active area
Energy resolution 178 eV at 5.9 keV
Offers different excitation conditions for elemental sensitivity optimization
Choice of spot size (3 mm / 8 mm)
Spot #532

## Slide 5
Methods Macro-XRF Imaging of the Cycladic Figurines
30W Rh-target X-ray tube coupled to a polycapillary lens
26μm spot diameter at Rh Kα-line, 1cm focus distance
two 50 mm2 active area SDDs
energy resolution 133eV at 5.9keV
time-list event mode
Two digital X-ray Processors
DSP with 40ns time resolution
3-axis fast scanner
LANDIS-X Scanner
30 scans on coloured areas from 14 figurines and vessels
Unfiltered 40kV excitation at 400μA
Non-invasive
Detailed mapping of the elemental distribution of samples
Capability of visualizing the distribution of chemical elements on the entire surface in images of easy understanding and interpretation
The MA-XRF Imaging Technique
NAM3909

## Slide 6
Results The marble throne
Identified pigments: cinnabar, HgS iron-based ochres, FexOy
Egyptian blue, CaCuSi4O10
lead white, 2PbCO3·Pb(OH)2 murex purple, C16H8Br2N2O2
Gold leafs on marble throne |  |  |  |  |  |  | 
XRF Reading | Thickness(μm) | Live time (s) | Current (μA) | Lα | Lβ | Lα/Lβ | σ(Lα/Lβ)
519 | 1.08 | 11.22 | 40.04 | 6057.57 | 5607.70 | 1.08 | 0.02
547 | 0.76 | 20.59 | 39.98 | 21772.10 | 19718.50 | 1.10 | 0.01
IAEA Reference Gold foils |  | 
Thickness (μm) | Lα/Lβ | σ(La/Lb)
0.0238 | 1.155 | 0.011
0.162 | 1.130 | 0.002
1.1 | 1.055 | 0.002
2.2 | 1.020 | 0.002
3.3 | 0.989 | 0.001
3.58 | 0.982 | 0.001
5.4 | 0.935 | 0.001
6.5 | 0.909 | 0.001
7.2 | 0.902 | 0.001
7.89 | 0.886 | 0.001
19.6 | 0.811 | 0.001
39.2 | 0.799 | 0.001
Gold leafs analysis – Thickness estimation using the Au Lα/Lβ intensity ratios

## Slide 7
Results Cycladic Figurines
As
Detection of an arsenic-based pigment; orpiment (As2S3) or realgar (As4S4). Earliest occurrence in Greek polychrome!
Hg
Identification of degraded cinnabar (HgS).
Phase transition to metacinnabar (α’-HgS)
Conversion into corderoite (Hg3S2Cl2)
NG304, MCA
6165, NAM
(R. Nöller, 2015, Birtacha, 2016)
(Da Pieve et al., 2013)

## Slide 8
Results Cycladic Figurines
Hg
Fe
Pb
Mn
Evidence of mixing of pigments or forming a paint layer stratigraphy!
NG252, MCA
Hg
Pb
Mn
Mixing or overpainting of cinnabar (HgS), lead white (Pb-2PbCO₃·Pb (OH)₂) and umber (Fe2O3·MnO2)
Hg
Fe
Hg
Fe
Ca
Mixing or overpainting of cinnabar (HgS) and red ochre
NG251, MCA

## Slide 9
Results Monte Carlo Simulations
5 cm Marble layer
1.75 μm Red ochre layer
0.7 μm Gold leaf layer
0.16 μm Cinnabar layer
Concentration estimation for gold leaf #547: 86.63% Au, 9.33% Ag, 4.04% Cu
Gold leaf thickness determined at 0.7 μm via MCS - 8% difference with the one calculated via the Au Lα/Lβ ratios
Simulated stratigraphy for #547
Spot #547

## Slide 10
Conclusions
Pigments identified by MA-XRF imaging of Cycladic Figurines and Vessels:
Cinnabar (6/11 Figurines, 1/3 Vessels)
Iron-based ochre (3/11 Figurines, 3/3 Vessels)
Lead white (3/12 Figurines, 1/3 Vessels)
Possible identification of Murex purple (1/3 Vessels)
Umber (Fe2O3·MnO2) (4/11 Figurines, 1/3 Vessels)
Orpiment (As2S3) or Realgar (As4S4) (1/11 Figurines)
Contaminants: Lithopone (BaSO4∙ZnS) (2/11 Figurines)
Indication that various pigments (cinnabar, lead white, umbra and iron-based ochre) were not only applied as single paint layers, but also by following a more complex elaboration (mixing or forming a paint layer stratigraphy)
Pigments identified by HH-XRF on the marble throne:
Cinnabar (HgS)
Iron-based ochres (FexOy)
Lead white (2PbCO3·Pb(OH)2)
Possible identification of organic Murex purple (C16H8Br2N2O2)
Egyptian blue (CaCuSi4O10)
Determination of the gold leafs’ thicknesses at 1.08 μm & 0.76 μm via the Au Lα/Lβ ratios
MC Simulations suggest gold leaf concentrations at
88.88% Au, 10.32% Ag, 0.80% Cu, 0.4 μm thick
86.63% Au, 9.33% Ag, 4.04% Cu, 0.7 μm thick

## Slide 11
Collaborators
Dr. Hariclia Brecoulaki, archaeologist
Dr. Claudia Caliri, Dr. Fransesco Paolo Romano, Kalliopi Tsampa, Dr. Sofia Sotiropoulou, Dr. Andreas G. Karydas
Dr. Katia Manteli, curator of the Collection of Prehistoric Antiquities of the National Archaeological Museum
Dr. Nikolas Papadimitriou, curator of Cycladic and Ancient Greek Art Collections of the Museum of Cycladic Art
Dr. Kiki Birtacha, archaeologist

## Slide 12
Thank you for your attention!